|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	03src0648

Empirical formula 	C24H14Br2FeO2

Formula weight 	550.02

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	Pc

Unit cell dimensions	a = 15.9575(4) Å	( = 90°

b = 8.8522(2) Å	( = 101.9050(10)°

c = 13.7492(3) Å	(  = 90°

Volume	1900.42(8) Å3

Z	4

Density (calculated)	1.922 Mg / m3

Absorption coefficient	5.018 mm(1

F(000)	1080

Crystal	Plate; Dark Grey

Crystal size	0.26 ( 0.12 ( 0.01 mm3

( range for data collection	2.91 ( 27.48°

Index ranges	(20 ( h ( 19, (11 ( k ( 11, (17 ( l ( 16

Reflections collected	24120

Independent reflections	7305 [Rint = 0.0935]

Completeness to ( = 27.48°	99.7 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9515 and 0.3553

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	7305 / 2 / 524

Goodness-of-fit on F2	1.033

Final R indices [F2 > 2((F2)]	R1 = 0.0445, wR2 = 0.0999

R indices (all data)	R1 = 0.0538, wR2 = 0.1057

Absolute structure parameter	(0.014(11)

Extinction coefficient	0.0017(3)

Largest diff. peak and hole	0.886 and (0.606 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

All hydrogen atoms were fixed.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	9993(5)	864(7)	434(5)	23(1)	1

C2	10584(4)	(42(7)	4(5)	20(1)	1

C3	10062(5)	(1034(7)	(693(5)	24(2)	1

C4	9182(5)	(766(8)	(674(5)	26(2)	1

C5	9143(4)	420(7)	24(5)	22(1)	1

C6	9103(4)	(2431(7)	1558(4)	17(1)	1

C7	9767(4)	(1536(7)	2176(5)	20(1)	1

C8	10560(4)	(2059(8)	2028(5)	22(1)	1

C9	10421(5)	(3263(8)	1349(5)	22(1)	1

C10	9537(5)	(3516(7)	1051(5)	20(1)	1

C11	8173(4)	(2236(7)	1415(4)	17(1)	1

C12	7805(4)	(1305(7)	2046(5)	21(1)	1

C13	6937(4)	(1156(7)	1918(5)	19(1)	1

C14	6568(4)	(172(7)	2611(5)	20(1)	1

C15	5622(4)	(65(7)	2481(5)	20(1)	1

C16	5268(5)	830(8)	3120(5)	23(1)	1

C17	4381(4)	948(7)	2996(5)	22(1)	1

C18	3850(5)	144(7)	2232(5)	19(1)	1

C19	4199(5)	(767(8)	1592(5)	23(1)	1

C20	5077(4)	(874(7)	1716(4)	18(1)	1

C21	5447(4)	(1812(8)	999(5)	21(1)	1

C22	6377(4)	(1945(7)	1145(5)	19(1)	1

C23	6739(4)	(2873(7)	518(5)	19(1)	1

C24	7618(4)	(2988(7)	645(5)	18(1)	1

O1	7043(4)	553(7)	3266(4)	40(1)	1

O2	4963(3)	(2408(6)	290(4)	30(1)	1

Fe1	9838(1)	(1353(1)	717(1)	17(1)	1

Br1	10353(1)	2361(1)	1404(1)	31(1)	1

Br2	2651(1)	344(1)	2059(1)	25(1)	1

C31	2802(5)	(4097(8)	(1324(5)	24(2)	1

C32	2237(4)	(5008(7)	(2038(5)	20(1)	1

C33	2772(5)	(6028(8)	(2442(5)	25(2)	1

C34	3640(5)	(5727(8)	(1994(5)	26(2)	1

C35	3664(4)	(4538(7)	(1279(5)	24(1)	1

C36	3710(4)	(7389(7)	261(4)	16(1)	1

C37	3052(5)	(6481(8)	568(5)	23(1)	1

C38	2249(4)	(6996(8)	64(5)	21(1)	1

C39	2374(5)	(8191(8)	(558(5)	23(1)	1

C40	3269(4)	(8473(7)	(440(5)	20(1)	1

C41	4635(4)	(7203(7)	560(4)	18(1)	1

C42	5004(4)	(6294(7)	1370(4)	18(1)	1

C43	5881(4)	(6141(7)	1673(4)	20(1)	1

C44	6248(5)	(5145(7)	2531(5)	21(1)	1

C45	7187(4)	(5067(8)	2855(5)	19(1)	1

C46	7556(4)	(4163(8)	3665(5)	22(1)	1

C47	8442(4)	(4053(7)	3979(5)	20(1)	1

C48	8964(5)	(4883(7)	3463(5)	20(2)	1

C49	8613(4)	(5770(8)	2663(5)	21(1)	1

C50	7730(4)	(5870(7)	2351(4)	18(1)	1

C51	7364(5)	(6821(8)	1459(5)	24(1)	1

C52	6429(4)	(6934(7)	1167(5)	19(1)	1

C53	6071(5)	(7853(8)	361(5)	21(1)	1

C54	5188(5)	(7990(8)	51(5)	23(2)	1

O31	5777(3)	(4414(7)	2948(4)	38(1)	1

O32	7843(3)	(7435(6)	989(4)	30(1)	1

Fe31	2966(1)	(6308(1)	(932(1)	18(1)	1

Br31	2410(1)	(2595(1)	(550(1)	33(1)	1

Br32	10161(1)	(4711(1)	3864(1)	24(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C5	1.414(10)

C1(C2	1.453(9)

C1(Br1	1.884(7)

C1(Fe1	2.026(7)

C2(C3	1.434(10)

C2(Fe1	2.052(6)

C2(H2	0.9500

C3(C4	1.429(10)

C3(Fe1	2.063(6)

C3(H3	0.9500

C4(C5	1.433(9)

C4(Fe1	2.049(7)

C4(H4	0.9500

C5(Fe1	2.041(6)

C5(H5	0.9500

C6(C10	1.445(9)

C6(C7	1.450(9)

C6(C11	1.466(9)

C6(Fe1	2.044(6)

C7(C8	1.400(10)

C7(Fe1	2.039(6)

C7(H7	0.9500

C8(C9	1.404(10)

C8(Fe1	2.028(7)

C8(H8	0.9500

C9(C10	1.403(10)

C9(Fe1	2.036(7)

C9(H9	0.9500

C10(Fe1	2.049(6)

C10(H10	0.9500

C11(C24	1.401(9)

C11(C12	1.409(9)

C12(C13	1.367(10)

C12(H12	0.9500

C13(C22	1.422(9)

C13(C14	1.498(9)

C14(O1	1.230(9)

C14(C15	1.486(9)

C15(C16	1.388(9)

C15(C20	1.414(9)

C16(C17	1.394(10)

C16(H16	0.9500

C17(C18	1.401(10)

C17(H17	0.9500

C18(C19	1.391(9)

C18(Br2	1.887(7)

C19(C20	1.379(10)

C19(H19	0.9500

C20(C21	1.500(9)

C21(O2	1.232(8)

C21(C22	1.460(9)

C22(C23	1.399(9)

C23(C24	1.381(9)

C23(H23	0.9500

C24(H24	0.9500

C31(C35	1.419(10)

C31(C32	1.436(10)

C31(Br31	1.888(7)

C31(Fe31	2.032(7)

C32(C33	1.431(10)

C32(Fe31	2.064(6)

C32(H32	0.9500

C33(C34	1.421(10)

C33(Fe31	2.050(6)

C33(H33	0.9500

C34(C35	1.435(10)

C34(Fe31	2.049(7)

C34(H34	0.9500

C35(Fe31	2.035(7)

C35(H35	0.9500

C36(C40	1.437(9)

C36(C37	1.452(9)

C36(C41	1.457(9)

C36(Fe31	2.053(6)

C37(C38	1.401(10)

C37(Fe31	2.045(6)

C37(H37	0.9500

C38(C39	1.399(10)

C38(Fe31	2.050(6)

C38(H38	0.9500

C39(C40	1.427(10)

C39(Fe31	2.034(7)

C39(H39	0.9500

C40(Fe31	2.057(6)

C40(H40	0.9500

C41(C42	1.402(9)

C41(C54	1.417(9)

C42(C43	1.383(9)

C42(H42	0.9500

C43(C52	1.411(9)

C43(C44	1.492(8)

C44(O31	1.222(8)

C44(C45	1.474(9)

C45(C46	1.399(9)

C45(C50	1.408(9)

C46(C47	1.394(10)

C46(H46	0.9500

C47(C48	1.408(9)

C47(H47	0.9500

C48(C49	1.373(10)

C48(Br32	1.881(7)

C49(C50	1.388(9)

C49(H49	0.9500

C50(C51	1.503(9)

C51(O32	1.225(8)

C51(C52	1.467(10)

C52(C53	1.398(9)

C53(C54	1.391(10)

C53(H53	0.9500

C54(H54	0.9500

C5(C1(C2	109.6(6)

C5(C1(Br1	127.2(5)

C2(C1(Br1	123.2(5)

C5(C1(Fe1	70.2(4)

C2(C1(Fe1	70.1(4)

Br1(C1(Fe1	125.2(3)

C3(C2(C1	105.9(6)

C3(C2(Fe1	70.0(4)

C1(C2(Fe1	68.2(3)

C3(C2(H2	127.1

C1(C2(H2	127.1

Fe1(C2(H2	126.3

C4(C3(C2	108.9(6)

C4(C3(Fe1	69.1(4)

C2(C3(Fe1	69.2(3)

C4(C3(H3	125.6

C2(C3(H3	125.6

Fe1(C3(H3	127.7

C3(C4(C5	108.3(6)

C3(C4(Fe1	70.2(4)

C5(C4(Fe1	69.2(4)

C3(C4(H4	125.9

C5(C4(H4	125.9

Fe1(C4(H4	126.3

C1(C5(C4	107.4(6)

C1(C5(Fe1	69.1(4)

C4(C5(Fe1	69.8(4)

C1(C5(H5	126.3

C4(C5(H5	126.3

Fe1(C5(H5	126.4

C10(C6(C7	106.3(6)

C10(C6(C11	125.9(6)

C7(C6(C11	127.7(6)

C10(C6(Fe1	69.5(3)

C7(C6(Fe1	69.0(3)

C11(C6(Fe1	123.5(4)

C8(C7(C6	107.9(6)

C8(C7(Fe1	69.4(4)

C6(C7(Fe1	69.4(3)

C8(C7(H7	126.1

C6(C7(H7	126.1

Fe1(C7(H7	126.7

C7(C8(C9	108.9(6)

C7(C8(Fe1	70.3(4)

C9(C8(Fe1	70.1(4)

C7(C8(H8	125.5

C9(C8(H8	125.5

Fe1(C8(H8	125.7

C10(C9(C8	109.1(6)

C10(C9(Fe1	70.4(4)

C8(C9(Fe1	69.5(4)

C10(C9(H9	125.4

C8(C9(H9	125.4

Fe1(C9(H9	126.3

C9(C10(C6	107.8(6)

C9(C10(Fe1	69.4(4)

C6(C10(Fe1	69.1(3)

C9(C10(H10	126.1

C6(C10(H10	126.1

Fe1(C10(H10	126.9

C24(C11(C12	117.7(6)

C24(C11(C6	120.7(6)

C12(C11(C6	121.7(6)

C13(C12(C11	121.2(6)

C13(C12(H12	119.4

C11(C12(H12	119.4

C12(C13(C22	120.8(6)

C12(C13(C14	119.7(6)

C22(C13(C14	119.5(6)

O1(C14(C15	120.8(6)

O1(C14(C13	120.4(6)

C15(C14(C13	118.8(6)

C16(C15(C20	119.5(6)

C16(C15(C14	119.7(6)

C20(C15(C14	120.8(6)

C15(C16(C17	120.0(6)

C15(C16(H16	120.0

C17(C16(H16	120.0

C16(C17(C18	119.7(6)

C16(C17(H17	120.1

C18(C17(H17	120.1

C19(C18(C17	120.6(7)

C19(C18(Br2	120.2(5)

C17(C18(Br2	119.2(5)

C20(C19(C18	119.4(6)

C20(C19(H19	120.3

C18(C19(H19	120.3

C19(C20(C15	120.7(6)

C19(C20(C21	119.0(6)

C15(C20(C21	120.2(6)

O2(C21(C22	121.9(6)

O2(C21(C20	119.3(6)

C22(C21(C20	118.8(6)

C23(C22(C13	118.3(6)

C23(C22(C21	120.0(6)

C13(C22(C21	121.8(6)

C24(C23(C22	120.1(6)

C24(C23(H23	119.9

C22(C23(H23	119.9

C23(C24(C11	121.9(6)

C23(C24(H24	119.0

C11(C24(H24	119.0

C1(Fe1(C8	113.6(3)

C1(Fe1(C9	145.4(3)

C8(Fe1(C9	40.4(3)

C1(Fe1(C7	107.5(3)

C8(Fe1(C7	40.3(3)

C9(Fe1(C7	68.1(3)

C1(Fe1(C5	40.7(3)

C8(Fe1(C5	143.8(3)

C9(Fe1(C5	173.9(3)

C7(Fe1(C5	112.7(3)

C1(Fe1(C6	131.9(3)

C8(Fe1(C6	68.9(3)

C9(Fe1(C6	68.7(3)

C7(Fe1(C6	41.6(3)

C5(Fe1(C6	107.7(3)

C1(Fe1(C4	68.5(3)

C8(Fe1(C4	174.4(3)

C9(Fe1(C4	135.2(3)

C7(Fe1(C4	144.9(3)

C5(Fe1(C4	41.0(3)

C6(Fe1(C4	113.9(3)

C1(Fe1(C10	172.8(3)

C8(Fe1(C10	68.2(3)

C9(Fe1(C10	40.2(3)

C7(Fe1(C10	69.1(3)

C5(Fe1(C10	133.9(3)

C6(Fe1(C10	41.4(2)

C4(Fe1(C10	110.4(3)

C1(Fe1(C2	41.7(3)

C8(Fe1(C2	108.7(3)

C9(Fe1(C2	114.5(3)

C7(Fe1(C2	132.1(3)

C5(Fe1(C2	69.8(3)

C6(Fe1(C2	172.5(2)

C4(Fe1(C2	69.2(3)

C10(Fe1(C2	145.2(2)

C1(Fe1(C3	68.6(3)

C8(Fe1(C3	134.5(3)

C9(Fe1(C3	111.2(3)

C7(Fe1(C3	172.5(3)

C5(Fe1(C3	68.8(3)

C6(Fe1(C3	145.7(3)

C4(Fe1(C3	40.7(3)

C10(Fe1(C3	115.6(3)

C2(Fe1(C3	40.8(3)

C35(C31(C32	109.9(6)

C35(C31(Br31	126.9(6)

C32(C31(Br31	123.1(5)

C35(C31(Fe31	69.7(4)

C32(C31(Fe31	70.7(4)

Br31(C31(Fe31	124.6(3)

C33(C32(C31	106.3(6)

C33(C32(Fe31	69.1(4)

C31(C32(Fe31	68.3(4)

C33(C32(H32	126.9

C31(C32(H32	126.9

Fe31(C32(H32	127.2

C34(C33(C32	108.6(6)

C34(C33(Fe31	69.7(4)

C32(C33(Fe31	70.2(4)

C34(C33(H33	125.7

C32(C33(H33	125.7

Fe31(C33(H33	126.0

C33(C34(C35	108.7(6)

C33(C34(Fe31	69.8(4)

C35(C34(Fe31	68.9(4)

C33(C34(H34	125.6

C35(C34(H34	125.6

Fe31(C34(H34	127.3

C31(C35(C34	106.4(6)

C31(C35(Fe31	69.5(4)

C34(C35(Fe31	70.0(4)

C31(C35(H35	126.8

C34(C35(H35	126.8

Fe31(C35(H35	125.4

C40(C36(C37	106.4(6)

C40(C36(C41	126.2(5)

C37(C36(C41	127.4(6)

C40(C36(Fe31	69.7(4)

C37(C36(Fe31	68.9(4)

C41(C36(Fe31	123.9(4)

C38(C37(C36	108.6(6)

C38(C37(Fe31	70.2(4)

C36(C37(Fe31	69.5(3)

C38(C37(H37	125.7

C36(C37(H37	125.7

Fe31(C37(H37	126.1

C39(C38(C37	108.5(6)

C39(C38(Fe31	69.3(4)

C37(C38(Fe31	69.8(4)

C39(C38(H38	125.8

C37(C38(H38	125.8

Fe31(C38(H38	126.7

C38(C39(C40	109.2(6)

C38(C39(Fe31	70.6(4)

C40(C39(Fe31	70.5(4)

C38(C39(H39	125.4

C40(C39(H39	125.4

Fe31(C39(H39	125.1

C39(C40(C36	107.4(6)

C39(C40(Fe31	68.7(4)

C36(C40(Fe31	69.4(4)

C39(C40(H40	126.3

C36(C40(H40	126.3

Fe31(C40(H40	127.2

C42(C41(C54	118.2(6)

C42(C41(C36	121.6(6)

C54(C41(C36	120.2(6)

C43(C42(C41	121.9(6)

C43(C42(H42	119.0

C41(C42(H42	119.0

C42(C43(C52	119.6(6)

C42(C43(C44	120.3(6)

C52(C43(C44	120.1(6)

O31(C44(C45	121.3(6)

O31(C44(C43	120.3(6)

C45(C44(C43	118.4(6)

C46(C45(C50	118.7(6)

C46(C45(C44	120.1(6)

C50(C45(C44	121.2(6)

C47(C46(C45	121.3(6)

C47(C46(H46	119.4

C45(C46(H46	119.4

C46(C47(C48	118.4(6)

C46(C47(H47	120.8

C48(C47(H47	120.8

C49(C48(C47	121.0(7)

C49(C48(Br32	120.2(5)

C47(C48(Br32	118.8(5)

C48(C49(C50	120.3(6)

C48(C49(H49	119.8

C50(C49(H49	119.8

C49(C50(C45	120.2(6)

C49(C50(C51	119.1(6)

C45(C50(C51	120.6(6)

O32(C51(C52	122.4(6)

O32(C51(C50	120.0(6)

C52(C51(C50	117.6(6)

C53(C52(C43	119.2(6)

C53(C52(C51	118.9(6)

C43(C52(C51	122.0(6)

C54(C53(C52	121.1(6)

C54(C53(H53	119.5

C52(C53(H53	119.5

C53(C54(C41	120.0(6)

C53(C54(H54	120.0

C41(C54(H54	120.0

C31(Fe31(C39	144.6(3)

C31(Fe31(C35	40.8(3)

C39(Fe31(C35	174.5(3)

C31(Fe31(C37	108.5(3)

C39(Fe31(C37	67.7(3)

C35(Fe31(C37	111.6(3)

C31(Fe31(C34	68.1(3)

C39(Fe31(C34	136.5(3)

C35(Fe31(C34	41.1(3)

C37(Fe31(C34	143.3(3)

C31(Fe31(C38	113.8(3)

C39(Fe31(C38	40.1(3)

C35(Fe31(C38	142.5(3)

C37(Fe31(C38	40.0(3)

C34(Fe31(C38	176.1(3)

C31(Fe31(C33	68.4(3)

C39(Fe31(C33	112.0(3)

C35(Fe31(C33	69.3(3)

C37(Fe31(C33	174.5(3)

C34(Fe31(C33	40.6(3)

C38(Fe31(C33	136.4(3)

C31(Fe31(C36	133.0(3)

C39(Fe31(C36	68.8(3)

C35(Fe31(C36	107.0(3)

C37(Fe31(C36	41.5(3)

C34(Fe31(C36	112.6(3)

C38(Fe31(C36	68.8(2)

C33(Fe31(C36	143.9(3)

C31(Fe31(C40	173.3(3)

C39(Fe31(C40	40.8(3)

C35(Fe31(C40	133.7(3)

C37(Fe31(C40	68.6(3)

C34(Fe31(C40	110.2(3)

C38(Fe31(C40	68.2(3)

C33(Fe31(C40	115.0(3)

C36(Fe31(C40	40.9(2)

C31(Fe31(C32	41.0(3)

C39(Fe31(C32	115.0(3)

C35(Fe31(C32	69.6(3)

C37(Fe31(C32	134.1(3)

C34(Fe31(C32	68.5(3)

C38(Fe31(C32	110.5(3)

C33(Fe31(C32	40.7(3)

C36(Fe31(C32	173.7(3)

C40(Fe31(C32	145.2(3)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	27(4) 	16(3)	25(3) 	6(3)	1(3) 	(3(3)

C2	24(4) 	18(3)	21(3) 	5(2)	10(3) 	3(3)

C3	36(4) 	22(3)	17(3) 	6(3)	12(3) 	7(3)

C4	29(4) 	26(4)	19(3) 	4(3)	(2(3) 	(3(3)

C5	23(4) 	20(3)	23(3) 	5(3)	5(3) 	3(3)

C6	20(3) 	17(3)	14(3) 	2(2)	5(3) 	0(2)

C7	24(4) 	20(3)	16(3) 	(1(3)	3(3) 	(4(3)

C8	17(3) 	23(3)	26(3) 	6(3)	3(3) 	(5(3)

C9	27(4) 	28(3)	14(3) 	8(3)	11(3) 	4(3)

C10	32(4) 	16(3)	14(3) 	(1(2)	9(3) 	1(3)

C11	24(4) 	15(3)	14(3) 	3(2)	7(3) 	(1(2)

C12	22(4) 	20(3)	21(3) 	4(3)	2(3) 	3(3)

C13	22(4) 	17(3)	17(3) 	(1(2)	5(3) 	(1(2)

C14	15(4) 	23(3)	23(3) 	(5(3)	2(3) 	(1(3)

C15	24(4) 	21(3)	12(3) 	0(2)	2(3) 	2(3)

C16	25(4) 	25(4)	18(3) 	(6(3)	5(3) 	(1(3)

C17	25(4) 	21(3)	21(3) 	(2(3)	8(3) 	4(3)

C18	13(3) 	25(3)	20(3) 	5(3)	3(3) 	1(2)

C19	35(4) 	19(3)	15(3) 	0(2)	3(3) 	(3(3)

C20	20(3) 	19(3)	14(3) 	(2(2)	2(3) 	(3(3)

C21	17(4) 	24(4)	21(3) 	5(3)	1(3) 	(2(3)

C22	22(4) 	20(3)	14(3) 	5(2)	3(3) 	4(3)

C23	27(4) 	13(3)	16(3) 	3(2)	2(3) 	(4(3)

C24	18(4) 	19(3)	15(3) 	2(2)	1(3) 	1(3)

O1	28(3) 	50(4)	43(3) 	(27(3)	6(3) 	(7(3)

O2	24(3) 	38(3)	26(3) 	(9(2)	1(2) 	0(2)

Fe1	19(1) 	16(1)	15(1) 	1(1)	4(1) 	1(1)

Br1	41(1) 	22(1)	35(1) 	(6(1)	17(1) 	(6(1)

Br2	20(1) 	31(1)	24(1) 	6(1)	6(1) 	2(1)

C31	27(4) 	23(4)	23(3) 	2(3)	6(3) 	4(3)

C32	12(3) 	27(3)	17(3) 	5(3)	(2(2) 	(2(2)

C33	37(4) 	21(3)	17(3) 	3(3)	7(3) 	(2(3)

C34	29(4) 	28(4)	24(3) 	(2(3)	9(3) 	(1(3)

C35	21(4) 	22(3)	29(4) 	5(3)	5(3) 	1(3)

C36	13(3) 	17(3)	18(3) 	2(2)	5(2) 	(3(2)

C37	27(4) 	29(4)	16(3) 	2(3)	10(3) 	(1(3)

C38	21(4) 	30(4)	15(3) 	10(3)	5(3) 	1(3)

C39	20(4) 	37(4)	9(3) 	4(3)	(4(2) 	(2(3)

C40	25(4) 	18(3)	16(3) 	0(2)	1(3) 	(2(3)

C41	21(4) 	16(3)	17(3) 	(1(2)	3(3) 	1(2)

C42	18(3) 	20(3)	16(3) 	(1(2)	7(3) 	(3(2)

C43	27(4) 	17(3)	14(3) 	(1(2)	4(3) 	(1(3)

C44	25(4) 	20(3)	16(3) 	(5(3)	(2(3) 	(3(3)

C45	20(4) 	24(3)	13(3) 	4(2)	3(3) 	2(3)

C46	23(4) 	25(3)	19(3) 	(5(3)	3(3) 	3(3)

C47	27(4) 	18(3)	17(3) 	(2(2)	7(3) 	(3(3)

C48	15(4) 	20(3)	26(4) 	3(3)	7(3) 	(5(3)

C49	23(4) 	24(3)	17(3) 	3(3)	8(3) 	(1(3)

C50	19(3) 	16(3)	17(3) 	3(2)	0(3) 	(2(2)

C51	30(4) 	22(3)	19(3) 	2(3)	6(3) 	2(3)

C52	24(4) 	16(3)	16(3) 	1(2)	6(3) 	0(3)

C53	26(4) 	19(3)	16(3) 	(5(2)	0(3) 	(3(3)

C54	25(4) 	21(3)	22(3) 	2(3)	3(3) 	(1(3)

O31	20(3) 	56(4)	39(3) 	(27(3)	7(2) 	0(3)

O32	22(3) 	41(3)	29(3) 	(15(2)	9(2) 	1(2)

Fe31	19(1) 	18(1)	15(1) 	2(1)	4(1) 	(3(1)

Br31	41(1) 	23(1)	32(1) 	(5(1)	5(1) 	4(1)

Br32	18(1) 	32(1)	21(1) 	3(1)	1(1) 	(4(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H2	11192	12	154	24	1

H3	10267	(1753	(1101	28	1

H4	8706	(1284	(1059	31	1

H5	8638	832	183	26	1

H7	9681	(736	2606	24	1

H8	11103	(1665	2338	27	1

H9	10855	(3817	1127	26	1

H10	9272	(4268	596	24	1

H12	8167	(772	2569	25	1

H16	5631	1364	3643	27	1

H17	4138	1572	3428	26	1

H19	3836	(1310	1075	27	1

H23	6379	(3425	3	23	1

H24	7853	(3595	198	21	1

H32	1630	(4945	(2209	23	1

H33	2578	(6781	(2929	30	1

H34	4124	(6229	(2142	32	1

H35	4160	(4128	(858	29	1

H37	3149	(5673	1033	27	1

H38	1711	(6601	132	26	1

H39	1932	(8728	(990	28	1

H40	3527	(9238	(765	24	1

H42	4640	(5767	1721	21	1

H46	7195	(3614	4008	27	1

H47	8687	(3432	4527	24	1

H49	8976	(6318	2322	25	1

H53	6437	(8394	20	25	1

H54	4955	(8612	(502	28	1