|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	02src723

Empirical formula 	C66H48Cr2N12S32

Formula weight 	2139.08

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 8.6560(2) Å	( = 82.8290(10)°

b = 10.2951(2) Å	( = 88.6050(10)°

c = 25.0197(5) Å	(  = 73.2990(10)°

Volume	2118.70(8) Å3

Z	1

Density (calculated)	1.677 Mg / m3

Absorption coefficient	1.095 mm(1

F(000)	1088

Crystal	Plate; Black

Crystal size	0.50 ( 0.42 ( 0.05 mm3

( range for data collection	4.76 ( 27.68°

Index ranges	(11 ( h ( 11, (13 ( k ( 13, (32 ( l ( 32

Reflections collected	19568

Independent reflections	19591 [Rint = 0.0000]

Completeness to ( = 27.68°	78.3 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9473 and 0.6104

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	19591 / 0 / 508

Goodness-of-fit on F2	1.045

Final R indices [F2 > 2((F2)]	R1 = 0.0684, wR2 = 0.1664

R indices (all data)	R1 = 0.0992, wR2 = 0.1887

Largest diff. peak and hole	0.649 and (0.814 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

All hydrogen atoms were fixed.

The crystals were twinned involving a rotation of 180° about a. The twin component value was 34.8(1) %.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

S1	(1144(2)	1895(2)	(2386(1)	25(1)	1

S2	(2782(2)	(877(2)	(2052(1)	23(1)	1

S3	(2646(2)	(243(1)	(943(1)	20(1)	1

S4	(1164(2)	1975(1)	(1215(1)	17(1)	1

S5	(1087(2)	2382(1)	41(1)	19(1)	1

S6	(2788(2)	307(2)	302(1)	23(1)	1

S7	(3125(2)	608(2)	1463(1)	29(1)	1

S8	(1072(2)	3123(2)	1129(1)	25(1)	1

C1	(1096(8)	531(6)	(2771(2)	23(2)	1

C2	(2559(8)	23(6)	(2711(2)	27(2)	1

C3	(2253(7)	161(6)	(1624(2)	17(1)	1

C4	(1599(7)	1186(5)	(1749(2)	17(1)	1

C5	(1891(7)	995(5)	(714(2)	18(1)	1

C6	(1908(7)	1203(5)	(185(2)	18(1)	1

C7	(1655(7)	2088(5)	716(2)	17(1)	1

C8	(2423(7)	1138(6)	835(2)	22(1)	1

C9	(3211(8)	2105(5)	1791(2)	27(2)	1

C10	(1664(8)	2443(6)	1786(2)	27(2)	1

S11	4862(2)	5837(1)	1876(1)	19(1)	1

S12	7542(2)	7327(2)	1122(1)	25(1)	1

S13	6425(2)	6318(2)	206(1)	25(1)	1

S14	4143(2)	5074(1)	830(1)	19(1)	1

C11	5802(7)	7076(5)	2059(2)	22(1)	1

C12	7485(7)	6894(6)	1846(2)	21(1)	1

C13	6243(7)	6491(5)	905(2)	18(1)	1

C14	5225(7)	5919(5)	1183(2)	14(1)	1

C15	5131(7)	5292(5)	217(2)	17(1)	1

Cr1	3766(1)	3126(1)	3558(1)	14(1)	1

S41	(168(2)	749(2)	4023(1)	27(1)	1

S42	1435(2)	4631(2)	1804(1)	23(1)	1

S43	8398(2)	4417(2)	3041(1)	29(1)	1

S44	7085(2)	(911(2)	2915(1)	24(1)	1

N21	2312(5)	4804(4)	3878(2)	13(1)	1

N22	4651(5)	2749(4)	4346(2)	12(1)	1

N41	2144(6)	2139(4)	3806(2)	14(1)	1

N42	2743(6)	3674(5)	2837(2)	19(1)	1

N43	5406(6)	4084(4)	3357(2)	19(1)	1

N44	5247(6)	1398(5)	3354(2)	20(1)	1

C21	1117(6)	5787(5)	3632(2)	13(1)	1

C22	92(7)	6814(5)	3908(2)	20(1)	1

C23	299(7)	6820(5)	4453(2)	16(1)	1

C24	1594(7)	5772(5)	4723(2)	13(1)	1

C25	2532(7)	4794(5)	4419(2)	12(1)	1

C26	3833(7)	3677(5)	4670(2)	13(1)	1

C27	4171(7)	3583(5)	5220(2)	14(1)	1

C28	5431(7)	2446(5)	5446(2)	16(1)	1

C29	6265(7)	1530(6)	5112(2)	21(1)	1

C30	5825(7)	1705(5)	4565(2)	19(1)	1

C31	1956(7)	5652(6)	5287(2)	18(1)	1

C32	3184(7)	4609(5)	5526(2)	18(1)	1

C33	(832(7)	7876(5)	4754(2)	21(1)	1

C34	5851(7)	2249(6)	6040(2)	24(2)	1

C41	1169(7)	1570(5)	3889(2)	17(1)	1

C42	2201(7)	4081(5)	2409(2)	17(1)	1

C43	6658(8)	4215(5)	3221(2)	18(1)	1

C44	6013(7)	435(6)	3176(2)	17(1)	1

Table 3. Bond lengths [Å] and angles [°].

S1(C4	1.753(5)

S1(C1	1.790(5)

S2(C3	1.758(6)

S2(C2	1.823(6)

S3(C5	1.749(6)

S3(C3	1.752(5)

S4(C5	1.731(5)

S4(C4	1.748(5)

S5(C6	1.728(6)

S5(C7	1.762(5)

S6(C6	1.730(6)

S6(C8	1.752(6)

S7(C8	1.751(5)

S7(C9	1.816(5)

S8(C7	1.751(6)

S8(C10	1.826(6)

C1(C2	1.501(8)

C1(H1A	0.9900

C1(H1B	0.9900

C2(H2A	0.9900

C2(H2B	0.9900

C3(C4	1.336(8)

C5(C6	1.366(7)

C7(C8	1.334(8)

C9(C10	1.477(8)

C9(H9A	0.9900

C9(H9B	0.9900

C10(H10A	0.9900

C10(H10B	0.9900

S11(C14	1.750(5)

S11(C11	1.806(6)

S12(C13	1.733(6)

S12(C12	1.813(5)

S13(C15	1.745(6)

S13(C13	1.779(5)

S14(C15	1.757(6)

S14(C14	1.766(6)

C11(C12	1.508(8)

C11(H11A	0.9900

C11(H11B	0.9900

C12(H12A	0.9900

C12(H12B	0.9900

C13(C14	1.331(7)

C15(C15i	1.360(10)

Cr1(N43	1.972(5)

Cr1(N42	1.976(5)

Cr1(N44	1.988(5)

Cr1(N41	2.002(5)

Cr1(N21	2.063(4)

Cr1(N22	2.082(4)

S41(C41	1.625(7)

S42(C42	1.633(6)

S43(C43	1.624(7)

S44(C44	1.633(6)

N21(C21	1.322(6)

N21(C25	1.369(6)

N22(C30	1.319(6)

N22(C26	1.358(6)

N41(C41	1.159(7)

N42(C42	1.158(7)

N43(C43	1.167(7)

N44(C44	1.157(6)

C21(C22	1.413(7)

C21(H21	0.9500

C22(C23	1.379(7)

C22(H22	0.9500

C23(C24	1.427(7)

C23(C33	1.506(7)

C24(C25	1.393(7)

C24(C31	1.437(7)

C25(C26	1.447(7)

C26(C27	1.400(7)

C27(C28	1.418(7)

C27(C32	1.442(7)

C28(C29	1.373(7)

C28(C34	1.512(7)

C29(C30	1.406(7)

C29(H29	0.9500

C30(H30	0.9500

C31(C32	1.362(7)

C31(H31	0.9500

C32(H32	0.9500

C33(H33A	0.9800

C33(H33B	0.9800

C33(H33C	0.9800

C34(H34A	0.9800

C34(H34B	0.9800

C34(H34C	0.9800

C4(S1(C1	100.2(3)

C3(S2(C2	101.1(3)

C5(S3(C3	95.3(3)

C5(S4(C4	95.9(3)

C6(S5(C7	94.9(3)

C6(S6(C8	95.4(3)

C8(S7(C9	98.5(3)

C7(S8(C10	100.3(3)

C2(C1(S1	114.4(4)

C2(C1(H1A	108.7

S1(C1(H1A	108.7

C2(C1(H1B	108.7

S1(C1(H1B	108.7

H1A(C1(H1B	107.6

C1(C2(S2	115.2(4)

C1(C2(H2A	108.5

S2(C2(H2A	108.5

C1(C2(H2B	108.5

S2(C2(H2B	108.5

H2A(C2(H2B	107.5

C4(C3(S3	117.1(4)

C4(C3(S2	129.0(4)

S3(C3(S2	113.9(3)

C3(C4(S4	117.0(4)

C3(C4(S1	128.7(4)

S4(C4(S1	114.2(3)

C6(C5(S4	122.3(5)

C6(C5(S3	123.0(5)

S4(C5(S3	114.6(3)

C5(C6(S5	122.7(5)

C5(C6(S6	121.6(5)

S5(C6(S6	115.7(3)

C8(C7(S8	130.5(4)

C8(C7(S5	117.2(4)

S8(C7(S5	112.4(3)

C7(C8(S7	128.0(5)

C7(C8(S6	116.8(4)

S7(C8(S6	115.2(3)

C10(C9(S7	113.6(4)

C10(C9(H9A	108.8

S7(C9(H9A	108.8

C10(C9(H9B	108.8

S7(C9(H9B	108.8

H9A(C9(H9B	107.7

C9(C10(S8	115.1(4)

C9(C10(H10A	108.5

S8(C10(H10A	108.5

C9(C10(H10B	108.5

S8(C10(H10B	108.5

H10A(C10(H10B	107.5

C14(S11(C11	100.9(3)

C13(S12(C12	101.0(3)

C15(S13(C13	94.6(3)

C15(S14(C14	94.5(3)

C12(C11(S11	113.9(4)

C12(C11(H11A	108.8

S11(C11(H11A	108.8

C12(C11(H11B	108.8

S11(C11(H11B	108.8

H11A(C11(H11B	107.7

C11(C12(S12	113.5(4)

C11(C12(H12A	108.9

S12(C12(H12A	108.9

C11(C12(H12B	108.9

S12(C12(H12B	108.9

H12A(C12(H12B	107.7

C14(C13(S12	130.1(4)

C14(C13(S13	117.2(4)

S12(C13(S13	112.7(3)

C13(C14(S11	127.9(4)

C13(C14(S14	117.7(4)

S11(C14(S14	114.4(3)

C15i(C15(S13	123.0(6)

C15i(C15(S14	121.4(6)

S13(C15(S14	115.6(3)

N43(Cr1(N42	91.8(2)

N43(Cr1(N44	90.4(2)

N42(Cr1(N44	93.44(19)

N43(Cr1(N41	176.82(19)

N42(Cr1(N41	91.36(19)

N44(Cr1(N41	90.01(18)

N43(Cr1(N21	91.49(18)

N42(Cr1(N21	94.15(18)

N44(Cr1(N21	172.13(18)

N41(Cr1(N21	87.72(18)

N43(Cr1(N22	88.70(18)

N42(Cr1(N22	173.36(18)

N44(Cr1(N22	93.19(17)

N41(Cr1(N22	88.13(18)

N21(Cr1(N22	79.22(17)

C21(N21(C25	118.0(4)

C21(N21(Cr1	127.1(4)

C25(N21(Cr1	114.6(3)

C30(N22(C26	117.9(5)

C30(N22(Cr1	128.0(4)

C26(N22(Cr1	114.0(3)

C41(N41(Cr1	172.4(4)

C42(N42(Cr1	174.4(5)

C43(N43(Cr1	157.7(4)

C44(N44(Cr1	171.7(4)

N21(C21(C22	122.0(5)

N21(C21(H21	119.0

C22(C21(H21	119.0

C23(C22(C21	120.8(5)

C23(C22(H22	119.6

C21(C22(H22	119.6

C22(C23(C24	117.8(5)

C22(C23(C33	121.0(5)

C24(C23(C33	121.2(5)

C25(C24(C23	117.5(5)

C25(C24(C31	118.6(5)

C23(C24(C31	123.9(5)

N21(C25(C24	124.0(5)

N21(C25(C26	115.5(4)

C24(C25(C26	120.5(5)

N22(C26(C27	123.6(5)

N22(C26(C25	116.4(5)

C27(C26(C25	120.0(5)

C26(C27(C28	117.4(5)

C26(C27(C32	118.5(5)

C28(C27(C32	124.1(5)

C29(C28(C27	118.3(5)

C29(C28(C34	120.8(5)

C27(C28(C34	120.9(5)

C28(C29(C30	120.1(5)

C28(C29(H29	120.0

C30(C29(H29	120.0

N22(C30(C29	122.7(5)

N22(C30(H30	118.6

C29(C30(H30	118.6

C32(C31(C24	121.3(5)

C32(C31(H31	119.3

C24(C31(H31	119.3

C31(C32(C27	121.2(5)

C31(C32(H32	119.4

C27(C32(H32	119.4

C23(C33(H33A	109.5

C23(C33(H33B	109.5

H33A(C33(H33B	109.5

C23(C33(H33C	109.5

H33A(C33(H33C	109.5

H33B(C33(H33C	109.5

C28(C34(H34A	109.5

C28(C34(H34B	109.5

H34A(C34(H34B	109.5

C28(C34(H34C	109.5

H34A(C34(H34C	109.5

H34B(C34(H34C	109.5

N41(C41(S41	178.2(5)

N42(C42(S42	179.0(5)

N43(C43(S43	178.8(5)

N44(C44(S44	179.1(5)

Symmetry transformations used to generate equivalent atoms:

(i) (x+1,(y+1,(z

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

S1	38(1) 	27(1)	13(1) 	(4(1)	8(1) 	(15(1)

S2	36(1) 	22(1)	16(1) 	(6(1)	2(1) 	(14(1)

S3	32(1) 	19(1)	11(1) 	(2(1)	1(1) 	(12(1)

S4	23(1) 	18(1)	12(1) 	(3(1)	1(1) 	(8(1)

S5	27(1) 	18(1)	13(1) 	(2(1)	(1(1) 	(8(1)

S6	36(1) 	25(1)	11(1) 	(2(1)	4(1) 	(16(1)

S7	53(1) 	23(1)	13(1) 	(4(1)	10(1) 	(13(1)

S8	35(1) 	23(1)	18(1) 	(7(1)	(3(1) 	(9(1)

C1	33(4) 	28(4)	10(3) 	(8(2)	4(3) 	(10(3)

C2	28(4) 	48(4)	11(3) 	(4(3)	1(3) 	(21(3)

C3	17(3) 	24(3)	9(2) 	(3(2)	0(2) 	(4(3)

C4	22(4) 	16(3)	14(3) 	(6(2)	2(3) 	(5(3)

C5	22(3) 	15(3)	19(3) 	(1(2)	5(3) 	(10(3)

C6	20(3) 	19(3)	16(3) 	(1(2)	0(3) 	(7(3)

C7	19(3) 	13(3)	11(2) 	(4(2)	0(2) 	7(3)

C8	27(4) 	22(4)	13(3) 	2(2)	7(3) 	(7(3)

C9	42(4) 	16(3)	18(3) 	(8(2)	2(3) 	1(3)

C10	33(4) 	34(4)	13(3) 	(5(3)	(6(3) 	(5(3)

S11	22(1) 	24(1)	12(1) 	(5(1)	2(1) 	(9(1)

S12	33(1) 	31(1)	17(1) 	(3(1)	1(1) 	(19(1)

S13	31(1) 	38(1)	13(1) 	(6(1)	6(1) 	(18(1)

S14	22(1) 	26(1)	12(1) 	(6(1)	4(1) 	(11(1)

C11	26(4) 	20(3)	18(3) 	(7(2)	(1(3) 	(1(3)

C12	25(4) 	29(4)	10(3) 	(6(2)	(3(3) 	(7(3)

C13	22(4) 	18(3)	12(3) 	(4(2)	2(3) 	(1(3)

C14	16(3) 	15(3)	12(3) 	(7(2)	7(2) 	(4(2)

C15	13(3) 	20(3)	21(3) 	(7(2)	4(3) 	(6(3)

Cr1	16(1) 	20(1)	9(1) 	(3(1)	3(1) 	(7(1)

S41	28(1) 	32(1)	29(1) 	(8(1)	12(1) 	(21(1)

S42	29(1) 	29(1)	13(1) 	3(1)	(2(1) 	(11(1)

S43	19(1) 	48(1)	23(1) 	2(1)	3(1) 	(18(1)

S44	23(1) 	24(1)	22(1) 	(9(1)	(1(1) 	1(1)

N21	15(3) 	14(3)	12(2) 	1(2)	2(2) 	(9(2)

N22	8(2) 	13(3)	15(2) 	(2(2)	(1(2) 	(1(2)

N41	14(3) 	17(3)	16(2) 	(3(2)	1(2) 	(10(2)

N42	24(3) 	28(3)	7(2) 	(4(2)	1(2) 	(10(2)

N43	19(3) 	22(3)	19(3) 	(5(2)	7(2) 	(11(2)

N44	23(3) 	24(3)	16(2) 	(8(2)	4(2) 	(9(2)

C21	12(3) 	14(3)	14(3) 	1(2)	2(2) 	(6(2)

C22	22(4) 	16(3)	19(3) 	(1(2)	(7(3) 	(2(3)

C23	18(3) 	11(3)	23(3) 	(5(2)	7(3) 	(13(3)

C24	15(3) 	16(3)	10(3) 	1(2)	2(2) 	(7(3)

C25	15(3) 	16(3)	10(2) 	(1(2)	2(2) 	(10(2)

C26	17(3) 	12(3)	12(3) 	(4(2)	2(2) 	(7(3)

C27	12(3) 	19(3)	14(3) 	2(2)	1(2) 	(9(3)

C28	18(3) 	20(3)	12(3) 	5(2)	(4(3) 	(13(3)

C29	16(3) 	20(3)	25(3) 	2(2)	(5(3) 	(2(3)

C30	15(3) 	17(3)	24(3) 	(5(2)	0(3) 	(2(3)

C31	25(4) 	19(3)	15(3) 	(8(2)	4(3) 	(11(3)

C32	24(4) 	29(4)	5(2) 	0(2)	0(2) 	(13(3)

C33	26(4) 	20(3)	17(3) 	(3(2)	10(3) 	(9(3)

C34	26(4) 	36(4)	10(3) 	0(2)	(3(3) 	(11(3)

C41	19(3) 	10(3)	16(3) 	(2(2)	1(3) 	5(3)

C42	16(3) 	15(3)	21(3) 	(6(2)	8(3) 	(7(3)

C43	30(4) 	10(3)	14(3) 	(2(2)	(5(3) 	(6(3)

C44	15(3) 	28(4)	11(3) 	5(2)	4(3) 	(10(3)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1A	(979	846	(3156	28	1

H1B	(131	(241	(2661	28	1

H2A	(2519	(598	(2987	33	1

H2B	(3529	812	(2788	33	1

H9A	(4045	2898	1608	32	1

H9B	(3545	1948	2169	32	1

H10A	(804	1608	1922	33	1

H10B	(1736	3123	2040	33	1

H11A	5123	8003	1922	26	1

H11B	5844	7012	2457	26	1

H12A	8127	5931	1942	25	1

H12B	7998	7474	2023	25	1

H21	942	5804	3257	16	1

H22	(749	7508	3717	24	1

H29	7139	776	5251	25	1

H30	6398	1045	4343	23	1

H31	1325	6313	5498	22	1

H32	3396	4557	5900	22	1

H33A	(1684	8466	4509	31	1

H33B	(232	8431	4899	31	1

H33C	(1318	7419	5051	31	1

H34A	4954	2061	6251	36	1

H34B	6047	3081	6138	36	1

H34C	6823	1478	6115	36	1