|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	03src0338

Empirical formula 	C70H56Cr2N12S32

Formula weight 	2195.19

Temperature 	300(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 8.9162(2) Å	( = 80.1440(10)°

b = 11.0761(2) Å	( = 87.5700(10)°

c = 23.8610(5) Å	(  = 77.5500(10)°

Volume	2267.02(8) Å3

Z	1

Density (calculated)	1.608 Mg / m3

Absorption coefficient	1.026 mm(1

F(000)	1120

Crystal	Block; Black

Crystal size	0.50 ( 0.42 ( 0.08 mm3

( range for data collection	2.92 ( 27.45°

Index ranges	(11 ( h ( 9, (14 ( k ( 13, (30 ( l ( 30

Reflections collected	39366

Independent reflections	10319 [Rint = 0.0990]

Completeness to ( = 27.45°	99.2 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9224 and 0.6280

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	10319 / 0 / 527

Goodness-of-fit on F2	1.030

Final R indices [F2 > 2((F2)]	R1 = 0.0564, wR2 = 0.1306

R indices (all data)	R1 = 0.0934, wR2 = 0.1501

Largest diff. peak and hole	0.953 and (0.521 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

All hydrogen atoms were fixed.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	12951(8)	(5198(7)	7633(2)	108(2)	1

C2	12629(7)	(6388(7)	7906(2)	100(2)	1

C3	12613(5)	(5371(4)	8881(2)	60(1)	1

C4	13619(5)	(4702(4)	8653(2)	67(1)	1

C5	13024(5)	(4070(4)	9639(2)	56(1)	1

C6	12972(5)	(3541(4)	10113(2)	57(1)	1

C7	13313(5)	(2148(4)	10838(2)	54(1)	1

C8	12203(5)	(2735(4)	11060(2)	60(1)	1

C9	12524(8)	(2025(8)	12067(2)	127(3)	1

C10	13304(8)	(1200(7)	11813(2)	116(2)	1

S1	14450(2)	(4701(2)	7977(1)	108(1)	1

S2	11857(2)	(6451(2)	8597(1)	99(1)	1

S3	11930(2)	(5152(1)	9553(1)	72(1)	1

S4	14157(2)	(3696(1)	9057(1)	74(1)	1

S5	14109(1)	(2494(1)	10192(1)	67(1)	1

S6	11751(2)	(3828(1)	10683(1)	79(1)	1

S7	11209(2)	(2588(2)	11695(1)	93(1)	1

S8	14139(2)	(1113(1)	11130(1)	72(1)	1

C11	9871(4)	(362(4)	9807(2)	52(1)	1

C12	8781(4)	(1787(4)	9268(2)	52(1)	1

C13	9945(4)	(1462(4)	8943(2)	50(1)	1

C14	9277(7)	(2877(7)	8193(3)	113(2)	1

C15	7756(6)	(2681(6)	8399(2)	86(2)	1

S11	10955(1)	(494(1)	9197(1)	59(1)	1

S12	8447(1)	(1211(1)	9907(1)	63(1)	1

S13	7494(2)	(2683(1)	9138(1)	78(1)	1

S14	10500(1)	(1843(1)	8274(1)	70(1)	1

C21	13366(4)	(583(3)	6283(2)	47(1)	1

C22	14112(4)	(1410(3)	5925(2)	51(1)	1

C23	13734(4)	(1168(3)	5359(2)	50(1)	1

C24	12598(4)	(85(3)	5156(2)	43(1)	1

C25	11928(3)	684(3)	5548(1)	36(1)	1

C26	10804(3)	1799(3)	5368(1)	35(1)	1

C27	10313(4)	2141(3)	4802(1)	40(1)	1

C28	9178(4)	3248(3)	4651(1)	45(1)	1

C29	8617(4)	3947(3)	5073(2)	42(1)	1

C30	9179(4)	3536(3)	5625(1)	41(1)	1

C31	12090(5)	282(4)	4585(2)	55(1)	1

C32	11020(5)	1324(4)	4414(2)	55(1)	1

C33	15301(5)	(2538(4)	6195(2)	72(1)	1

C34	14513(5)	(2018(4)	4952(2)	73(1)	1

C35	8611(5)	3658(4)	4050(2)	63(1)	1

C36	7403(4)	5141(4)	4972(2)	58(1)	1

C41	8505(5)	295(4)	6814(2)	50(1)	1

C42	9272(4)	4175(3)	6978(1)	45(1)	1

C43	12856(4)	264(3)	7678(2)	46(1)	1

C44	13972(4)	3065(3)	6397(1)	45(1)	1

N21	12316(3)	439(2)	6107(1)	38(1)	1

N22	10242(3)	2504(2)	5775(1)	35(1)	1

N41	9491(3)	831(3)	6713(1)	48(1)	1

N42	9953(3)	3201(3)	6905(1)	47(1)	1

N43	12163(4)	875(3)	7294(1)	53(1)	1

N44	12888(3)	2657(3)	6398(1)	47(1)	1

S41	7117(2)	(434(2)	6950(1)	99(1)	1

S42	8312(2)	5535(1)	7074(1)	79(1)	1

S43	13801(1)	(601(1)	8214(1)	73(1)	1

S44	15454(1)	3686(1)	6392(1)	76(1)	1

Cr1	11163(1)	1766(1)	6574(1)	36(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C2	1.448(8)

C1(S1	1.824(7)

C1(H1A	0.9700

C1(H1B	0.9700

C2(S2	1.756(6)

C2(H2A	0.9700

C2(H2B	0.9700

C3(C4	1.326(6)

C3(S3	1.730(4)

C3(S2	1.733(4)

C4(S4	1.743(4)

C4(S1	1.747(4)

C5(C6	1.354(5)

C5(S4	1.728(4)

C5(S3	1.742(4)

C6(S5	1.734(4)

C6(S6	1.734(4)

C7(C8	1.340(6)

C7(S5	1.738(4)

C7(S8	1.739(4)

C8(S7	1.737(4)

C8(S6	1.746(4)

C9(C10	1.318(7)

C9(S7	1.773(5)

C9(H9A	0.9700

C9(H9B	0.9700

C10(S8	1.760(5)

C10(H10A	0.9700

C10(H10B	0.9700

C11(C11i	1.376(7)

C11(S12	1.721(4)

C11(S11	1.722(4)

C12(C13	1.343(5)

C12(S13	1.739(4)

C12(S12	1.742(4)

C13(S11	1.737(4)

C13(S14	1.746(4)

C14(C15	1.408(7)

C14(S14	1.780(5)

C14(H14A	0.9700

C14(H14B	0.9700

C15(S13	1.769(5)

C15(H15A	0.9700

C15(H15B	0.9700

C21(N21	1.321(4)

C21(C22	1.403(5)

C21(H21	0.9300

C22(C23	1.373(6)

C22(C33	1.520(5)

C23(C24	1.421(5)

C23(C34	1.511(5)

C24(C25	1.402(4)

C24(C31	1.417(5)

C25(N21	1.358(4)

C25(C26	1.427(4)

C26(N22	1.362(4)

C26(C27	1.402(4)

C27(C28	1.415(5)

C27(C32	1.436(5)

C28(C29	1.386(5)

C28(C35	1.502(5)

C29(C30	1.395(5)

C29(C36	1.508(5)

C30(N22	1.324(4)

C30(H30	0.9300

C31(C32	1.344(5)

C31(H31	0.9300

C32(H32	0.9300

C33(H33A	0.9600

C33(H33B	0.9600

C33(H33C	0.9600

C34(H34A	0.9600

C34(H34B	0.9600

C34(H34C	0.9600

C35(H35A	0.9600

C35(H35B	0.9600

C35(H35C	0.9600

C36(H36A	0.9600

C36(H36B	0.9600

C36(H36C	0.9600

C41(N41	1.158(4)

C41(S41	1.611(4)

C42(N42	1.156(4)

C42(S42	1.612(4)

C43(N43	1.156(5)

C43(S43	1.609(4)

C44(N44	1.152(4)

C44(S44	1.615(4)

N21(Cr1	2.068(3)

N22(Cr1	2.070(3)

N41(Cr1	1.978(3)

N42(Cr1	1.982(3)

N43(Cr1	1.971(3)

N44(Cr1	1.993(3)

C2(C1(S1	114.3(4)

C2(C1(H1A	108.7

S1(C1(H1A	108.7

C2(C1(H1B	108.7

S1(C1(H1B	108.7

H1A(C1(H1B	107.6

C1(C2(S2	116.7(4)

C1(C2(H2A	108.1

S2(C2(H2A	108.1

C1(C2(H2B	108.1

S2(C2(H2B	108.1

H2A(C2(H2B	107.3

C4(C3(S3	116.8(3)

C4(C3(S2	129.0(3)

S3(C3(S2	114.2(3)

C3(C4(S4	117.5(3)

C3(C4(S1	126.5(3)

S4(C4(S1	116.0(3)

C6(C5(S4	122.6(3)

C6(C5(S3	123.4(3)

S4(C5(S3	114.0(2)

C5(C6(S5	122.2(3)

C5(C6(S6	123.2(3)

S5(C6(S6	114.5(2)

C8(C7(S5	117.3(3)

C8(C7(S8	128.2(3)

S5(C7(S8	114.4(2)

C7(C8(S7	127.7(3)

C7(C8(S6	116.5(3)

S7(C8(S6	115.7(2)

C10(C9(S7	122.2(5)

C10(C9(H9A	106.8

S7(C9(H9A	106.8

C10(C9(H9B	106.8

S7(C9(H9B	106.8

H9A(C9(H9B	106.6

C9(C10(S8	127.8(4)

C9(C10(H10A	105.4

S8(C10(H10A	105.4

C9(C10(H10B	105.4

S8(C10(H10B	105.4

H10A(C10(H10B	106.0

C4(S1(C1	98.3(3)

C3(S2(C2	104.0(3)

C3(S3(C5	96.1(2)

C5(S4(C4	95.6(2)

C6(S5(C7	95.69(19)

C6(S6(C8	95.71(19)

C8(S7(C9	100.5(2)

C7(S8(C10	101.6(2)

C11i(C11(S12	122.1(4)

C11i(C11(S11	122.5(4)

S12(C11(S11	115.5(2)

C13(C12(S13	129.5(3)

C13(C12(S12	116.8(3)

S13(C12(S12	113.8(2)

C12(C13(S11	116.9(3)

C12(C13(S14	127.1(3)

S11(C13(S14	116.0(2)

C15(C14(S14	121.3(4)

C15(C14(H14A	107.0

S14(C14(H14A	107.0

C15(C14(H14B	107.0

S14(C14(H14B	107.0

H14A(C14(H14B	106.7

C14(C15(S13	117.1(4)

C14(C15(H15A	108.0

S13(C15(H15A	108.0

C14(C15(H15B	108.0

S13(C15(H15B	108.0

H15A(C15(H15B	107.3

C11(S11(C13	95.46(18)

C11(S12(C12	95.34(18)

C12(S13(C15	101.3(2)

C13(S14(C14	101.6(2)

N21(C21(C22	123.8(3)

N21(C21(H21	118.1

C22(C21(H21	118.1

C23(C22(C21	119.0(3)

C23(C22(C33	123.8(3)

C21(C22(C33	117.2(4)

C22(C23(C24	118.7(3)

C22(C23(C34	121.4(4)

C24(C23(C34	119.9(4)

C25(C24(C31	117.3(3)

C25(C24(C23	117.7(3)

C31(C24(C23	125.0(3)

N21(C25(C24	123.1(3)

N21(C25(C26	116.5(3)

C24(C25(C26	120.4(3)

N22(C26(C27	122.3(3)

N22(C26(C25	116.4(3)

C27(C26(C25	121.4(3)

C26(C27(C28	118.7(3)

C26(C27(C32	116.5(3)

C28(C27(C32	124.8(3)

C29(C28(C27	118.0(3)

C29(C28(C35	121.1(3)

C27(C28(C35	120.9(3)

C28(C29(C30	119.3(3)

C28(C29(C36	123.6(3)

C30(C29(C36	117.1(3)

N22(C30(C29	123.7(3)

N22(C30(H30	118.1

C29(C30(H30	118.1

C32(C31(C24	122.6(3)

C32(C31(H31	118.7

C24(C31(H31	118.7

C31(C32(C27	121.9(3)

C31(C32(H32	119.1

C27(C32(H32	119.1

C22(C33(H33A	109.5

C22(C33(H33B	109.5

H33A(C33(H33B	109.5

C22(C33(H33C	109.5

H33A(C33(H33C	109.5

H33B(C33(H33C	109.5

C23(C34(H34A	109.5

C23(C34(H34B	109.5

H34A(C34(H34B	109.5

C23(C34(H34C	109.5

H34A(C34(H34C	109.5

H34B(C34(H34C	109.5

C28(C35(H35A	109.5

C28(C35(H35B	109.5

H35A(C35(H35B	109.5

C28(C35(H35C	109.5

H35A(C35(H35C	109.5

H35B(C35(H35C	109.5

C29(C36(H36A	109.5

C29(C36(H36B	109.5

H36A(C36(H36B	109.5

C29(C36(H36C	109.5

H36A(C36(H36C	109.5

H36B(C36(H36C	109.5

N41(C41(S41	179.2(4)

N42(C42(S42	179.3(3)

N43(C43(S43	179.1(3)

N44(C44(S44	178.0(3)

C21(N21(C25	117.7(3)

C21(N21(Cr1	128.3(2)

C25(N21(Cr1	114.0(2)

C30(N22(C26	118.0(3)

C30(N22(Cr1	128.1(2)

C26(N22(Cr1	113.9(2)

C41(N41(Cr1	177.5(3)

C42(N42(Cr1	165.0(3)

C43(N43(Cr1	172.2(3)

C44(N44(Cr1	167.2(3)

N43(Cr1(N41	91.10(13)

N43(Cr1(N42	95.25(13)

N41(Cr1(N42	92.36(12)

N43(Cr1(N44	90.09(13)

N41(Cr1(N44	176.76(12)

N42(Cr1(N44	90.54(12)

N43(Cr1(N21	93.64(12)

N41(Cr1(N21	89.10(11)

N42(Cr1(N21	170.96(12)

N44(Cr1(N21	87.81(11)

N43(Cr1(N22	172.78(12)

N41(Cr1(N22	87.78(11)

N42(Cr1(N22	91.93(11)

N44(Cr1(N22	90.67(11)

N21(Cr1(N22	79.21(10)

Symmetry transformations used to generate equivalent atoms:

(i) (x+2,(y,(z+2

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	128(5) 	127(5)	54(3) 	(33(3)	(4(3) 	18(4)

C2	84(4) 	151(6)	82(4) 	(71(4)	5(3) 	(22(4)

C3	69(3) 	69(3)	47(2) 	(25(2)	(1(2) 	(14(2)

C4	75(3) 	77(3)	53(2) 	(27(2)	8(2) 	(14(2)

C5	65(2) 	61(2)	45(2) 	(16(2)	(1(2) 	(12(2)

C6	71(3) 	61(2)	43(2) 	(16(2)	1(2) 	(17(2)

C7	59(2) 	59(2)	48(2) 	(20(2)	2(2) 	(11(2)

C8	82(3) 	59(2)	45(2) 	(19(2)	7(2) 	(23(2)

C9	151(6) 	216(8)	65(3) 	(66(4)	36(3) 	(126(6)

C10	155(6) 	159(6)	72(3) 	(54(4)	28(4) 	(97(5)

S1	145(1) 	131(1)	75(1) 	(53(1)	52(1) 	(64(1)

S2	129(1) 	104(1)	87(1) 	(57(1)	6(1) 	(43(1)

S3	97(1) 	83(1)	49(1) 	(25(1)	11(1) 	(40(1)

S4	83(1) 	94(1)	57(1) 	(29(1)	13(1) 	(39(1)

S5	69(1) 	88(1)	55(1) 	(32(1)	11(1) 	(29(1)

S6	121(1) 	85(1)	53(1) 	(32(1)	21(1) 	(57(1)

S7	117(1) 	133(1)	58(1) 	(45(1)	31(1) 	(75(1)

S8	89(1) 	85(1)	58(1) 	(30(1)	10(1) 	(43(1)

C11	52(2) 	65(3)	43(2) 	(14(2)	(1(2) 	(15(2)

C12	58(2) 	57(2)	45(2) 	(15(2)	(3(2) 	(16(2)

C13	51(2) 	59(2)	45(2) 	(18(2)	(3(2) 	(12(2)

C14	92(4) 	176(6)	109(5) 	(97(5)	15(3) 	(55(4)

C15	80(3) 	130(5)	70(3) 	(43(3)	9(3) 	(51(3)

S11	58(1) 	79(1)	50(1) 	(24(1)	5(1) 	(28(1)

S12	72(1) 	83(1)	47(1) 	(23(1)	9(1) 	(39(1)

S13	100(1) 	98(1)	59(1) 	(29(1)	13(1) 	(63(1)

S14	62(1) 	101(1)	60(1) 	(41(1)	13(1) 	(29(1)

C21	42(2) 	35(2)	61(2) 	(7(2)	(11(2) 	(2(2)

C22	38(2) 	33(2)	82(3) 	(16(2)	(4(2) 	(1(2)

C23	43(2) 	43(2)	70(3) 	(26(2)	8(2) 	(9(2)

C24	40(2) 	39(2)	52(2) 	(18(2)	6(2) 	(7(2)

C25	34(2) 	33(2)	42(2) 	(10(1)	3(1) 	(5(1)

C26	34(2) 	34(2)	38(2) 	(9(1)	5(1) 	(6(1)

C27	41(2) 	43(2)	36(2) 	(9(2)	3(1) 	(9(2)

C28	46(2) 	49(2)	39(2) 	(2(2)	(1(1) 	(15(2)

C29	34(2) 	42(2)	48(2) 	(2(2)	2(1) 	(6(1)

C30	39(2) 	35(2)	45(2) 	(10(2)	4(1) 	(1(1)

C31	63(2) 	58(2)	45(2) 	(26(2)	9(2) 	(6(2)

C32	64(2) 	62(2)	38(2) 	(18(2)	0(2) 	(5(2)

C33	58(3) 	43(2)	110(4) 	(23(2)	(17(2) 	10(2)

C34	65(3) 	55(3)	102(4) 	(43(3)	8(2) 	5(2)

C35	65(3) 	70(3)	47(2) 	(4(2)	(9(2) 	(4(2)

C36	54(2) 	51(2)	60(2) 	1(2)	(3(2) 	3(2)

C41	64(2) 	55(2)	39(2) 	(17(2)	9(2) 	(22(2)

C42	49(2) 	52(2)	37(2) 	(12(2)	1(2) 	(11(2)

C43	51(2) 	50(2)	40(2) 	(6(2)	3(2) 	(22(2)

C44	47(2) 	44(2)	41(2) 	(8(2)	(1(2) 	(5(2)

N21	36(1) 	32(1)	43(2) 	(7(1)	(2(1) 	(4(1)

N22	35(1) 	35(1)	34(1) 	(7(1)	3(1) 	(4(1)

N41	51(2) 	48(2)	47(2) 	(11(1)	6(1) 	(14(2)

N42	54(2) 	48(2)	43(2) 	(17(1)	5(1) 	(9(2)

N43	62(2) 	53(2)	44(2) 	(4(2)	(6(2) 	(13(2)

N44	44(2) 	42(2)	53(2) 	(7(1)	(3(1) 	(9(1)

S41	119(1) 	152(1)	67(1) 	(45(1)	30(1) 	(101(1)

S42	81(1) 	59(1)	91(1) 	(33(1)	(4(1) 	12(1)

S43	63(1) 	91(1)	58(1) 	18(1)	(16(1) 	(22(1)

S44	56(1) 	90(1)	91(1) 	(16(1)	1(1) 	(37(1)

Cr1	40(1) 	35(1)	34(1) 	(8(1)	1(1) 	(7(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1A	12014	(4559	7627	129	1

H1B	13254	(5257	7242	129	1

H2A	13577	(7016	7919	120	1

H2B	11919	(6621	7668	120	1

H9A	11956	(1669	12377	152	1

H9B	13271	(2753	12239	152	1

H10A	14137	(1246	12070	139	1

H10B	12628	(387	11817	139	1

H14A	9228	(2893	7789	136	1

H14B	9791	(3710	8369	136	1

H15A	7284	(3326	8299	103	1

H15B	7201	(1882	8201	103	1

H21	13624	(763	6666	56	1

H30	8784	4013	5903	49	1

H31	12513	(219	4318	66	1

H32	10729	1522	4034	66	1

H33A	15006	(3294	6141	108	1

H33B	15362	(2527	6595	108	1

H33C	16284	(2506	6020	108	1

H34A	15521	(1864	4860	110	1

H34B	13918	(1852	4611	110	1

H34C	14594	(2877	5127	110	1

H35A	7686	4293	4043	94	1

H35B	8404	2953	3906	94	1

H35C	9380	3991	3817	94	1

H36A	7804	5775	4724	87	1

H36B	7109	5418	5329	87	1

H36C	6522	4989	4800	87	1