|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	02src071

Empirical formula 	C50H90O15Si10

Formula weight 	1212.12

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 15.3777(2) Å	( = 72.76°

b = 19.8946(2) Å	( = 89.25°

c = 21.2081(3) Å	(  = 83.24°

Volume	6152.09(13) Å3

Z	4

Density (calculated)	1.309 Mg / m3

Absorption coefficient	0.274 mm(1

F(000)	2600

Crystal	block; colourless

Crystal size	0.38 ( 0.28 ( 0.16 mm3

( range for data collection	2.96 ( 27.50°

Index ranges	(19 ( h ( 19, (25 ( k ( 25, (27 ( l ( 27

Reflections collected	92784

Independent reflections	27468 [Rint = 0.0775]

Completeness to ( = 27.50°	97.2 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9574 and 0.9029

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	27468 / 0 / 1382

Goodness-of-fit on F2	1.013

Final R indices [F2 > 2((F2)]	R1 = 0.0557, wR2 = 0.1307

R indices (all data)	R1 = 0.0968, wR2 = 0.1523

Extinction coefficient	0.00000(15)

Largest diff. peak and hole	1.517 and (0.876 e Å(3

Diffractometer: Enraf Nonius KappaCCD area detector (( scans and ( scans to fill Ewald sphere). Data collection and cell

refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography,

part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing,

Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Program used to solve structure:

SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Program used to refine structure: SHELXL97 (G. M. Sheldrick

(1997), University of Göttingen, Germany).

Further information:  http://www.soton.ac.uk/~xservice/strat.htm

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	5512(2)	8775(2)	3761(1)	18(1)	1

C2	4881(2)	8432(2)	4291(2)	25(1)	1

C3	3985(2)	8811(2)	4021(2)	40(1)	1

C4	4026(2)	8917(2)	3287(2)	47(1)	1

C5	4998(2)	8893(2)	3107(2)	28(1)	1

C6	7831(2)	8153(2)	5757(1)	19(1)	1

C7	7747(3)	8953(2)	5653(2)	39(1)	1

C8	7196(2)	9097(2)	6215(2)	33(1)	1

C9	7019(2)	8369(2)	6663(2)	29(1)	1

C10	7061(2)	7910(2)	6198(2)	28(1)	1

C11	10472(2)	8292(1)	5094(1)	19(1)	1

C12	10391(2)	9111(2)	4948(2)	26(1)	1

C13	11319(2)	9289(2)	5040(2)	38(1)	1

C14	11865(2)	8591(2)	5363(2)	32(1)	1

C15	11467(2)	8065(2)	5086(2)	25(1)	1

C16	10609(2)	9084(2)	2496(1)	20(1)	1

C17	10607(2)	9129(2)	1758(2)	30(1)	1

C18	11507(2)	9327(2)	1522(2)	41(1)	1

C19	12112(3)	8921(3)	2096(2)	60(1)	1

C20	11592(2)	8888(2)	2716(2)	29(1)	1

C21	7513(2)	9463(2)	1912(1)	20(1)	1

C22	6560(2)	9494(2)	1671(2)	29(1)	1

C23	6584(3)	9744(2)	914(2)	48(1)	1

C24	7451(3)	9953(3)	728(2)	65(2)	1

C25	8074(2)	9525(2)	1292(2)	33(1)	1

C26	5946(2)	6189(2)	3745(2)	24(1)	1

C27	5315(3)	6528(2)	3154(2)	50(1)	1

C28	4445(3)	6266(4)	3380(3)	95(2)	1

C29	4485(3)	5940(4)	4087(3)	100(2)	1

C30	5346(2)	6063(2)	4341(2)	42(1)	1

C31	7841(2)	5606(1)	5804(1)	19(1)	1

C32	8439(2)	5545(2)	6410(2)	29(1)	1

C33	7834(2)	5518(2)	6991(2)	36(1)	1

C34	6952(2)	5377(2)	6770(2)	30(1)	1

C35	6907(2)	5764(2)	6035(2)	26(1)	1

C36	10938(2)	5756(1)	5011(2)	21(1)	1

C37	10874(2)	5547(2)	5771(2)	35(1)	1

C38	11820(3)	5285(2)	6041(2)	45(1)	1

C39	12430(2)	5526(2)	5463(2)	36(1)	1

C40	11844(2)	6033(2)	4895(2)	30(1)	1

C41	10877(2)	6522(2)	2548(1)	21(1)	1

C42	11816(2)	6557(2)	2783(2)	29(1)	1

C43	12375(2)	6560(2)	2186(2)	33(1)	1

C44	11815(2)	7052(2)	1611(2)	28(1)	1

C45	10868(2)	6918(2)	1792(1)	25(1)	1

C46	7679(3)	6918(2)	1808(2)	50(1)	1

C47	7970(5)	7326(4)	1172(3)	102(2)	1

C48	7731(7)	6963(4)	674(3)	143(4)	1

C49	7675(3)	6246(3)	1043(2)	57(1)	1

C50	7901(3)	6168(2)	1778(2)	60(1)	1

C51	13765(2)	9403(1)	(3179(1)	18(1)	1

C52	14700(2)	9249(2)	(3432(2)	26(1)	1

C53	14568(3)	9270(3)	(4144(2)	70(2)	1

C54	13781(8)	9280(15)	(4289(7)	39(5)	0.33(2)

C54'	13691(4)	9709(6)	(4383(2)	27(2)	0.67(2)

C55	13144(2)	9548(2)	(3786(2)	32(1)	1

C56	10653(2)	8991(2)	(2294(2)	26(1)	1

C57	10589(2)	9200(2)	(3055(2)	40(1)	1

C58	9635(3)	9208(3)	(3228(2)	68(1)	1

C59	9338(12)	8663(14)	(2631(7)	59(4)	0.53(3)

C59'	9126(7)	8989(9)	(2642(6)	36(3)	0.47(3)

C60	9792(2)	8677(2)	(2062(2)	50(1)	1

C61	10811(2)	8211(2)	26(2)	21(1)	1

C62	10540(2)	9016(2)	(225(2)	31(1)	1

C63	9595(2)	9115(2)	(10(2)	41(1)	1

C64	9278(6)	8383(6)	268(9)	33(4)	0.362(17)

C64'	9206(4)	8526(3)	(177(5)	38(2)	0.638(17)

C65	9955(2)	7901(2)	(38(2)	35(1)	1

C66	13994(2)	7965(2)	852(2)	29(1)	1

C67	14929(3)	7655(2)	1112(2)	46(1)	1

C68	15198(5)	8132(2)	1497(3)	118(3)	1

C69	14506(2)	8738(2)	1420(2)	43(1)	1

C70	13932(2)	8752(2)	832(2)	32(1)	1

C71	15571(2)	8965(2)	(1259(1)	21(1)	1

C72	16227(2)	9019(2)	(1829(2)	39(1)	1

C73	17096(3)	9112(4)	(1559(3)	103(2)	1

C74	16937(3)	9212(3)	(894(2)	59(1)	1

C75	16161(3)	8819(2)	(647(2)	52(1)	1

C76	14157(2)	6749(2)	(3157(1)	21(1)	1

C77	14986(2)	6979(2)	(3524(2)	28(1)	1

C78	14860(2)	6845(2)	(4192(2)	33(1)	1

C79	13893(2)	7126(2)	(4366(2)	35(1)	1

C80	13422(2)	6967(2)	(3706(2)	28(1)	1

C81	11387(2)	6416(2)	(2438(1)	22(1)	1

C82	11071(2)	6902(2)	(3135(2)	32(1)	1

C83	10088(2)	6841(2)	(3184(2)	36(1)	1

C84	9959(2)	6144(2)	(2668(2)	38(1)	1

C85	10544(2)	6157(2)	(2101(2)	41(1)	1

C86	11442(2)	5621(2)	105(1)	19(1)	1

C87	10438(2)	5858(2)	(9(2)	24(1)	1

C88	10029(2)	5679(2)	675(2)	30(1)	1

C89	10734(2)	5190(2)	1147(2)	28(1)	1

C90	11588(2)	5457(2)	857(1)	24(1)	1

C91	14549(2)	5531(2)	709(1)	19(1)	1

C92	15523(2)	5557(2)	844(2)	27(1)	1

C93	15686(3)	5170(3)	1579(2)	54(1)	1

C94	14805(2)	5093(2)	1894(2)	37(1)	1

C95	14121(2)	5542(2)	1368(1)	25(1)	1

C96	16385(2)	6392(2)	(1290(1)	18(1)	1

C97	16977(2)	6353(2)	(691(2)	31(1)	1

C98	17825(2)	6629(2)	(969(2)	47(1)	1

C99	17821(2)	6652(2)	(1696(2)	35(1)	1

C100	16853(2)	6825(2)	(1895(2)	31(1)	1

O1	7066(1)	8220(1)	4525(1)	18(1)	1

O2	8781(1)	8175(1)	4596(1)	18(1)	1

O3	10084(1)	8396(1)	3779(1)	19(1)	1

O4	8864(1)	8763(1)	2842(1)	22(1)	1

O5	7230(1)	8667(1)	3235(1)	20(1)	1

O6	6504(1)	7493(1)	3778(1)	22(1)	1

O7	7885(1)	7968(1)	2428(1)	25(1)	1

O8	10109(1)	7709(1)	2890(1)	20(1)	1

O9	10055(1)	7142(1)	4674(1)	22(1)	1

O10	8025(1)	7033(1)	5186(1)	20(1)	1

O11	7424(2)	6305(1)	4462(1)	30(1)	1

O12	7486(1)	6726(1)	3165(1)	30(1)	1

O13	9060(1)	6828(1)	2709(1)	32(1)	1

O14	10081(2)	6457(1)	3773(1)	29(1)	1

O15	9098(1)	6092(1)	4815(1)	20(1)	1

O16	14108(1)	8608(1)	(1832(1)	27(1)	1

O17	14216(1)	8280(1)	(537(1)	22(1)	1

O18	12658(1)	8049(1)	(69(1)	22(1)	1

O19	11717(1)	8266(1)	(1154(1)	23(1)	1

O20	12496(1)	8760(1)	(2281(1)	21(1)	1

O21	13717(1)	7938(1)	(2679(1)	21(1)	1

O22	11626(1)	7646(1)	(2083(1)	23(1)	1

O23	11820(1)	7030(1)	(230(1)	21(1)	1

O24	13927(1)	6982(1)	133(1)	22(1)	1

O25	15251(1)	7558(1)	(1168(1)	21(1)	1

O26	13045(1)	6759(1)	(2087(1)	23(1)	1

O27	11907(1)	6400(1)	(1166(1)	23(1)	1

O28	13138(1)	6048(1)	(234(1)	20(1)	1

O29	14737(1)	6291(1)	(635(1)	20(1)	1

O30	14725(1)	6832(1)	(1926(1)	21(1)	1

Si1	6613(1)	8278(1)	3821(1)	15(1)	1

Si2	7929(1)	7887(1)	4998(1)	14(1)	1

Si3	9827(1)	7990(1)	4529(1)	14(1)	1

Si4	9887(1)	8476(1)	3013(1)	15(1)	1

Si5	7881(1)	8694(1)	2624(1)	16(1)	1

Si6	6866(1)	6694(1)	3787(1)	17(1)	1

Si7	8113(1)	6274(1)	5042(1)	16(1)	1

Si8	10021(1)	6380(1)	4554(1)	18(1)	1

Si9	10006(1)	6885(1)	2998(1)	17(1)	1

Si10	8041(1)	7119(1)	2548(1)	18(1)	1

Si11	13513(1)	8662(1)	(2473(1)	15(1)	1

Si12	11650(1)	8398(1)	(1940(1)	16(1)	1

Si13	11774(1)	7878(1)	(369(1)	16(1)	1

Si14	13695(1)	7813(1)	72(1)	16(1)	1

Si15	14766(1)	8336(1)	(1201(1)	16(1)	1

Si16	13905(1)	7081(1)	(2446(1)	15(1)	1

Si17	12014(1)	6818(1)	(1937(1)	17(1)	1

Si18	12104(1)	6291(1)	(396(1)	15(1)	1

Si19	14074(1)	6232(1)	(25(1)	16(1)	1

Si20	15238(1)	6775(1)	(1250(1)	15(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C2	1.530(4)

C1(C5	1.548(4)

C1(Si1	1.843(3)

C1(H1	1.0000

C2(C3	1.521(4)

C2(H2A	0.9900

C2(H2B	0.9900

C3(C4	1.510(5)

C3(H3A	0.9900

C3(H3B	0.9900

C4(C5	1.537(5)

C4(H4A	0.9900

C4(H4B	0.9900

C5(H5A	0.9900

C5(H5B	0.9900

C6(C7	1.532(4)

C6(C10	1.532(4)

C6(Si2	1.837(3)

C6(H6	1.0000

C7(C8	1.529(5)

C7(H7A	0.9900

C7(H7B	0.9900

C8(C9	1.532(5)

C8(H8A	0.9900

C8(H8B	0.9900

C9(C10	1.528(4)

C9(H9A	0.9900

C9(H9B	0.9900

C10(H10A	0.9900

C10(H10B	0.9900

C11(C15	1.544(4)

C11(C12	1.556(4)

C11(Si3	1.838(3)

C11(H11	1.0000

C12(C13	1.538(4)

C12(H12A	0.9900

C12(H12B	0.9900

C13(C14	1.511(5)

C13(H13A	0.9900

C13(H13B	0.9900

C14(C15	1.529(4)

C14(H14A	0.9900

C14(H14B	0.9900

C15(H15A	0.9900

C15(H15B	0.9900

C16(C17	1.540(4)

C16(C20	1.558(4)

C16(Si4	1.844(3)

C16(H16	1.0000

C17(C18	1.521(4)

C17(H17A	0.9900

C17(H17B	0.9900

C18(C19	1.507(5)

C18(H18A	0.9900

C18(H18B	0.9900

C19(C20	1.518(5)

C19(H19A	0.9900

C19(H19B	0.9900

C20(H20A	0.9900

C20(H20B	0.9900

C21(C25	1.545(4)

C21(C22	1.547(4)

C21(Si5	1.841(3)

C21(H21	1.0000

C22(C23	1.536(5)

C22(H22A	0.9900

C22(H22B	0.9900

C23(C24	1.458(6)

C23(H23A	0.9900

C23(H23B	0.9900

C24(C25	1.518(5)

C24(H24A	0.9900

C24(H24B	0.9900

C25(H25A	0.9900

C25(H25B	0.9900

C26(C27	1.531(5)

C26(C30	1.533(5)

C26(Si6	1.846(3)

C26(H26	1.0000

C27(C28	1.514(6)

C27(H27A	0.9900

C27(H27B	0.9900

C28(C29	1.446(8)

C28(H28A	0.9900

C28(H28B	0.9900

C29(C30	1.509(6)

C29(H29A	0.9900

C29(H29B	0.9900

C30(H30A	0.9900

C30(H30B	0.9900

C31(C35	1.539(4)

C31(C32	1.555(4)

C31(Si7	1.842(3)

C31(H31	1.0000

C32(C33	1.528(5)

C32(H32A	0.9900

C32(H32B	0.9900

C33(C34	1.525(5)

C33(H33A	0.9900

C33(H33B	0.9900

C34(C35	1.519(4)

C34(H34A	0.9900

C34(H34B	0.9900

C35(H35A	0.9900

C35(H35B	0.9900

C36(C37	1.544(4)

C36(C40	1.547(4)

C36(Si8	1.838(3)

C36(H36	1.0000

C37(C38	1.542(5)

C37(H37A	0.9900

C37(H37B	0.9900

C38(C39	1.529(5)

C38(H38A	0.9900

C38(H38B	0.9900

C39(C40	1.542(5)

C39(H39A	0.9900

C39(H39B	0.9900

C40(H40A	0.9900

C40(H40B	0.9900

C41(C42	1.550(4)

C41(C45	1.561(4)

C41(Si9	1.837(3)

C41(H41	1.0000

C42(C43	1.521(4)

C42(H42A	0.9900

C42(H42B	0.9900

C43(C44	1.519(4)

C43(H43A	0.9900

C43(H43B	0.9900

C44(C45	1.535(4)

C44(H44A	0.9900

C44(H44B	0.9900

C45(H45A	0.9900

C45(H45B	0.9900

C46(C47	1.448(7)

C46(C50	1.510(5)

C46(Si10	1.839(4)

C46(H46	1.0000

C47(C48	1.515(7)

C47(H47A	0.9900

C47(H47B	0.9900

C48(C49	1.421(8)

C48(H48A	0.9900

C48(H48B	0.9900

C49(C50	1.561(6)

C49(H49A	0.9900

C49(H49B	0.9900

C50(H50A	0.9900

C50(H50B	0.9900

C51(C55	1.548(4)

C51(C52	1.557(4)

C51(Si11	1.838(3)

C51(H51	1.0000

C52(C53	1.514(5)

C52(H52A	0.9900

C52(H52B	0.9900

C53(C54	1.250(12)

C53(C54'	1.522(10)

C53(H53A	0.9900

C53(H53B	0.9900

C54(C55	1.603(13)

C54(H54A	0.9900

C54(H54B	0.9900

C54'(C55	1.487(6)

C54'(H54C	0.9900

C54'(H54D	0.9900

C55(H55A	0.9900

C55(H55B	0.9900

C56(C60	1.543(5)

C56(C57	1.545(4)

C56(Si12	1.841(3)

C56(H56	1.0000

C57(C58	1.513(6)

C57(H57A	0.9900

C57(H57B	0.9900

C58(C59'	1.443(14)

C58(C59	1.509(17)

C58(H58A	0.9900

C58(H58B	0.9900

C59(C60	1.411(13)

C59(H59A	0.9900

C59(H59B	0.9900

C59'(C60	1.542(11)

C59'(H59C	0.9900

C59'(H59D	0.9900

C60(H60A	0.9900

C60(H60B	0.9900

C61(C62	1.537(4)

C61(C65	1.542(4)

C61(Si13	1.844(3)

C61(H61	1.0000

C62(C63	1.526(5)

C62(H62A	0.9900

C62(H62B	0.9900

C63(C64'	1.507(7)

C63(C64	1.535(11)

C63(H63A	0.9900

C63(H63B	0.9900

C64(C65	1.594(11)

C64(H64A	0.9900

C64(H64B	0.9900

C64'(C65	1.554(6)

C64'(H64C	0.9900

C64'(H64D	0.9900

C65(H65A	0.9900

C65(H65B	0.9900

C66(C67	1.537(5)

C66(C70	1.546(4)

C66(Si14	1.839(3)

C66(H66	1.0000

C67(C68	1.516(6)

C67(H67A	0.9900

C67(H67B	0.9900

C68(C69	1.482(7)

C68(H68A	0.9900

C68(H68B	0.9900

C69(C70	1.528(5)

C69(H69A	0.9900

C69(H69B	0.9900

C70(H70A	0.9900

C70(H70B	0.9900

C71(C75	1.529(5)

C71(C72	1.551(4)

C71(Si15	1.839(3)

C71(H71	1.0000

C72(C73	1.514(6)

C72(H72A	0.9900

C72(H72B	0.9900

C73(C74	1.496(7)

C73(H73A	0.9900

C73(H73B	0.9900

C74(C75	1.507(5)

C74(H74A	0.9900

C74(H74B	0.9900

C75(H75A	0.9900

C75(H75B	0.9900

C76(C77	1.530(4)

C76(C80	1.562(4)

C76(Si16	1.837(3)

C76(H76	1.0000

C77(C78	1.535(4)

C77(H77A	0.9900

C77(H77B	0.9900

C78(C79	1.535(5)

C78(H78A	0.9900

C78(H78B	0.9900

C79(C80	1.532(4)

C79(H79A	0.9900

C79(H79B	0.9900

C80(H80A	0.9900

C80(H80B	0.9900

C81(C85	1.541(4)

C81(C82	1.554(4)

C81(Si17	1.847(3)

C81(H81	1.0000

C82(C83	1.537(5)

C82(H82A	0.9900

C82(H82B	0.9900

C83(C84	1.523(5)

C83(H83A	0.9900

C83(H83B	0.9900

C84(C85	1.521(5)

C84(H84A	0.9900

C84(H84B	0.9900

C85(H85A	0.9900

C85(H85B	0.9900

C86(C90	1.544(4)

C86(C87	1.561(4)

C86(Si18	1.842(3)

C86(H86	1.0000

C87(C88	1.533(4)

C87(H87A	0.9900

C87(H87B	0.9900

C88(C89	1.526(5)

C88(H88A	0.9900

C88(H88B	0.9900

C89(C90	1.528(4)

C89(H89A	0.9900

C89(H89B	0.9900

C90(H90A	0.9900

C90(H90B	0.9900

C91(C92	1.539(4)

C91(C95	1.543(4)

C91(Si19	1.844(3)

C91(H91	1.0000

C92(C93	1.530(4)

C92(H92A	0.9900

C92(H92B	0.9900

C93(C94	1.506(5)

C93(H93A	0.9900

C93(H93B	0.9900

C94(C95	1.538(4)

C94(H94A	0.9900

C94(H94B	0.9900

C95(H95A	0.9900

C95(H95B	0.9900

C96(C100	1.541(4)

C96(C97	1.549(4)

C96(Si20	1.849(3)

C96(H96	1.0000

C97(C98	1.518(5)

C97(H97A	0.9900

C97(H97B	0.9900

C98(C99	1.529(5)

C98(H98A	0.9900

C98(H98B	0.9900

C99(C100	1.524(4)

C99(H99A	0.9900

C99(H99B	0.9900

C100(H10C	0.9900

C100(H10D	0.9900

O1(Si1	1.622(2)

O1(Si2	1.6245(19)

O2(Si3	1.621(2)

O2(Si2	1.622(2)

O3(Si4	1.615(2)

O3(Si3	1.622(2)

O4(Si4	1.616(2)

O4(Si5	1.619(2)

O5(Si1	1.618(2)

O5(Si5	1.619(2)

O6(Si6	1.616(2)

O6(Si1	1.619(2)

O7(Si5	1.616(2)

O7(Si10	1.621(2)

O8(Si9	1.613(2)

O8(Si4	1.618(2)

O9(Si8	1.616(2)

O9(Si3	1.6198(19)

O10(Si2	1.6150(19)

O10(Si7	1.6181(19)

O11(Si6	1.613(2)

O11(Si7	1.616(2)

O12(Si10	1.604(2)

O12(Si6	1.609(2)

O13(Si10	1.608(2)

O13(Si9	1.616(2)

O14(Si9	1.609(2)

O14(Si8	1.621(2)

O15(Si7	1.617(2)

O15(Si8	1.622(2)

O16(Si15	1.608(2)

O16(Si11	1.617(2)

O17(Si14	1.614(2)

O17(Si15	1.616(2)

O18(Si14	1.614(2)

O18(Si13	1.621(2)

O19(Si12	1.611(2)

O19(Si13	1.614(2)

O20(Si11	1.615(2)

O20(Si12	1.619(2)

O21(Si16	1.619(2)

O21(Si11	1.621(2)

O22(Si12	1.616(2)

O22(Si17	1.624(2)

O23(Si13	1.616(2)

O23(Si18	1.621(2)

O24(Si19	1.614(2)

O24(Si14	1.617(2)

O25(Si20	1.620(2)

O25(Si15	1.620(2)

O26(Si17	1.611(2)

O26(Si16	1.620(2)

O27(Si18	1.612(2)

O27(Si17	1.615(2)

O28(Si18	1.617(2)

O28(Si19	1.624(2)

O29(Si20	1.619(2)

O29(Si19	1.622(2)

O30(Si20	1.613(2)

O30(Si16	1.619(2)

C2(C1(C5	103.4(2)

C2(C1(Si1	114.7(2)

C5(C1(Si1	115.4(2)

C2(C1(H1	107.6

C5(C1(H1	107.6

Si1(C1(H1	107.6

C3(C2(C1	103.9(2)

C3(C2(H2A	111.0

C1(C2(H2A	111.0

C3(C2(H2B	111.0

C1(C2(H2B	111.0

H2A(C2(H2B	109.0

C4(C3(C2	104.6(3)

C4(C3(H3A	110.8

C2(C3(H3A	110.8

C4(C3(H3B	110.8

C2(C3(H3B	110.8

H3A(C3(H3B	108.9

C3(C4(C5	107.1(3)

C3(C4(H4A	110.3

C5(C4(H4A	110.3

C3(C4(H4B	110.3

C5(C4(H4B	110.3

H4A(C4(H4B	108.6

C4(C5(C1	105.8(3)

C4(C5(H5A	110.6

C1(C5(H5A	110.6

C4(C5(H5B	110.6

C1(C5(H5B	110.6

H5A(C5(H5B	108.7

C7(C6(C10	103.9(2)

C7(C6(Si2	115.1(2)

C10(C6(Si2	116.4(2)

C7(C6(H6	107.0

C10(C6(H6	107.0

Si2(C6(H6	107.0

C8(C7(C6	107.0(3)

C8(C7(H7A	110.3

C6(C7(H7A	110.3

C8(C7(H7B	110.3

C6(C7(H7B	110.3

H7A(C7(H7B	108.6

C7(C8(C9	105.8(3)

C7(C8(H8A	110.6

C9(C8(H8A	110.6

C7(C8(H8B	110.6

C9(C8(H8B	110.6

H8A(C8(H8B	108.7

C10(C9(C8	103.8(3)

C10(C9(H9A	111.0

C8(C9(H9A	111.0

C10(C9(H9B	111.0

C8(C9(H9B	111.0

H9A(C9(H9B	109.0

C9(C10(C6	103.1(2)

C9(C10(H10A	111.1

C6(C10(H10A	111.1

C9(C10(H10B	111.1

C6(C10(H10B	111.1

H10A(C10(H10B	109.1

C15(C11(C12	104.3(2)

C15(C11(Si3	113.8(2)

C12(C11(Si3	114.4(2)

C15(C11(H11	108.0

C12(C11(H11	108.0

Si3(C11(H11	108.0

C13(C12(C11	106.1(2)

C13(C12(H12A	110.5

C11(C12(H12A	110.5

C13(C12(H12B	110.5

C11(C12(H12B	110.5

H12A(C12(H12B	108.7

C14(C13(C12	106.2(3)

C14(C13(H13A	110.5

C12(C13(H13A	110.5

C14(C13(H13B	110.5

C12(C13(H13B	110.5

H13A(C13(H13B	108.7

C13(C14(C15	103.8(3)

C13(C14(H14A	111.0

C15(C14(H14A	111.0

C13(C14(H14B	111.0

C15(C14(H14B	111.0

H14A(C14(H14B	109.0

C14(C15(C11	103.2(2)

C14(C15(H15A	111.1

C11(C15(H15A	111.1

C14(C15(H15B	111.1

C11(C15(H15B	111.1

H15A(C15(H15B	109.1

C17(C16(C20	104.3(2)

C17(C16(Si4	115.4(2)

C20(C16(Si4	113.3(2)

C17(C16(H16	107.8

C20(C16(H16	107.8

Si4(C16(H16	107.8

C18(C17(C16	105.0(3)

C18(C17(H17A	110.8

C16(C17(H17A	110.8

C18(C17(H17B	110.8

C16(C17(H17B	110.8

H17A(C17(H17B	108.8

C19(C18(C17	103.9(3)

C19(C18(H18A	111.0

C17(C18(H18A	111.0

C19(C18(H18B	111.0

C17(C18(H18B	111.0

H18A(C18(H18B	109.0

C18(C19(C20	106.3(3)

C18(C19(H19A	110.5

C20(C19(H19A	110.5

C18(C19(H19B	110.5

C20(C19(H19B	110.5

H19A(C19(H19B	108.7

C19(C20(C16	106.8(3)

C19(C20(H20A	110.4

C16(C20(H20A	110.4

C19(C20(H20B	110.4

C16(C20(H20B	110.4

H20A(C20(H20B	108.6

C25(C21(C22	105.1(2)

C25(C21(Si5	114.4(2)

C22(C21(Si5	114.9(2)

C25(C21(H21	107.3

C22(C21(H21	107.3

Si5(C21(H21	107.3

C23(C22(C21	105.6(3)

C23(C22(H22A	110.6

C21(C22(H22A	110.6

C23(C22(H22B	110.6

C21(C22(H22B	110.6

H22A(C22(H22B	108.8

C24(C23(C22	107.8(3)

C24(C23(H23A	110.1

C22(C23(H23A	110.1

C24(C23(H23B	110.1

C22(C23(H23B	110.1

H23A(C23(H23B	108.5

C23(C24(C25	106.5(3)

C23(C24(H24A	110.4

C25(C24(H24A	110.4

C23(C24(H24B	110.4

C25(C24(H24B	110.4

H24A(C24(H24B	108.6

C24(C25(C21	103.6(3)

C24(C25(H25A	111.0

C21(C25(H25A	111.0

C24(C25(H25B	111.0

C21(C25(H25B	111.0

H25A(C25(H25B	109.0

C27(C26(C30	103.7(3)

C27(C26(Si6	114.8(2)

C30(C26(Si6	115.2(2)

C27(C26(H26	107.6

C30(C26(H26	107.6

Si6(C26(H26	107.6

C28(C27(C26	105.1(4)

C28(C27(H27A	110.7

C26(C27(H27A	110.7

C28(C27(H27B	110.7

C26(C27(H27B	110.7

H27A(C27(H27B	108.8

C29(C28(C27	109.3(4)

C29(C28(H28A	109.8

C27(C28(H28A	109.8

C29(C28(H28B	109.8

C27(C28(H28B	109.8

H28A(C28(H28B	108.3

C28(C29(C30	107.6(4)

C28(C29(H29A	110.2

C30(C29(H29A	110.2

C28(C29(H29B	110.2

C30(C29(H29B	110.2

H29A(C29(H29B	108.5

C29(C30(C26	105.1(3)

C29(C30(H30A	110.7

C26(C30(H30A	110.7

C29(C30(H30B	110.7

C26(C30(H30B	110.7

H30A(C30(H30B	108.8

C35(C31(C32	104.3(2)

C35(C31(Si7	113.05(19)

C32(C31(Si7	113.99(19)

C35(C31(H31	108.4

C32(C31(H31	108.4

Si7(C31(H31	108.4

C33(C32(C31	106.6(3)

C33(C32(H32A	110.4

C31(C32(H32A	110.4

C33(C32(H32B	110.4

C31(C32(H32B	110.4

H32A(C32(H32B	108.6

C34(C33(C32	105.5(3)

C34(C33(H33A	110.6

C32(C33(H33A	110.6

C34(C33(H33B	110.6

C32(C33(H33B	110.6

H33A(C33(H33B	108.8

C35(C34(C33	103.4(3)

C35(C34(H34A	111.1

C33(C34(H34A	111.1

C35(C34(H34B	111.1

C33(C34(H34B	111.1

H34A(C34(H34B	109.0

C34(C35(C31	103.9(2)

C34(C35(H35A	111.0

C31(C35(H35A	111.0

C34(C35(H35B	111.0

C31(C35(H35B	111.0

H35A(C35(H35B	109.0

C37(C36(C40	102.5(3)

C37(C36(Si8	115.0(2)

C40(C36(Si8	114.8(2)

C37(C36(H36	108.0

C40(C36(H36	108.0

Si8(C36(H36	108.0

C38(C37(C36	105.6(3)

C38(C37(H37A	110.6

C36(C37(H37A	110.6

C38(C37(H37B	110.6

C36(C37(H37B	110.6

H37A(C37(H37B	108.7

C39(C38(C37	107.1(3)

C39(C38(H38A	110.3

C37(C38(H38A	110.3

C39(C38(H38B	110.3

C37(C38(H38B	110.3

H38A(C38(H38B	108.6

C38(C39(C40	105.6(3)

C38(C39(H39A	110.6

C40(C39(H39A	110.6

C38(C39(H39B	110.6

C40(C39(H39B	110.6

H39A(C39(H39B	108.7

C39(C40(C36	104.2(3)

C39(C40(H40A	110.9

C36(C40(H40A	110.9

C39(C40(H40B	110.9

C36(C40(H40B	110.9

H40A(C40(H40B	108.9

C42(C41(C45	103.8(2)

C42(C41(Si9	114.0(2)

C45(C41(Si9	113.9(2)

C42(C41(H41	108.3

C45(C41(H41	108.3

Si9(C41(H41	108.3

C43(C42(C41	104.1(3)

C43(C42(H42A	110.9

C41(C42(H42A	110.9

C43(C42(H42B	110.9

C41(C42(H42B	110.9

H42A(C42(H42B	109.0

C44(C43(C42	103.5(3)

C44(C43(H43A	111.1

C42(C43(H43A	111.1

C44(C43(H43B	111.1

C42(C43(H43B	111.1

H43A(C43(H43B	109.0

C43(C44(C45	105.2(3)

C43(C44(H44A	110.7

C45(C44(H44A	110.7

C43(C44(H44B	110.7

C45(C44(H44B	110.7

H44A(C44(H44B	108.8

C44(C45(C41	106.9(2)

C44(C45(H45A	110.4

C41(C45(H45A	110.4

C44(C45(H45B	110.4

C41(C45(H45B	110.4

H45A(C45(H45B	108.6

C47(C46(C50	101.8(4)

C47(C46(Si10	118.0(4)

C50(C46(Si10	117.5(3)

C47(C46(H46	106.2

C50(C46(H46	106.2

Si10(C46(H46	106.2

C46(C47(C48	106.8(5)

C46(C47(H47A	110.4

C48(C47(H47A	110.4

C46(C47(H47B	110.4

C48(C47(H47B	110.3

H47A(C47(H47B	108.6

C49(C48(C47	105.7(5)

C49(C48(H48A	110.6

C47(C48(H48A	110.6

C49(C48(H48B	110.6

C47(C48(H48B	110.6

H48A(C48(H48B	108.7

C48(C49(C50	107.3(4)

C48(C49(H49A	110.3

C50(C49(H49A	110.2

C48(C49(H49B	110.2

C50(C49(H49B	110.2

H49A(C49(H49B	108.5

C46(C50(C49	102.1(3)

C46(C50(H50A	111.4

C49(C50(H50A	111.4

C46(C50(H50B	111.3

C49(C50(H50B	111.4

H50A(C50(H50B	109.2

C55(C51(C52	105.2(2)

C55(C51(Si11	113.9(2)

C52(C51(Si11	110.75(19)

C55(C51(H51	108.9

C52(C51(H51	108.9

Si11(C51(H51	108.9

C53(C52(C51	105.3(3)

C53(C52(H52A	110.7

C51(C52(H52A	110.7

C53(C52(H52B	110.7

C51(C52(H52B	110.7

H52A(C52(H52B	108.8

C54(C53(C52	112.3(6)

C54(C53(C54'	32.2(11)

C52(C53(C54'	107.2(4)

C54(C53(H53A	109.2

C52(C53(H53A	109.2

C54'(C53(H53A	82.0

C54(C53(H53B	109.1

C52(C53(H53B	109.2

C54'(C53(H53B	136.2

H53A(C53(H53B	107.9

C53(C54(C55	111.4(9)

C53(C54(H54A	109.3

C55(C54(H54A	109.3

C53(C54(H54B	109.3

C55(C54(H54B	109.3

H54A(C54(H54B	108.0

C55(C54'(C53	103.7(5)

C55(C54'(H54C	111.0

C53(C54'(H54C	111.0

C55(C54'(H54D	111.0

C53(C54'(H54D	111.0

H54C(C54'(H54D	109.0

C54'(C55(C51	107.3(3)

C54'(C55(C54	30.2(7)

C51(C55(C54	101.4(5)

C54'(C55(H55A	82.1

C51(C55(H55A	111.5

C54(C55(H55A	111.5

C54'(C55(H55B	130.9

C51(C55(H55B	111.5

C54(C55(H55B	111.5

H55A(C55(H55B	109.3

C60(C56(C57	104.4(3)

C60(C56(Si12	114.2(2)

C57(C56(Si12	113.6(2)

C60(C56(H56	108.1

C57(C56(H56	108.1

Si12(C56(H56	108.1

C58(C57(C56	106.1(3)

C58(C57(H57A	110.5

C56(C57(H57A	110.5

C58(C57(H57B	110.5

C56(C57(H57B	110.5

H57A(C57(H57B	108.7

C59'(C58(C59	26.7(5)

C59'(C58(C57	111.3(5)

C59(C58(C57	102.1(7)

C59'(C58(H58A	84.8

C59(C58(H58A	111.4

C57(C58(H58A	111.4

C59'(C58(H58B	125.4

C59(C58(H58B	111.4

C57(C58(H58B	111.4

H58A(C58(H58B	109.2

C60(C59(C58	109.6(9)

C60(C59(H59A	109.8

C58(C59(H59A	109.8

C60(C59(H59B	109.8

C58(C59(H59B	109.8

H59A(C59(H59B	108.2

C58(C59'(C60	106.2(7)

C58(C59'(H59C	110.5

C60(C59'(H59C	110.5

C58(C59'(H59D	110.5

C60(C59'(H59D	110.5

H59C(C59'(H59D	108.7

C59(C60(C59'	26.3(6)

C59(C60(C56	107.1(6)

C59'(C60(C56	106.5(5)

C59(C60(H60A	110.3

C59'(C60(H60A	131.4

C56(C60(H60A	110.3

C59(C60(H60B	110.3

C59'(C60(H60B	86.7

C56(C60(H60B	110.3

H60A(C60(H60B	108.5

C62(C61(C65	103.2(2)

C62(C61(Si13	115.5(2)

C65(C61(Si13	115.8(2)

C62(C61(H61	107.3

C65(C61(H61	107.3

Si13(C61(H61	107.3

C63(C62(C61	104.5(3)

C63(C62(H62A	110.8

C61(C62(H62A	110.8

C63(C62(H62B	110.8

C61(C62(H62B	110.8

H62A(C62(H62B	108.9

C64'(C63(C62	102.2(3)

C64'(C63(C64	34.6(5)

C62(C63(C64	108.7(4)

C64'(C63(H63A	81.3

C62(C63(H63A	110.0

C64(C63(H63A	110.0

C64'(C63(H63B	139.9

C62(C63(H63B	110.0

C64(C63(H63B	110.0

H63A(C63(H63B	108.3

C63(C64(C65	102.0(7)

C63(C64(H64A	111.4

C65(C64(H64A	111.4

C63(C64(H64B	111.4

C65(C64(H64B	111.4

H64A(C64(H64B	109.2

C63(C64'(C65	105.2(4)

C63(C64'(H64C	110.7

C65(C64'(H64C	110.7

C63(C64'(H64D	110.7

C65(C64'(H64D	110.7

H64C(C64'(H64D	108.8

C61(C65(C64'	106.8(3)

C61(C65(C64	100.6(5)

C64'(C65(C64	33.4(4)

C61(C65(H65A	111.7

C64'(C65(H65A	133.0

C64(C65(H65A	111.7

C61(C65(H65B	111.7

C64'(C65(H65B	79.2

C64(C65(H65B	111.7

H65A(C65(H65B	109.4

C67(C66(C70	104.4(3)

C67(C66(Si14	114.8(2)

C70(C66(Si14	115.0(2)

C67(C66(H66	107.4

C70(C66(H66	107.4

Si14(C66(H66	107.4

C68(C67(C66	105.3(4)

C68(C67(H67A	110.7

C66(C67(H67A	110.7

C68(C67(H67B	110.7

C66(C67(H67B	110.7

H67A(C67(H67B	108.8

C69(C68(C67	109.4(4)

C69(C68(H68A	109.8

C67(C68(H68A	109.8

C69(C68(H68B	109.8

C67(C68(H68B	109.8

H68A(C68(H68B	108.2

C68(C69(C70	105.8(3)

C68(C69(H69A	110.6

C70(C69(H69A	110.6

C68(C69(H69B	110.6

C70(C69(H69B	110.6

H69A(C69(H69B	108.7

C69(C70(C66	103.8(3)

C69(C70(H70A	111.0

C66(C70(H70A	111.0

C69(C70(H70B	111.0

C66(C70(H70B	111.0

H70A(C70(H70B	109.0

C75(C71(C72	103.7(3)

C75(C71(Si15	115.3(2)

C72(C71(Si15	115.4(2)

C75(C71(H71	107.3

C72(C71(H71	107.3

Si15(C71(H71	107.3

C73(C72(C71	106.1(3)

C73(C72(H72A	110.5

C71(C72(H72A	110.5

C73(C72(H72B	110.5

C71(C72(H72B	110.5

H72A(C72(H72B	108.7

C74(C73(C72	107.4(4)

C74(C73(H73A	110.2

C72(C73(H73A	110.2

C74(C73(H73B	110.2

C72(C73(H73B	110.2

H73A(C73(H73B	108.5

C73(C74(C75	104.1(4)

C73(C74(H74A	110.9

C75(C74(H74A	110.9

C73(C74(H74B	110.9

C75(C74(H74B	110.9

H74A(C74(H74B	108.9

C74(C75(C71	104.5(3)

C74(C75(H75A	110.8

C71(C75(H75A	110.8

C74(C75(H75B	110.8

C71(C75(H75B	110.8

H75A(C75(H75B	108.9

C77(C76(C80	104.5(2)

C77(C76(Si16	115.4(2)

C80(C76(Si16	114.4(2)

C77(C76(H76	107.3

C80(C76(H76	107.3

Si16(C76(H76	107.3

C76(C77(C78	103.0(3)

C76(C77(H77A	111.2

C78(C77(H77A	111.2

C76(C77(H77B	111.2

C78(C77(H77B	111.2

H77A(C77(H77B	109.1

C77(C78(C79	102.7(3)

C77(C78(H78A	111.2

C79(C78(H78A	111.2

C77(C78(H78B	111.2

C79(C78(H78B	111.2

H78A(C78(H78B	109.1

C80(C79(C78	105.6(3)

C80(C79(H79A	110.6

C78(C79(H79A	110.6

C80(C79(H79B	110.6

C78(C79(H79B	110.6

H79A(C79(H79B	108.7

C79(C80(C76	106.1(3)

C79(C80(H80A	110.5

C76(C80(H80A	110.5

C79(C80(H80B	110.5

C76(C80(H80B	110.5

H80A(C80(H80B	108.7

C85(C81(C82	104.3(3)

C85(C81(Si17	112.3(2)

C82(C81(Si17	116.3(2)

C85(C81(H81	107.9

C82(C81(H81	107.9

Si17(C81(H81	107.9

C83(C82(C81	106.0(3)

C83(C82(H82A	110.5

C81(C82(H82A	110.5

C83(C82(H82B	110.5

C81(C82(H82B	110.5

H82A(C82(H82B	108.7

C84(C83(C82	104.5(3)

C84(C83(H83A	110.8

C82(C83(H83A	110.8

C84(C83(H83B	110.8

C82(C83(H83B	110.8

H83A(C83(H83B	108.9

C85(C84(C83	101.9(3)

C85(C84(H84A	111.4

C83(C84(H84A	111.4

C85(C84(H84B	111.4

C83(C84(H84B	111.4

H84A(C84(H84B	109.3

C84(C85(C81	104.0(3)

C84(C85(H85A	111.0

C81(C85(H85A	111.0

C84(C85(H85B	111.0

C81(C85(H85B	111.0

H85A(C85(H85B	109.0

C90(C86(C87	104.4(2)

C90(C86(Si18	113.9(2)

C87(C86(Si18	112.48(19)

C90(C86(H86	108.6

C87(C86(H86	108.6

Si18(C86(H86	108.6

C88(C87(C86	106.6(2)

C88(C87(H87A	110.4

C86(C87(H87A	110.4

C88(C87(H87B	110.4

C86(C87(H87B	110.4

H87A(C87(H87B	108.6

C89(C88(C87	105.6(2)

C89(C88(H88A	110.6

C87(C88(H88A	110.6

C89(C88(H88B	110.6

C87(C88(H88B	110.6

H88A(C88(H88B	108.7

C88(C89(C90	103.7(2)

C88(C89(H89A	111.0

C90(C89(H89A	111.0

C88(C89(H89B	111.0

C90(C89(H89B	111.0

H89A(C89(H89B	109.0

C89(C90(C86	103.7(2)

C89(C90(H90A	111.0

C86(C90(H90A	111.0

C89(C90(H90B	111.0

C86(C90(H90B	111.0

H90A(C90(H90B	109.0

C92(C91(C95	103.0(2)

C92(C91(Si19	114.3(2)

C95(C91(Si19	115.11(19)

C92(C91(H91	108.0

C95(C91(H91	108.0

Si19(C91(H91	108.0

C93(C92(C91	105.7(3)

C93(C92(H92A	110.6

C91(C92(H92A	110.6

C93(C92(H92B	110.6

C91(C92(H92B	110.6

H92A(C92(H92B	108.7

C94(C93(C92	107.4(3)

C94(C93(H93A	110.2

C92(C93(H93A	110.2

C94(C93(H93B	110.2

C92(C93(H93B	110.2

H93A(C93(H93B	108.5

C93(C94(C95	106.5(3)

C93(C94(H94A	110.4

C95(C94(H94A	110.4

C93(C94(H94B	110.4

C95(C94(H94B	110.4

H94A(C94(H94B	108.6

C94(C95(C91	103.8(2)

C94(C95(H95A	111.0

C91(C95(H95A	111.0

C94(C95(H95B	111.0

C91(C95(H95B	111.0

H95A(C95(H95B	109.0

C100(C96(C97	104.7(2)

C100(C96(Si20	112.13(19)

C97(C96(Si20	114.8(2)

C100(C96(H96	108.3

C97(C96(H96	108.3

Si20(C96(H96	108.3

C98(C97(C96	106.8(3)

C98(C97(H97A	110.4

C96(C97(H97A	110.4

C98(C97(H97B	110.4

C96(C97(H97B	110.4

H97A(C97(H97B	108.6

C97(C98(C99	106.2(3)

C97(C98(H98A	110.5

C99(C98(H98A	110.5

C97(C98(H98B	110.5

C99(C98(H98B	110.5

H98A(C98(H98B	108.7

C100(C99(C98	103.3(3)

C100(C99(H99A	111.1

C98(C99(H99A	111.1

C100(C99(H99B	111.1

C98(C99(H99B	111.1

H99A(C99(H99B	109.1

C99(C100(C96	104.0(3)

C99(C100(H10C	110.9

C96(C100(H10C	110.9

C99(C100(H10D	110.9

C96(C100(H10D	110.9

H10C(C100(H10D	109.0

Si1(O1(Si2	144.03(13)

Si3(O2(Si2	143.68(13)

Si4(O3(Si3	143.49(13)

Si4(O4(Si5	153.58(14)

Si1(O5(Si5	153.83(14)

Si6(O6(Si1	153.88(14)

Si5(O7(Si10	155.87(15)

Si9(O8(Si4	155.33(14)

Si8(O9(Si3	156.26(15)

Si2(O10(Si7	155.98(14)

Si6(O11(Si7	153.82(15)

Si10(O12(Si6	154.16(15)

Si10(O13(Si9	150.88(15)

Si9(O14(Si8	154.66(15)

Si7(O15(Si8	147.37(13)

Si15(O16(Si11	164.33(15)

Si14(O17(Si15	149.34(13)

Si14(O18(Si13	145.18(13)

Si12(O19(Si13	161.71(15)

Si11(O20(Si12	148.30(13)

Si16(O21(Si11	148.12(14)

Si12(O22(Si17	149.40(14)

Si13(O23(Si18	154.03(14)

Si19(O24(Si14	163.66(15)

Si20(O25(Si15	151.13(14)

Si17(O26(Si16	152.33(14)

Si18(O27(Si17	150.73(14)

Si18(O28(Si19	148.50(14)

Si20(O29(Si19	149.70(13)

Si20(O30(Si16	154.59(14)

O5(Si1(O6	109.76(11)

O5(Si1(O1	108.76(11)

O6(Si1(O1	109.83(11)

O5(Si1(C1	111.52(12)

O6(Si1(C1	108.01(12)

O1(Si1(C1	108.95(12)

O10(Si2(O2	109.39(10)

O10(Si2(O1	109.35(11)

O2(Si2(O1	108.44(10)

O10(Si2(C6	109.37(12)

O2(Si2(C6	110.13(12)

O1(Si2(C6	110.16(12)

O9(Si3(O2	108.92(10)

O9(Si3(O3	109.92(11)

O2(Si3(O3	107.84(10)

O9(Si3(C11	109.65(12)

O2(Si3(C11	112.56(12)

O3(Si3(C11	107.91(12)

O3(Si4(O4	108.98(11)

O3(Si4(O8	109.07(10)

O4(Si4(O8	109.77(11)

O3(Si4(C16	108.84(12)

O4(Si4(C16	111.80(12)

O8(Si4(C16	108.34(12)

O7(Si5(O4	109.21(11)

O7(Si5(O5	108.72(11)

O4(Si5(O5	109.68(11)

O7(Si5(C21	110.23(12)

O4(Si5(C21	108.89(12)

O5(Si5(C21	110.09(12)

O12(Si6(O11	109.51(13)

O12(Si6(O6	108.96(11)

O11(Si6(O6	109.19(11)

O12(Si6(C26	109.74(13)

O11(Si6(C26	108.98(13)

O6(Si6(C26	110.45(13)

O11(Si7(O15	109.52(12)

O11(Si7(O10	109.56(11)

O15(Si7(O10	109.29(10)

O11(Si7(C31	108.98(13)

O15(Si7(C31	111.67(12)

O10(Si7(C31	107.79(12)

O9(Si8(O14	110.10(11)

O9(Si8(O15	109.11(11)

O14(Si8(O15	108.40(12)

O9(Si8(C36	109.01(12)

O14(Si8(C36	110.23(13)

O15(Si8(C36	109.97(12)

O14(Si9(O8	110.04(11)

O14(Si9(O13	109.52(13)

O8(Si9(O13	108.91(11)

O14(Si9(C41	110.31(12)

O8(Si9(C41	108.29(12)

O13(Si9(C41	109.74(13)

O12(Si10(O13	108.21(13)

O12(Si10(O7	109.89(11)

O13(Si10(O7	110.25(12)

O12(Si10(C46	108.95(18)

O13(Si10(C46	110.13(17)

O7(Si10(C46	109.39(15)

O20(Si11(O16	108.20(12)

O20(Si11(O21	109.27(11)

O16(Si11(O21	109.57(11)

O20(Si11(C51	111.02(12)

O16(Si11(C51	110.79(12)

O21(Si11(C51	107.97(12)

O19(Si12(O22	109.06(11)

O19(Si12(O20	109.10(11)

O22(Si12(O20	109.78(11)

O19(Si12(C56	110.73(13)

O22(Si12(C56	109.32(13)

O20(Si12(C56	108.84(13)

O19(Si13(O23	109.69(11)

O19(Si13(O18	108.89(11)

O23(Si13(O18	108.69(11)

O19(Si13(C61	109.60(12)

O23(Si13(C61	110.46(12)

O18(Si13(C61	109.49(12)

O17(Si14(O18	108.39(11)

O17(Si14(O24	109.48(11)

O18(Si14(O24	109.97(11)

O17(Si14(C66	110.91(13)

O18(Si14(C66	108.65(13)

O24(Si14(C66	109.42(13)

O16(Si15(O17	109.39(12)

O16(Si15(O25	108.85(11)

O17(Si15(O25	108.93(11)

O16(Si15(C71	110.14(12)

O17(Si15(C71	108.74(12)

O25(Si15(C71	110.76(12)

O21(Si16(O30	109.27(11)

O21(Si16(O26	108.78(11)

O30(Si16(O26	109.09(11)

O21(Si16(C76	110.76(12)

O30(Si16(C76	109.32(12)

O26(Si16(C76	109.59(13)

O26(Si17(O27	107.43(11)

O26(Si17(O22	109.49(11)

O27(Si17(O22	109.83(11)

O26(Si17(C81	112.46(13)

O27(Si17(C81	108.50(12)

O22(Si17(C81	109.09(12)

O27(Si18(O28	109.45(11)

O27(Si18(O23	109.46(11)

O28(Si18(O23	109.62(11)

O27(Si18(C86	108.91(12)

O28(Si18(C86	111.08(12)

O23(Si18(C86	108.29(12)

O24(Si19(O29	109.23(11)

O24(Si19(O28	108.91(11)

O29(Si19(O28	109.04(11)

O24(Si19(C91	109.82(12)

O29(Si19(C91	109.39(12)

O28(Si19(C91	110.43(12)

O30(Si20(O29	108.72(11)

O30(Si20(O25	109.88(11)

O29(Si20(O25	109.60(11)

O30(Si20(C96	109.06(12)

O29(Si20(C96	111.71(12)

O25(Si20(C96	107.86(12)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	15(1) 	18(2)	19(2) 	(5(1)	(4(1) 	(1(1)

C2	18(2) 	34(2)	21(2) 	(4(1)	2(1) 	(2(1)

C3	23(2) 	54(2)	36(2) 	(4(2)	2(2) 	(2(2)

C4	22(2) 	74(3)	38(2) 	(5(2)	(6(2) 	(7(2)

C5	21(2) 	37(2)	22(2) 	(6(1)	(7(1) 	2(1)

C6	17(2) 	23(2)	17(1) 	(7(1)	(3(1) 	(2(1)

C7	64(3) 	25(2)	30(2) 	(12(2)	10(2) 	(13(2)

C8	36(2) 	30(2)	34(2) 	(16(2)	0(2) 	5(1)

C9	25(2) 	40(2)	23(2) 	(12(1)	5(1) 	2(1)

C10	32(2) 	32(2)	22(2) 	(9(1)	7(1) 	(11(1)

C11	21(2) 	19(2)	17(1) 	(4(1)	(3(1) 	(3(1)

C12	26(2) 	22(2)	34(2) 	(13(1)	(7(1) 	(2(1)

C13	31(2) 	27(2)	54(2) 	(8(2)	(9(2) 	(9(1)

C14	22(2) 	33(2)	42(2) 	(13(2)	(7(2) 	(4(1)

C15	21(2) 	26(2)	30(2) 	(12(1)	(9(1) 	3(1)

C16	19(2) 	19(2)	21(2) 	(1(1)	0(1) 	(4(1)

C17	23(2) 	41(2)	20(2) 	2(1)	(1(1) 	(11(1)

C18	28(2) 	66(3)	25(2) 	(5(2)	4(2) 	(16(2)

C19	27(2) 	116(4)	32(2) 	(18(2)	1(2) 	(2(2)

C20	21(2) 	40(2)	24(2) 	(4(1)	(2(1) 	(8(1)

C21	18(2) 	19(2)	21(2) 	(4(1)	(2(1) 	(4(1)

C22	19(2) 	40(2)	22(2) 	(2(1)	(3(1) 	(4(1)

C23	35(2) 	78(3)	24(2) 	1(2)	(8(2) 	(14(2)

C24	36(2) 	113(4)	25(2) 	8(2)	(2(2) 	3(2)

C25	24(2) 	41(2)	23(2) 	5(1)	2(1) 	(2(1)

C26	26(2) 	23(2)	24(2) 	(8(1)	(4(1) 	(9(1)

C27	46(2) 	62(3)	40(2) 	(4(2)	(20(2) 	(23(2)

C28	42(3) 	154(6)	91(5) 	(29(4)	(19(3) 	(34(3)

C29	41(3) 	172(7)	80(4) 	(10(4)	0(3) 	(55(4)

C30	38(2) 	57(2)	37(2) 	(15(2)	11(2) 	(26(2)

C31	15(1) 	16(1)	24(2) 	(2(1)	(1(1) 	(4(1)

C32	25(2) 	32(2)	24(2) 	4(1)	(4(1) 	(8(1)

C33	41(2) 	42(2)	24(2) 	(9(2)	2(2) 	(8(2)

C34	28(2) 	30(2)	29(2) 	(3(1)	8(1) 	(3(1)

C35	19(2) 	24(2)	32(2) 	(1(1)	2(1) 	(2(1)

C36	25(2) 	12(1)	25(2) 	(6(1)	3(1) 	1(1)

C37	40(2) 	35(2)	26(2) 	(7(1)	2(2) 	6(2)

C38	49(2) 	46(2)	35(2) 	(15(2)	(10(2) 	15(2)

C39	29(2) 	30(2)	53(2) 	(18(2)	(11(2) 	1(1)

C40	24(2) 	21(2)	44(2) 	(10(1)	1(2) 	1(1)

C41	26(2) 	18(2)	18(2) 	(7(1)	0(1) 	1(1)

C42	21(2) 	39(2)	23(2) 	(6(1)	(3(1) 	8(1)

C43	23(2) 	40(2)	29(2) 	(6(2)	2(1) 	4(1)

C44	29(2) 	30(2)	24(2) 	(5(1)	3(1) 	(3(1)

C45	25(2) 	31(2)	18(2) 	(9(1)	1(1) 	3(1)

C46	76(3) 	45(2)	34(2) 	(25(2)	(20(2) 	10(2)

C47	138(6) 	142(6)	45(3) 	(47(4)	5(3) 	(44(5)

C48	291(12) 	98(5)	51(4) 	(34(4)	(56(5) 	(40(6)

C49	30(2) 	100(4)	69(3) 	(68(3)	3(2) 	(9(2)

C50	69(3) 	48(3)	74(3) 	(39(2)	(31(3) 	11(2)

C51	18(2) 	15(1)	19(2) 	(3(1)	1(1) 	(3(1)

C52	20(2) 	24(2)	28(2) 	(2(1)	5(1) 	(3(1)

C53	63(3) 	101(4)	33(2) 	(20(2)	8(2) 	36(3)

C54	36(7) 	55(14)	32(7) 	(24(8)	(5(5) 	4(7)

C54'	42(3) 	28(5)	14(3) 	(6(2)	(2(2) 	(10(3)

C55	28(2) 	38(2)	22(2) 	3(1)	(7(1) 	(10(1)

C56	23(2) 	29(2)	23(2) 	(3(1)	(3(1) 	5(1)

C57	32(2) 	53(2)	23(2) 	4(2)	(4(2) 	10(2)

C58	47(3) 	120(4)	38(2) 	(26(3)	(15(2) 	(3(3)

C59	44(8) 	73(11)	72(7) 	(35(8)	(9(6) 	(18(7)

C59'	21(5) 	34(7)	50(6) 	(10(5)	(14(4) 	3(4)

C60	15(2) 	71(3)	46(2) 	9(2)	(2(2) 	2(2)

C61	19(2) 	24(2)	19(2) 	(6(1)	1(1) 	2(1)

C62	32(2) 	24(2)	38(2) 	(11(1)	7(2) 	2(1)

C63	35(2) 	40(2)	45(2) 	(12(2)	5(2) 	12(2)

C64	13(5) 	46(6)	37(9) 	(8(5)	10(5) 	4(4)

C64'	22(3) 	43(4)	45(6) 	(12(3)	5(3) 	2(2)

C65	21(2) 	26(2)	56(2) 	(10(2)	1(2) 	0(1)

C66	34(2) 	30(2)	23(2) 	(9(1)	(7(1) 	(4(1)

C67	46(2) 	42(2)	47(2) 	(9(2)	(25(2) 	(6(2)

C68	174(6) 	37(3)	144(6) 	(33(3)	(134(5) 	14(3)

C69	38(2) 	69(3)	39(2) 	(36(2)	(1(2) 	(17(2)

C70	34(2) 	37(2)	32(2) 	(22(2)	(6(2) 	(1(1)

C71	21(2) 	19(2)	23(2) 	(5(1)	(1(1) 	(5(1)

C72	39(2) 	44(2)	41(2) 	(16(2)	15(2) 	(23(2)

C73	39(3) 	181(7)	136(6) 	(106(5)	37(3) 	(51(4)

C74	40(2) 	71(3)	68(3) 	(18(2)	(13(2) 	(26(2)

C75	54(3) 	64(3)	36(2) 	(3(2)	(16(2) 	(35(2)

C76	24(2) 	22(2)	19(2) 	(7(1)	(3(1) 	0(1)

C77	22(2) 	38(2)	24(2) 	(10(1)	2(1) 	2(1)

C78	33(2) 	43(2)	21(2) 	(9(1)	3(1) 	5(2)

C79	34(2) 	48(2)	20(2) 	(8(2)	(3(1) 	1(2)

C80	24(2) 	43(2)	21(2) 	(13(1)	(4(1) 	(2(1)

C81	22(2) 	24(2)	20(2) 	(6(1)	(2(1) 	(8(1)

C82	39(2) 	34(2)	22(2) 	(5(1)	(3(2) 	(15(1)

C83	32(2) 	40(2)	38(2) 	(16(2)	(8(2) 	2(2)

C84	35(2) 	61(2)	24(2) 	(13(2)	(2(2) 	(27(2)

C85	38(2) 	64(3)	29(2) 	(14(2)	4(2) 	(32(2)

C86	20(2) 	18(2)	18(2) 	(4(1)	1(1) 	(5(1)

C87	18(2) 	23(2)	28(2) 	(3(1)	(5(1) 	(5(1)

C88	22(2) 	31(2)	40(2) 	(12(2)	3(1) 	(4(1)

C89	28(2) 	33(2)	23(2) 	(3(1)	7(1) 	(12(1)

C90	25(2) 	26(2)	18(2) 	0(1)	0(1) 	(6(1)

C91	19(2) 	18(2)	18(2) 	(5(1)	(1(1) 	0(1)

C92	22(2) 	34(2)	21(2) 	(2(1)	(3(1) 	0(1)

C93	34(2) 	82(3)	29(2) 	13(2)	(13(2) 	(9(2)

C94	41(2) 	43(2)	22(2) 	(4(2)	(4(2) 	(3(2)

C95	28(2) 	24(2)	19(2) 	(2(1)	2(1) 	(3(1)

C96	16(1) 	18(2)	19(2) 	(4(1)	(2(1) 	1(1)

C97	19(2) 	47(2)	24(2) 	(11(2)	(7(1) 	4(1)

C98	27(2) 	77(3)	48(2) 	(33(2)	3(2) 	(17(2)

C99	21(2) 	40(2)	40(2) 	(7(2)	8(2) 	(4(1)

C100	23(2) 	36(2)	25(2) 	0(1)	6(1) 	2(1)

O1	14(1) 	25(1)	15(1) 	(5(1)	(3(1) 	0(1)

O2	16(1) 	16(1)	22(1) 	(4(1)	1(1) 	(2(1)

O3	19(1) 	22(1)	15(1) 	(6(1)	0(1) 	(6(1)

O4	16(1) 	23(1)	24(1) 	(4(1)	(3(1) 	0(1)

O5	18(1) 	26(1)	15(1) 	(4(1)	1(1) 	(4(1)

O6	22(1) 	17(1)	28(1) 	(9(1)	(3(1) 	(3(1)

O7	38(1) 	17(1)	21(1) 	(5(1)	1(1) 	(4(1)

O8	21(1) 	18(1)	22(1) 	(7(1)	3(1) 	(4(1)

O9	21(1) 	13(1)	33(1) 	(7(1)	2(1) 	(2(1)

O10	22(1) 	12(1)	26(1) 	(6(1)	1(1) 	(4(1)

O11	38(1) 	19(1)	30(1) 	(2(1)	(19(1) 	(5(1)

O12	31(1) 	22(1)	38(1) 	(8(1)	15(1) 	(7(1)

O13	17(1) 	33(1)	53(2) 	(25(1)	0(1) 	(4(1)

O14	42(1) 	22(1)	18(1) 	(2(1)	9(1) 	2(1)

O15	24(1) 	16(1)	20(1) 	(5(1)	3(1) 	(4(1)

O16	30(1) 	27(1)	21(1) 	(4(1)	(12(1) 	(1(1)

O17	25(1) 	20(1)	22(1) 	(8(1)	5(1) 	(7(1)

O18	18(1) 	20(1)	28(1) 	(10(1)	(3(1) 	0(1)

O19	30(1) 	22(1)	15(1) 	(3(1)	1(1) 	1(1)

O20	19(1) 	20(1)	22(1) 	(1(1)	3(1) 	(2(1)

O21	25(1) 	15(1)	22(1) 	(5(1)	2(1) 	(3(1)

O22	26(1) 	21(1)	25(1) 	(8(1)	(3(1) 	(2(1)

O23	21(1) 	16(1)	25(1) 	(5(1)	0(1) 	(3(1)

O24	25(1) 	17(1)	24(1) 	(7(1)	(1(1) 	0(1)

O25	20(1) 	17(1)	24(1) 	(7(1)	(1(1) 	(1(1)

O26	18(1) 	23(1)	29(1) 	(6(1)	1(1) 	(6(1)

O27	26(1) 	30(1)	14(1) 	(3(1)	(1(1) 	(11(1)

O28	16(1) 	22(1)	22(1) 	(6(1)	(1(1) 	(1(1)

O29	21(1) 	21(1)	18(1) 	(4(1)	2(1) 	(1(1)

O30	17(1) 	29(1)	16(1) 	(8(1)	(4(1) 	0(1)

Si1	14(1) 	15(1)	14(1) 	(4(1)	(1(1) 	(2(1)

Si2	14(1) 	13(1)	14(1) 	(4(1)	(2(1) 	(2(1)

Si3	14(1) 	13(1)	16(1) 	(5(1)	0(1) 	(2(1)

Si4	14(1) 	14(1)	14(1) 	(2(1)	0(1) 	(2(1)

Si5	16(1) 	16(1)	14(1) 	(3(1)	(1(1) 	(1(1)

Si6	18(1) 	15(1)	19(1) 	(5(1)	(3(1) 	(4(1)

Si7	18(1) 	12(1)	18(1) 	(2(1)	(3(1) 	(3(1)

Si8	21(1) 	12(1)	19(1) 	(4(1)	5(1) 	(1(1)

Si9	19(1) 	15(1)	18(1) 	(5(1)	4(1) 	(1(1)

Si10	24(1) 	16(1)	15(1) 	(6(1)	(1(1) 	(3(1)

Si11	15(1) 	14(1)	15(1) 	(3(1)	(2(1) 	(1(1)

Si12	16(1) 	16(1)	15(1) 	(2(1)	0(1) 	1(1)

Si13	15(1) 	15(1)	15(1) 	(3(1)	0(1) 	0(1)

Si14	18(1) 	16(1)	15(1) 	(5(1)	(4(1) 	0(1)

Si15	16(1) 	16(1)	15(1) 	(5(1)	(3(1) 	(2(1)

Si16	15(1) 	15(1)	14(1) 	(5(1)	(2(1) 	(1(1)

Si17	16(1) 	19(1)	15(1) 	(4(1)	(1(1) 	(5(1)

Si18	16(1) 	15(1)	14(1) 	(2(1)	0(1) 	(3(1)

Si19	16(1) 	14(1)	15(1) 	(3(1)	(1(1) 	0(1)

Si20	14(1) 	16(1)	14(1) 	(4(1)	(1(1) 	1(1)