|  | University of Southampton · Department of Chemistry # EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	02src173

Empirical formula 	C40H90O15Si10

Formula weight 	1092.02

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 10.8380(6) Å	 = 90°

b = 27.4492(14) Å	 = 92.810(2)°

c = 19.9239(14) Å	  = 90°

Volume	5920.1(6) Å3

Z	4

Density (calculated)	1.225 Mg / m3

Absorption coefficient	0.277 mm1

F(000)	2360

Crystal	Shard; Colourless

Crystal size	0.30  0.10  0.04 mm3

 range for data collection	2.91  25.03°

Index ranges	12  h  11, 26  k  32, 23  l  23

Reflections collected	29266

Independent reflections	8987 [Rint = 0.1397]

Completeness to  = 25.03°	86.0 %

Absorption correction	Semiempirical from equivalents

Max. and min. transmission	0.9890 and 0.9214

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	8987 / 6 / 606

Goodness-of-fit on F2	0.954

Final R indices [F2 > 2(F2)]	R1 = 0.0904, wR2 = 0.1833

R indices (all data)	R1 = 0.2406, wR2 = 0.2352

Largest diff. peak and hole	0.891 and 0.591 e Å3

Diffractometer: Nonius KappaCCD area detector ( scans and  scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 3337; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

All hydrogen atoms were fixed.

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Si1	2775(2)	4411(1)	8248(1)	34(1)	1

Si4	3814(2)	3458(1)	6265(1)	31(1)	1

Si5	3238(2)	4530(1)	6713(1)	34(1)	1

Si8	6447(2)	2900(1)	7857(1)	36(1)	1

Si2	2947(2)	3316(1)	8725(1)	34(1)	1

Si6	5593(2)	4552(1)	8595(1)	33(1)	1

Si9	6618(2)	3618(1)	6663(1)	34(1)	1

Si3	3623(2)	2735(1)	7464(1)	33(1)	1

Si7	5757(2)	3470(1)	9109(1)	32(1)	1

Si10	6043(2)	4694(1)	7059(1)	37(1)	1

O9	5303(4)	3463(2)	6301(2)	30(1)	1

O8	5106(5)	2693(2)	7620(3)	38(2)	1

O6	4105(5)	4597(2)	8542(3)	37(2)	1

O10	4620(5)	4744(2)	6797(3)	45(2)	1

O7	4306(5)	3350(2)	9093(3)	34(1)	1

O2	2965(5)	2915(2)	8129(3)	37(2)	1

O15	6116(5)	4650(2)	7871(3)	44(2)	1

O4	3299(5)	4006(2)	6347(3)	38(2)	1

O11	5978(5)	4012(2)	8828(3)	42(2)	1

O12	6413(5)	3094(2)	8623(3)	37(2)	1

O14	6626(5)	4211(2)	6758(3)	44(2)	1

O5	2688(5)	4475(2)	7449(3)	44(2)	1

O13	6762(5)	3361(2)	7386(3)	48(2)	1

O1	2611(5)	3836(2)	8396(3)	46(2)	1

O3	3349(5)	3130(2)	6884(3)	37(2)	1

C9	3055(8)	2131(3)	7198(5)	42(2)	1

C13	3240(7)	3197(3)	5454(4)	35(2)	1

C37	6902(8)	5233(3)	6766(4)	41(2)	1

C5	1817(8)	3128(3)	9338(4)	37(2)	1

C25	6401(8)	3429(3)	9982(4)	44(2)	1

C14	3268(8)	3517(3)	4843(4)	44(2)	1

C15	2795(10)	3240(4)	4206(5)	60(3)	1

C36	10014(9)	3584(4)	5711(6)	64(3)	1

C26	5943(9)	3004(4)	10402(5)	53(3)	1

C35	9634(10)	3692(4)	6939(6)	75(3)	1

C17	2205(10)	4944(3)	6244(4)	57(3)	1

C33	7882(7)	3446(3)	6121(5)	41(2)	1

C34	9098(8)	3742(4)	6225(5)	51(3)	1

C21	6268(9)	4997(3)	9212(4)	45(2)	1

C30	7590(10)	2006(4)	8308(5)	58(3)	1

C27	6479(11)	3022(5)	11119(5)	85(4)	1

C3	870(10)	5514(4)	9239(6)	85(4)	1

C6	515(8)	3017(3)	9107(5)	50(3)	1

C38	8272(8)	5168(4)	6712(5)	51(3)	1

C31	8767(10)	1706(4)	8330(7)	92(4)	1

C10	1721(11)	2044(5)	7101(9)	98(5)	1

C29	7645(8)	2428(3)	7829(5)	47(3)	1

C4	2040(10)	5590(4)	8203(6)	68(3)	1

C28	6199(10)	2519(4)	10097(5)	67(3)	1

C16	4514(10)	3724(4)	4723(5)	64(3)	1

C7	199(9)	2767(4)	9639(5)	70(3)	1

C32	6499(11)	1679(4)	8146(6)	79(4)	1

C2	1847(9)	5291(4)	8835(6)	59(3)	1

C8	158(9)	3478(4)	8868(6)	77(4)	1

C40	8890(9)	5626(4)	6432(6)	78(4)	1

C1	1568(8)	4758(3)	8673(4)	43(2)	1

C12	1025(17)	2329(6)	6766(12)	197(12)	1

C39	8922(9)	5031(4)	7394(6)	70(3)	1

C11	1431(12)	1519(5)	6864(11)	160(8)	1

C19	3446(12)	5029(8)	5211(8)	206(12)	1

C24	6783(15)	5819(5)	9628(6)	120(6)	1

C18	2410(20)	5062(9)	5556(8)	290(20)	1

C23	5623(14)	5748(5)	8550(7)	106(5)	1

C22	6140(20)	5501(5)	9085(9)	209(13)	1

C20	1470(30)	5435(14)	5263(8)	560(50)	1

Table 3. Bond lengths [Å] and angles [°].

Si1O5	1.600(6)

Si1O6	1.612(6)

Si1O1	1.619(6)

Si1C1	1.854(8)

Si4O9	1.611(5)

Si4O4	1.614(6)

Si4O3	1.626(6)

Si4C13	1.848(8)

Si5O10	1.610(6)

Si5O4	1.616(6)

Si5O5	1.617(6)

Si5C17	1.823(9)

Si8O8	1.610(6)

Si8O12	1.618(6)

Si8O13	1.620(6)

Si8C29	1.837(9)

Si2O1	1.604(6)

Si2O7	1.616(6)

Si2O2	1.620(6)

Si2C5	1.845(8)

Si6O15	1.598(6)

Si6O11	1.602(6)

Si6O6	1.616(6)

Si6C21	1.857(9)

Si9O13	1.607(6)

Si9O9	1.622(6)

Si9O14	1.637(6)

Si9C33	1.848(9)

Si3O3	1.602(6)

Si3O2	1.612(6)

Si3O8	1.626(6)

Si3C9	1.837(9)

Si7O7	1.605(6)

Si7O12	1.606(6)

Si7O11	1.612(6)

Si7C25	1.844(9)

Si10O14	1.598(6)

Si10O10	1.610(6)

Si10O15	1.620(6)

Si10C37	1.858(8)

C9C10	1.469(14)

C13C14	1.504(11)

C37C38	1.504(12)

C5C6	1.495(12)

C25C26	1.532(13)

C14C16	1.495(12)

C14C15	1.543(12)

C36C34	1.524(12)

C26C28	1.496(13)

C26C27	1.517(13)

C35C34	1.516(13)

C17C18	1.435(13)

C33C34	1.554(12)

C21C22	1.413(16)

C30C29	1.505(13)

C30C32	1.508(14)

C30C31	1.517(13)

C3C2	1.494(13)

C6C7	1.508(13)

C6C8	1.524(13)

C38C40	1.543(13)

C38C39	1.546(13)

C10C12	1.256(17)

C10C11	1.543(16)

C4C2	1.528(14)

C2C1	1.525(13)

C19C18	1.351(15)

C24C22	1.529(15)

C18C20	1.537(13)

C23C22	1.361(17)

O5Si1O6	109.5(3)

O5Si1O1	106.6(3)

O6Si1O1	110.3(3)

O5Si1C1	112.9(4)

O6Si1C1	108.1(4)

O1Si1C1	109.4(4)

O9Si4O4	109.9(3)

O9Si4O3	108.5(3)

O4Si4O3	108.5(3)

O9Si4C13	109.6(3)

O4Si4C13	110.2(3)

O3Si4C13	110.1(3)

O10Si5O4	108.3(3)

O10Si5O5	108.8(3)

O4Si5O5	110.7(3)

O10Si5C17	111.7(4)

O4Si5C17	111.2(4)

O5Si5C17	106.2(4)

O8Si8O12	109.3(3)

O8Si8O13	108.6(3)

O12Si8O13	107.7(3)

O8Si8C29	111.8(4)

O12Si8C29	108.0(4)

O13Si8C29	111.3(4)

O1Si2O7	108.5(3)

O1Si2O2	108.4(3)

O7Si2O2	109.1(3)

O1Si2C5	112.0(4)

O7Si2C5	109.6(3)

O2Si2C5	109.2(3)

O15Si6O11	108.7(3)

O15Si6O6	109.0(3)

O11Si6O6	109.6(3)

O15Si6C21	109.9(4)

O11Si6C21	109.1(4)

O6Si6C21	110.6(4)

O13Si9O9	109.1(3)

O13Si9O14	109.5(3)

O9Si9O14	108.2(3)

O13Si9C33	111.7(4)

O9Si9C33	109.5(3)

O14Si9C33	108.8(3)

O3Si3O2	108.1(3)

O3Si3O8	109.5(3)

O2Si3O8	109.7(3)

O3Si3C9	110.8(4)

O2Si3C9	111.0(4)

O8Si3C9	107.7(3)

O7Si7O12	108.6(3)

O7Si7O11	110.2(3)

O12Si7O11	107.8(3)

O7Si7C25	109.4(4)

O12Si7C25	111.8(4)

O11Si7C25	109.1(4)

O14Si10O10	109.8(3)

O14Si10O15	108.3(3)

O10Si10O15	109.3(3)

O14Si10C37	109.2(4)

O10Si10C37	108.5(4)

O15Si10C37	111.8(4)

Si4O9Si9	151.3(4)

Si8O8Si3	154.2(4)

Si1O6Si6	150.6(4)

Si10O10Si5	150.9(4)

Si7O7Si2	153.1(4)

Si3O2Si2	146.3(4)

Si6O15Si10	155.7(4)

Si4O4Si5	153.6(4)

Si6O11Si7	156.0(4)

Si7O12Si8	144.3(4)

Si10O14Si9	150.1(4)

Si1O5Si5	155.0(4)

Si9O13Si8	148.0(4)

Si2O1Si1	156.6(4)

Si3O3Si4	150.2(4)

C10C9Si3	119.9(7)

C14C13Si4	117.5(6)

C38C37Si10	116.1(6)

C6C5Si2	120.0(6)

C26C25Si7	116.4(6)

C16C14C13	113.9(7)

C16C14C15	108.8(8)

C13C14C15	111.1(7)

C28C26C27	110.0(9)

C28C26C25	112.6(8)

C27C26C25	111.8(8)

C18C17Si5	120.8(7)

C34C33Si9	115.8(6)

C35C34C36	111.9(9)

C35C34C33	111.2(8)

C36C34C33	109.6(8)

C22C21Si6	119.7(8)

C29C30C32	112.2(8)

C29C30C31	112.2(9)

C32C30C31	109.4(9)

C5C6C7	112.6(8)

C5C6C8	110.9(8)

C7C6C8	110.0(8)

C37C38C40	112.1(8)

C37C38C39	112.0(8)

C40C38C39	109.2(8)

C12C10C9	122.0(15)

C12C10C11	108.1(14)

C9C10C11	112.1(10)

C30C29Si8	118.3(7)

C3C2C1	111.7(9)

C3C2C4	110.6(9)

C1C2C4	112.1(8)

C2C1Si1	116.8(6)

C19C18C17	129.8(15)

C19C18C20	113.9(14)

C17C18C20	112.6(10)

C23C22C21	131.3(11)

C23C22C24	115.2(12)

C21C22C24	113.3(12)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Si1	37(2) 	31(2)	33(2) 	1(1)	3(1) 	1(1)

Si4	34(1) 	33(2)	26(2) 	1(1)	1(1) 	2(1)

Si5	39(2) 	31(2)	32(2) 	4(1)	2(1) 	1(1)

Si8	36(2) 	43(2)	30(2) 	0(1)	0(1) 	5(1)

Si2	38(2) 	28(2)	35(2) 	2(1)	2(1) 	1(1)

Si6	39(2) 	29(2)	30(2) 	1(1)	3(1) 	5(1)

Si9	32(2) 	39(2)	32(2) 	1(1)	2(1) 	2(1)

Si3	38(2) 	30(2)	30(2) 	1(1)	2(1) 	5(1)

Si7	38(2) 	29(2)	30(2) 	2(1)	1(1) 	1(1)

Si10	42(2) 	36(2)	35(2) 	4(1)	5(1) 	6(1)

O9	34(3) 	34(3)	22(3) 	2(3)	2(3) 	5(3)

O8	49(4) 	27(3)	39(4) 	5(3)	9(3) 	5(3)

O6	39(4) 	23(3)	50(4) 	4(3)	1(3) 	0(3)

O10	44(4) 	40(4)	51(4) 	5(3)	0(3) 	5(3)

O7	32(3) 	35(4)	34(4) 	4(3)	2(3) 	3(3)

O2	47(4) 	32(4)	31(4) 	4(3)	8(3) 	7(3)

O15	61(4) 	42(4)	30(4) 	4(3)	13(3) 	10(3)

O4	41(4) 	32(4)	41(4) 	3(3)	5(3) 	5(3)

O11	39(4) 	40(4)	44(4) 	3(3)	3(3) 	1(3)

O12	39(3) 	37(4)	36(4) 	4(3)	2(3) 	7(3)

O14	40(4) 	47(4)	44(4) 	1(3)	4(3) 	3(3)

O5	48(4) 	44(4)	40(4) 	11(3)	3(3) 	1(3)

O13	39(4) 	68(5)	36(4) 	16(3)	2(3) 	12(3)

O1	45(4) 	38(4)	53(4) 	2(3)	7(3) 	5(3)

O3	33(3) 	38(4)	40(4) 	9(3)	0(3) 	5(3)

C9	44(6) 	41(6)	44(6) 	3(5)	12(4) 	1(4)

C13	27(5) 	35(6)	44(6) 	6(5)	2(4) 	2(4)

C37	51(6) 	40(6)	32(6) 	8(5)	4(4) 	15(5)

C5	48(6) 	29(5)	35(6) 	4(4)	2(4) 	2(4)

C25	51(6) 	54(7)	27(6) 	5(5)	2(4) 	7(5)

C14	52(6) 	45(6)	35(6) 	9(5)	1(5) 	7(5)

C15	90(8) 	55(7)	36(6) 	1(5)	5(5) 	1(6)

C36	43(6) 	61(7)	90(9) 	2(6)	30(6) 	5(5)

C26	63(7) 	50(7)	46(7) 	3(6)	5(5) 	2(5)

C35	54(7) 	96(9)	73(9) 	17(7)	15(6) 	17(6)

C17	89(8) 	46(7)	36(7) 	4(5)	7(5) 	20(5)

C33	45(6) 	24(5)	54(7) 	3(5)	3(5) 	3(4)

C34	46(6) 	49(7)	60(8) 	8(5)	14(5) 	5(5)

C21	63(7) 	42(7)	31(6) 	13(5)	7(5) 	5(5)

C30	77(8) 	50(7)	45(7) 	4(6)	2(5) 	16(6)

C27	106(10) 	106(10)	41(8) 	14(7)	12(6) 	6(8)

C3	70(8) 	82(9)	103(10) 	42(8)	10(7) 	18(6)

C6	39(6) 	51(7)	58(7) 	5(5)	6(5) 	3(5)

C38	36(6) 	66(7)	53(7) 	7(6)	4(5) 	2(5)

C31	77(8) 	67(8)	131(12) 	18(8)	15(8) 	47(7)

C10	50(8) 	63(9)	180(15) 	42(10)	2(8) 	0(6)

C29	43(6) 	57(7)	39(6) 	10(5)	2(4) 	2(5)

C4	80(8) 	31(6)	93(10) 	1(6)	9(7) 	8(5)

C28	63(7) 	70(8)	67(8) 	21(7)	5(6) 	0(6)

C16	81(8) 	76(8)	36(7) 	10(6)	15(5) 	0(6)

C7	54(7) 	86(9)	72(8) 	3(7)	27(6) 	21(6)

C32	106(10) 	59(8)	76(9) 	38(7)	28(7) 	28(7)

C2	43(6) 	51(7)	82(8) 	16(7)	3(5) 	13(5)

C8	38(6) 	83(9)	111(10) 	12(8)	2(6) 	11(6)

C40	42(7) 	88(9)	105(10) 	55(7)	16(6) 	19(6)

C1	52(6) 	43(6)	34(6) 	0(5)	8(4) 	12(5)

C12	134(15) 	78(12)	360(30) 	9(15)	159(18) 	17(11)

C39	60(7) 	66(8)	81(9) 	16(6)	11(6) 	3(6)

C11	67(9) 	95(12)	320(30) 	114(14)	6(12) 	17(8)

C19	104(13) 	360(30)	156(18) 	140(20)	16(12) 	138(17)

C24	215(16) 	65(9)	75(10) 	29(7)	60(10) 	27(10)

C18	420(40) 	360(30)	88(14) 	93(17)	78(18) 	370(30)

C23	159(13) 	59(9)	97(12) 	0(8)	9(9) 	3(9)

C22	440(30) 	40(10)	125(15) 	4(9)	183(19) 	60(14)

C20	930(90) 	710(70)	48(13) 	100(20)	80(20) 	760(80)