|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	02src514

Empirical formula 	C32H48O8Si8

Formula weight 	785.42

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 10.6038(12) Å	( = 86.132(5)°

b = 11.3298(14) Å	( = 81.457(5)°

c = 19.444(3) Å	(  = 68.060(12)°

Volume	2142.6(5) Å3

Z	2

Density (calculated)	1.217 Mg / m3

Absorption coefficient	0.293 mm(1

F(000)	832

Crystal	Block; Colourless

Crystal size	0.38 ( 0.24 ( 0.18 mm3

( range for data collection	3.17 ( 27.59°

Index ranges	(13 ( h ( 13, (14 ( k ( 14, (25 ( l ( 25

Reflections collected	12780

Independent reflections	5962 [Rint = 0.0864]

Completeness to ( = 27.59°	60.1 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9492 and 0.8968

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	5962 / 16 / 453

Goodness-of-fit on F2	1.000

Final R indices [F2 > 2((F2)]	R1 = 0.0751, wR2 = 0.1505

R indices (all data)	R1 = 0.1995, wR2 = 0.1901

Largest diff. peak and hole	0.857 and (0.411 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

All hydrogen atoms were fixed.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Si1	(1780(2)	873(2)	7516(1)	35(1)	1

Si2	1359(2)	40(2)	6824(1)	33(1)	1

Si3	1710(2)	(2819(2)	6980(1)	32(1)	1

Si4	(1331(2)	(1999(2)	7820(1)	35(1)	1

Si5	(2751(3)	1976(2)	8978(1)	71(1)	1

Si6	1982(2)	1349(2)	7993(1)	55(1)	1

Si7	3232(2)	(3789(2)	8261(1)	51(1)	1

Si8	(1791(2)	(3122(2)	9297(1)	58(1)	1

O1	(274(4)	589(4)	7103(2)	36(1)	1

O2	1896(4)	(1488(4)	6769(2)	32(1)	1

O3	199(4)	(2554(4)	7398(2)	35(1)	1

O4	(1911(4)	(463(4)	7787(2)	36(1)	1

O5	(2009(4)	1752(4)	8173(2)	39(1)	1

O6	2199(4)	371(4)	7359(2)	37(1)	1

O7	2839(4)	(3645(4)	7474(2)	36(1)	1

O8	(1229(4)	(2435(4)	8620(2)	44(1)	1

C1	(3087(7)	1683(7)	6943(3)	30(2)	1

C2	(4132(8)	2832(8)	7109(3)	41(2)	1

C3	(5152(8)	3402(7)	6688(4)	48(2)	1

C4	(5128(9)	2807(9)	6083(4)	54(2)	1

C5	(4099(8)	1673(8)	5899(4)	46(2)	1

C6	(3088(7)	1120(7)	6320(3)	38(2)	1

C7	1617(7)	762(6)	5959(3)	32(2)	1

C8	576(7)	1216(7)	5539(3)	44(2)	1

C9	769(8)	1754(7)	4892(3)	48(2)	1

C10	2012(8)	1844(6)	4640(3)	41(2)	1

C11	3064(7)	1402(6)	5037(3)	41(2)	1

C12	2860(7)	880(6)	5695(3)	39(2)	1

C13	1914(6)	(3690(6)	6186(3)	31(2)	1

C14	1247(7)	(4535(6)	6159(3)	37(2)	1

C15	1320(7)	(5176(6)	5569(3)	41(2)	1

C16	2149(7)	(5020(7)	4971(3)	44(2)	1

C17	2827(7)	(4185(7)	4973(3)	49(2)	1

C18	2722(6)	(3575(7)	5576(3)	41(2)	1

C19	(2435(7)	(2614(8)	7432(3)	31(2)	1

C20	(2063(7)	(3932(8)	7364(3)	44(2)	1

C21	(2856(9)	(4416(8)	7045(4)	52(2)	1

C22	(4039(9)	(3596(10)	6798(3)	56(3)	1

C23	(4449(8)	(2311(9)	6875(3)	51(2)	1

C24	(3652(8)	(1820(8)	7190(3)	45(2)	1

C25	(1854(12)	674(8)	9525(4)	140(5)	1

C26	(2929(9)	3515(7)	9251(4)	86(3)	1

C27	1067(8)	3002(6)	7721(4)	74(3)	1

C28	3650(7)	1095(7)	8241(4)	68(3)	1

C29	2529(10)	(2237(8)	8678(4)	106(4)	1

C30	2605(8)	(4938(7)	8753(3)	69(3)	1

C31	(974(8)	(2941(7)	10035(3)	70(3)	1

C32	(3672(8)	(2441(10)	9443(5)	135(4)	1

Table 3. Bond lengths [Å] and angles [°].

Si1(O1	1.603(4)

Si1(O5	1.606(4)

Si1(O4	1.617(4)

Si1(C1	1.837(7)

Si2(O6	1.610(4)

Si2(O2	1.614(4)

Si2(O1	1.626(4)

Si2(C7	1.849(6)

Si3(O2	1.612(4)

Si3(O3	1.613(4)

Si3(O7	1.618(4)

Si3(C13	1.831(6)

Si4(O8	1.607(4)

Si4(O4	1.616(4)

Si4(O3	1.617(4)

Si4(C19	1.835(7)

Si5(O5	1.636(4)

Si5(C26	1.791(7)

Si5(C25	1.803(8)

Si5(H5S	1.55(3)

Si6(O6	1.646(4)

Si6(C28	1.815(7)

Si6(C27	1.841(7)

Si6(H6S	1.52(3)

Si7(O7	1.626(4)

Si7(C29	1.827(7)

Si7(C30	1.828(6)

Si7(H7S	1.48(3)

Si8(O8	1.634(4)

Si8(C32	1.834(8)

Si8(C31	1.841(6)

Si8(H8S	1.52(3)

C1(C2	1.378(8)

C1(C6	1.407(8)

C2(C3	1.389(8)

C2(H2	0.9500

C3(C4	1.387(9)

C3(H3	0.9500

C4(C5	1.366(9)

C4(H4	0.9500

C5(C6	1.378(8)

C5(H5	0.9500

C6(H6	0.9500

C7(C8	1.391(8)

C7(C12	1.393(8)

C8(C9	1.382(8)

C8(H8	0.9500

C9(C10	1.375(8)

C9(H9	0.9500

C10(C11	1.371(8)

C10(H10	0.9500

C11(C12	1.394(8)

C11(H11	0.9500

C12(H12	0.9500

C13(C18	1.386(8)

C13(C14	1.394(8)

C14(C15	1.376(7)

C14(H14	0.9500

C15(C16	1.392(8)

C15(H15	0.9500

C16(C17	1.387(8)

C16(H16	0.9500

C17(C18	1.369(8)

C17(H17	0.9500

C18(H18	0.9500

C19(C24	1.397(8)

C19(C20	1.405(8)

C20(C21	1.393(9)

C20(H20	0.9500

C21(C22	1.384(9)

C21(H21	0.9500

C22(C23	1.367(9)

C22(H22	0.9500

C23(C24	1.396(9)

C23(H23	0.9500

C24(H24	0.9500

C25(H25A	0.9800

C25(H25B	0.9800

C25(H25C	0.9800

C26(H26A	0.9800

C26(H26B	0.9800

C26(H26C	0.9800

C27(H27A	0.9800

C27(H27B	0.9800

C27(H27C	0.9800

C28(H28A	0.9800

C28(H28B	0.9800

C28(H28C	0.9800

C29(H29A	0.9800

C29(H29B	0.9800

C29(H29C	0.9800

C30(H30A	0.9800

C30(H30B	0.9800

C30(H30C	0.9800

C31(H31A	0.9800

C31(H31B	0.9800

C31(H31C	0.9800

C32(H32A	0.9800

C32(H32B	0.9800

C32(H32C	0.9800

O1(Si1(O5	109.5(2)

O1(Si1(O4	108.7(2)

O5(Si1(O4	109.2(2)

O1(Si1(C1	110.3(2)

O5(Si1(C1	109.6(3)

O4(Si1(C1	109.4(3)

O6(Si2(O2	108.0(2)

O6(Si2(O1	110.6(2)

O2(Si2(O1	109.2(2)

O6(Si2(C7	110.8(3)

O2(Si2(C7	110.4(2)

O1(Si2(C7	108.0(3)

O2(Si3(O3	109.8(2)

O2(Si3(O7	109.8(2)

O3(Si3(O7	108.8(2)

O2(Si3(C13	108.8(2)

O3(Si3(C13	109.3(3)

O7(Si3(C13	110.3(3)

O8(Si4(O4	107.9(2)

O8(Si4(O3	107.8(2)

O4(Si4(O3	109.5(2)

O8(Si4(C19	111.9(2)

O4(Si4(C19	110.8(3)

O3(Si4(C19	108.9(3)

O5(Si5(C26	109.5(3)

O5(Si5(C25	110.4(3)

C26(Si5(C25	114.6(4)

O5(Si5(H5S	106(2)

C26(Si5(H5S	109.5(19)

C25(Si5(H5S	106.2(19)

O6(Si6(C28	108.5(3)

O6(Si6(C27	110.1(3)

C28(Si6(C27	113.0(3)

O6(Si6(H6S	106(2)

C28(Si6(H6S	109.3(19)

C27(Si6(H6S	110(2)

O7(Si7(C29	109.9(3)

O7(Si7(C30	109.7(3)

C29(Si7(C30	111.7(4)

O7(Si7(H7S	112(2)

C29(Si7(H7S	106(2)

C30(Si7(H7S	108(2)

O8(Si8(C32	109.7(3)

O8(Si8(C31	107.4(3)

C32(Si8(C31	114.1(4)

O8(Si8(H8S	104(2)

C32(Si8(H8S	114(2)

C31(Si8(H8S	107(2)

Si1(O1(Si2	166.4(3)

Si3(O2(Si2	150.5(3)

Si3(O3(Si4	168.6(3)

Si4(O4(Si1	151.9(3)

Si1(O5(Si5	141.2(3)

Si2(O6(Si6	141.2(3)

Si3(O7(Si7	144.0(3)

Si4(O8(Si8	147.1(3)

C2(C1(C6	117.0(7)

C2(C1(Si1	122.3(5)

C6(C1(Si1	120.7(6)

C1(C2(C3	121.7(7)

C1(C2(H2	119.2

C3(C2(H2	119.2

C4(C3(C2	119.6(8)

C4(C3(H3	120.2

C2(C3(H3	120.2

C5(C4(C3	120.2(8)

C5(C4(H4	119.9

C3(C4(H4	119.9

C4(C5(C6	119.7(7)

C4(C5(H5	120.2

C6(C5(H5	120.2

C5(C6(C1	121.9(7)

C5(C6(H6	119.1

C1(C6(H6	119.1

C8(C7(C12	116.7(6)

C8(C7(Si2	121.6(5)

C12(C7(Si2	121.7(5)

C9(C8(C7	121.6(7)

C9(C8(H8	119.2

C7(C8(H8	119.2

C10(C9(C8	120.5(7)

C10(C9(H9	119.7

C8(C9(H9	119.7

C11(C10(C9	119.6(6)

C11(C10(H10	120.2

C9(C10(H10	120.2

C10(C11(C12	119.8(6)

C10(C11(H11	120.1

C12(C11(H11	120.1

C7(C12(C11	121.8(6)

C7(C12(H12	119.1

C11(C12(H12	119.1

C18(C13(C14	114.9(6)

C18(C13(Si3	123.9(5)

C14(C13(Si3	121.1(4)

C15(C14(C13	123.6(6)

C15(C14(H14	118.2

C13(C14(H14	118.2

C14(C15(C16	118.7(6)

C14(C15(H15	120.6

C16(C15(H15	120.6

C17(C16(C15	119.6(6)

C17(C16(H16	120.2

C15(C16(H16	120.2

C18(C17(C16	119.1(6)

C18(C17(H17	120.4

C16(C17(H17	120.4

C17(C18(C13	123.8(6)

C17(C18(H18	118.1

C13(C18(H18	118.1

C24(C19(C20	117.4(6)

C24(C19(Si4	122.7(6)

C20(C19(Si4	120.0(6)

C21(C20(C19	120.8(7)

C21(C20(H20	119.6

C19(C20(H20	119.6

C22(C21(C20	120.0(8)

C22(C21(H21	120.0

C20(C21(H21	120.0

C23(C22(C21	120.4(8)

C23(C22(H22	119.8

C21(C22(H22	119.8

C22(C23(C24	119.8(8)

C22(C23(H23	120.1

C24(C23(H23	120.1

C23(C24(C19	121.5(8)

C23(C24(H24	119.3

C19(C24(H24	119.3

Si5(C25(H25A	109.5

Si5(C25(H25B	109.5

H25A(C25(H25B	109.5

Si5(C25(H25C	109.5

H25A(C25(H25C	109.5

H25B(C25(H25C	109.5

Si5(C26(H26A	109.5

Si5(C26(H26B	109.5

H26A(C26(H26B	109.5

Si5(C26(H26C	109.5

H26A(C26(H26C	109.5

H26B(C26(H26C	109.5

Si6(C27(H27A	109.5

Si6(C27(H27B	109.5

H27A(C27(H27B	109.5

Si6(C27(H27C	109.5

H27A(C27(H27C	109.5

H27B(C27(H27C	109.5

Si6(C28(H28A	109.5

Si6(C28(H28B	109.5

H28A(C28(H28B	109.5

Si6(C28(H28C	109.5

H28A(C28(H28C	109.5

H28B(C28(H28C	109.5

Si7(C29(H29A	109.5

Si7(C29(H29B	109.5

H29A(C29(H29B	109.5

Si7(C29(H29C	109.5

H29A(C29(H29C	109.5

H29B(C29(H29C	109.5

Si7(C30(H30A	109.5

Si7(C30(H30B	109.5

H30A(C30(H30B	109.5

Si7(C30(H30C	109.5

H30A(C30(H30C	109.5

H30B(C30(H30C	109.5

Si8(C31(H31A	109.5

Si8(C31(H31B	109.5

H31A(C31(H31B	109.5

Si8(C31(H31C	109.5

H31A(C31(H31C	109.5

H31B(C31(H31C	109.5

Si8(C32(H32A	109.5

Si8(C32(H32B	109.5

H32A(C32(H32B	109.5

Si8(C32(H32C	109.5

H32A(C32(H32C	109.5

H32B(C32(H32C	109.5

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Si1	34(2) 	32(2)	37(1) 	(4(1)	(1(1) 	(11(1)

Si2	34(2) 	30(2)	36(1) 	(1(1)	(4(1) 	(11(1)

Si3	32(2) 	29(2)	35(1) 	(3(1)	(4(1) 	(9(1)

Si4	35(2) 	34(2)	35(1) 	(3(1)	0(1) 	(14(1)

Si5	104(2) 	61(2)	45(1) 	(16(1)	8(1) 	(32(2)

Si6	68(2) 	47(2)	57(1) 	(4(1)	(19(1) 	(24(2)

Si7	67(2) 	50(2)	41(1) 	5(1)	(18(1) 	(26(2)

Si8	66(2) 	70(2)	44(1) 	13(1)	(7(1) 	(36(2)

O1	20(3) 	34(3)	45(3) 	4(2)	(4(2) 	(3(3)

O2	37(3) 	16(3)	41(2) 	(2(2)	(2(2) 	(8(3)

O3	28(3) 	25(3)	50(3) 	(9(2)	1(2) 	(7(3)

O4	39(3) 	19(4)	47(3) 	(10(2)	0(2) 	(8(3)

O5	35(3) 	33(4)	48(3) 	(5(2)	(6(2) 	(10(3)

O6	43(3) 	27(3)	37(2) 	(4(2)	(8(2) 	(7(3)

O7	27(3) 	35(3)	39(2) 	(3(2)	(10(2) 	(3(3)

O8	47(3) 	48(4)	38(2) 	0(2)	(5(2) 	(20(3)

C1	23(5) 	22(6)	39(4) 	(6(4)	2(3) 	(4(5)

C2	33(6) 	37(7)	50(4) 	(4(4)	(4(4) 	(9(6)

C3	30(6) 	25(6)	76(6) 	(8(5)	(2(4) 	5(5)

C4	41(6) 	51(8)	69(6) 	3(5)	(15(4) 	(14(6)

C5	41(6) 	43(7)	53(5) 	(7(5)	(16(4) 	(9(6)

C6	29(5) 	33(6)	48(4) 	(6(4)	6(4) 	(9(5)

C7	32(5) 	21(5)	40(4) 	(5(3)	(8(3) 	(5(5)

C8	34(5) 	53(6)	44(4) 	3(4)	(5(4) 	(14(5)

C9	45(6) 	46(6)	48(4) 	1(4)	(18(4) 	(9(5)

C10	57(6) 	38(6)	30(4) 	(9(3)	(1(4) 	(18(5)

C11	41(6) 	44(6)	41(4) 	(3(4)	3(4) 	(21(5)

C12	36(5) 	37(6)	41(4) 	(8(4)	(6(3) 	(10(5)

C13	26(5) 	28(6)	34(4) 	2(3)	(9(3) 	(2(4)

C14	41(5) 	35(6)	31(4) 	(4(3)	1(3) 	(12(5)

C15	44(5) 	37(6)	42(4) 	(6(4)	(4(4) 	(12(5)

C16	47(6) 	38(6)	38(4) 	(12(4)	(7(4) 	(3(5)

C17	55(6) 	46(6)	43(4) 	(3(4)	7(4) 	(21(5)

C18	40(5) 	56(6)	34(4) 	(2(4)	(7(3) 	(27(5)

C19	24(5) 	28(6)	34(4) 	(2(3)	(1(3) 	(1(5)

C20	30(5) 	43(7)	48(4) 	(7(4)	5(3) 	(3(5)

C21	54(7) 	43(7)	67(5) 	(10(4)	(3(5) 	(27(6)

C22	42(7) 	84(9)	51(5) 	(16(5)	1(4) 	(34(7)

C23	28(6) 	57(8)	62(5) 	1(5)	(3(4) 	(11(6)

C24	41(6) 	52(7)	47(4) 	(6(4)	3(4) 	(25(6)

C25	260(14) 	54(8)	53(6) 	4(5)	(8(7) 	(4(8)

C26	139(9) 	51(7)	61(5) 	(12(5)	(27(5) 	(20(6)

C27	93(7) 	16(7)	109(7) 	3(5)	(55(6) 	(1(6)

C28	63(6) 	52(7)	97(6) 	(22(5)	(15(5) 	(25(6)

C29	199(11) 	64(8)	54(5) 	(12(5)	(31(6) 	(41(7)

C30	93(7) 	63(7)	55(5) 	6(4)	(1(4) 	(40(6)

C31	109(7) 	73(7)	32(4) 	3(4)	(8(4) 	(38(6)

C32	66(7) 	231(13)	90(7) 	45(8)	6(6) 	(49(8)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H2	(4154	3245	7523	49	1

H3	(5863	4194	6813	58	1

H4	(5828	3189	5795	64	1

H5	(4081	1267	5484	55	1

H6	(2371	337	6185	46	1

H8	(288	1155	5702	53	1

H9	36	2064	4619	57	1

H10	2141	2211	4194	50	1

H11	3930	1450	4865	49	1

H12	3589	597	5971	46	1

H14	713	(4676	6570	44	1

H15	816	(5714	5569	50	1

H16	2248	(5483	4564	53	1

H17	3358	(4037	4562	58	1

H18	3233	(3042	5575	49	1

H20	(1260	(4501	7539	53	1

H21	(2584	(5309	6996	63	1

H22	(4570	(3929	6573	67	1

H23	(5273	(1753	6714	61	1

H24	(3944	(925	7241	54	1

H25A	(1633	(133	9293	210	1

H25B	(2437	689	9969	210	1

H25C	(1005	759	9612	210	1

H26A	(2019	3561	9229	129	1

H26B	(3394	3656	9730	129	1

H26C	(3472	4169	8944	129	1

H27A	1642	3248	7341	111	1

H27B	866	3568	8116	111	1

H27C	207	3071	7563	111	1

H28A	4050	226	8423	102	1

H28B	3544	1703	8600	102	1

H28C	4254	1219	7833	102	1

H29A	2841	(1633	8386	159	1

H29B	2845	(2317	9133	159	1

H29C	1525	(1929	8737	159	1

H30A	1615	(4671	8745	103	1

H30B	2789	(4980	9236	103	1

H30C	3075	(5779	8543	103	1

H31A	25	(3314	9917	105	1

H31B	(1258	(3378	10446	105	1

H31C	(1255	(2035	10134	105	1

H32A	(3982	(1522	9512	203	1

H32B	(4005	(2837	9857	203	1

H32C	(4034	(2600	9038	203	1

H5S	(4200(40)	1920(50)	8980(30)	162	1

H6S	1120(50)	970(50)	8600(20)	162	1

H7S	4730(30)	(4250(50)	8270(30)	162	1

H8S	(1210(50)	(4520(30)	9120(30)	162	1