|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	02src488

Empirical formula 	C32H40N2O8

Formula weight 	580.66

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2

Unit cell dimensions	a = 19.403(2) Å	( = 90°

b = 8.9915(11) Å	( = 93.313(4)°

c = 17.855(2) Å	(  = 90°

Volume	3109.8(7) Å3

Z	4

Density (calculated)	1.240 Mg / m3

Absorption coefficient	0.089 mm(1

F(000)	1240

Crystal	Block; Colourless

Crystal size	0.28 ( 0.16 ( 0.12 mm3

( range for data collection	3.02 ( 25.02°

Index ranges	(22 ( h ( 21, (10 ( k ( 10, (21 ( l ( 21

Reflections collected	9511

Independent reflections	4596 [Rint = 0.1615]

Completeness to ( = 25.02°	94.2 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9894 and 0.9755

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	4596 / 1 / 384

Goodness-of-fit on F2	0.980

Final R indices [F2 > 2((F2)]	R1 = 0.0942, wR2 = 0.2282

R indices (all data)	R1 = 0.1777, wR2 = 0.2782

Absolute structure parameter	(4(3)

Extinction coefficient	0.0055(16)

Largest diff. peak and hole	0.375 and (0.366 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

The absolute structure could not be determined accurately.

All hydrogen atoms are fixed.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

O8	4402(3)	8727(6)	1991(3)	45(1)	1

O6	6123(3)	10904(8)	944(3)	57(2)	1

O7	4916(3)	10966(7)	1921(3)	51(2)	1

O1	8110(3)	7404(7)	2690(4)	62(2)	1

O5	6406(3)	12299(7)	1942(3)	46(1)	1

N1	7328(3)	9710(7)	3773(3)	40(2)	1

N2	6372(3)	9969(7)	2910(3)	38(2)	1

O2	8664(3)	9620(7)	2708(3)	56(2)	1

C30	4952(4)	9644(12)	1952(4)	44(2)	1

O4	6643(3)	7496(7)	798(3)	55(2)	1

C20	8110(4)	8737(11)	2607(5)	46(2)	1

O3	7521(3)	9175(8)	800(4)	66(2)	1

C17	4128(4)	8647(12)	4124(4)	53(2)	1

C8	8046(4)	10035(8)	4946(4)	37(2)	1

C15	5082(4)	10042(11)	3682(4)	48(2)	1

C3	7115(4)	10326(10)	3047(4)	42(2)	1

C14	5466(4)	8763(10)	3658(4)	46(2)	1

C7	7754(4)	10731(10)	4238(5)	46(2)	1

C6	6262(4)	9637(9)	2111(4)	39(2)	1

C26	6256(4)	11113(10)	1671(5)	40(2)	1

C2	6216(4)	8822(10)	3454(4)	38(2)	1

C29	5598(4)	8733(10)	1910(4)	43(2)	1

C13	8579(4)	8935(10)	4900(5)	48(2)	1

C4	7494(4)	9630(9)	2374(4)	43(2)	1

C1	6680(4)	9228(9)	4121(4)	42(2)	1

C23	7077(5)	8528(11)	1117(5)	54(2)	1

C32	3215(4)	8323(11)	2135(5)	56(2)	1

C19	5191(4)	7417(10)	3889(5)	48(2)	1

C11	8672(4)	8608(10)	6218(5)	51(2)	1

C10	8125(5)	9711(12)	6283(5)	65(3)	1

C5	6933(4)	8728(11)	1943(4)	45(2)	1

C22	9808(5)	9575(11)	2266(5)	60(3)	1

C31	3736(4)	9469(10)	2040(5)	50(2)	1

C16	4397(4)	9968(10)	3912(5)	50(2)	1

C24	6700(5)	7246(14)	10(5)	67(3)	1

C21	9351(4)	8916(12)	2830(5)	58(3)	1

C9	7855(4)	10337(9)	5636(5)	39(2)	1

C18	4525(5)	7352(13)	4117(5)	57(3)	1

C27	6128(6)	12190(14)	480(5)	70(3)	1

C12	8874(5)	8319(10)	5524(5)	53(2)	1

C28	6050(8)	11758(15)	(307(6)	91(4)	1

C25	6082(6)	6473(15)	(265(6)	80(3)	1

Table 3. Bond lengths [Å] and angles [°].

O8(C30	1.354(10)

O8(C31	1.460(10)

O6(C26	1.323(10)

O6(C27	1.422(12)

O7(C30	1.192(10)

O1(C20	1.208(11)

O5(C26	1.199(10)

N1(C3	1.448(10)

N1(C7	1.461(10)

N1(C1	1.498(10)

N2(C6	1.461(10)

N2(C2	1.460(10)

N2(C3	1.485(10)

O2(C20	1.339(10)

O2(C21	1.480(10)

C30(C29	1.502(12)

O4(C23	1.356(11)

O4(C24	1.435(11)

C20(C4	1.479(12)

O3(C23	1.206(11)

C17(C16	1.361(13)

C17(C18	1.397(14)

C17(H17	0.9500

C8(C9	1.336(11)

C8(C13	1.438(12)

C8(C7	1.492(12)

C15(C14	1.372(12)

C15(C16	1.413(12)

C15(H15	0.9500

C3(C4	1.574(12)

C3(H3	1.0000

C14(C19	1.395(12)

C14(C2	1.520(11)

C7(H7A	0.9900

C7(H7B	0.9900

C6(C26	1.542(12)

C6(C29	1.548(11)

C6(C5	1.580(11)

C2(C1	1.495(11)

C2(H2	1.0000

C29(H29A	0.9900

C29(H29B	0.9900

C13(C12	1.342(12)

C13(H13	0.9500

C4(C5	1.530(11)

C4(H4	1.0000

C1(H1A	0.9900

C1(H1B	0.9900

C23(C5	1.528(11)

C32(C31	1.460(12)

C32(H32A	0.9800

C32(H32B	0.9800

C32(H32C	0.9800

C19(C18	1.377(12)

C19(H19	0.9500

C11(C12	1.346(12)

C11(C10	1.462(14)

C11(H11	0.9500

C10(C9	1.362(13)

C10(H10	0.9500

C5(H5	1.0000

C22(C21	1.502(12)

C22(H22A	0.9800

C22(H22B	0.9800

C22(H22C	0.9800

C31(H31A	0.9900

C31(H31B	0.9900

C16(H16	0.9500

C24(C25	1.448(14)

C24(H24A	0.9900

C24(H24B	0.9900

C21(H21A	0.9900

C21(H21B	0.9900

C9(H9	0.9500

C18(H18	0.9500

C27(C28	1.457(15)

C27(H27A	0.9900

C27(H27B	0.9900

C12(H12	0.9500

C28(H28A	0.9800

C28(H28B	0.9800

C28(H28C	0.9800

C25(H25A	0.9800

C25(H25B	0.9800

C25(H25C	0.9800

C30(O8(C31	115.4(6)

C26(O6(C27	116.6(7)

C3(N1(C7	113.0(6)

C3(N1(C1	106.2(6)

C7(N1(C1	114.0(6)

C6(N2(C2	118.7(6)

C6(N2(C3	106.9(5)

C2(N2(C3	106.3(6)

C20(O2(C21	118.3(7)

O7(C30(O8	124.4(8)

O7(C30(C29	126.1(8)

O8(C30(C29	109.5(8)

C23(O4(C24	116.0(7)

O1(C20(O2	125.3(8)

O1(C20(C4	124.5(7)

O2(C20(C4	110.2(8)

C16(C17(C18	120.3(8)

C16(C17(H17	119.8

C18(C17(H17	119.8

C9(C8(C13	115.6(7)

C9(C8(C7	125.8(8)

C13(C8(C7	118.6(7)

C14(C15(C16	119.5(8)

C14(C15(H15	120.3

C16(C15(H15	120.3

N1(C3(N2	106.8(6)

N1(C3(C4	114.2(7)

N2(C3(C4	106.3(6)

N1(C3(H3	109.8

N2(C3(H3	109.8

C4(C3(H3	109.8

C15(C14(C19	119.9(7)

C15(C14(C2	120.5(8)

C19(C14(C2	119.3(8)

N1(C7(C8	113.1(7)

N1(C7(H7A	109.0

C8(C7(H7A	109.0

N1(C7(H7B	109.0

C8(C7(H7B	109.0

H7A(C7(H7B	107.8

N2(C6(C26	108.5(7)

N2(C6(C29	114.0(6)

C26(C6(C29	110.6(6)

N2(C6(C5	102.5(6)

C26(C6(C5	109.2(6)

C29(C6(C5	111.6(7)

O5(C26(O6	123.5(8)

O5(C26(C6	124.4(8)

O6(C26(C6	111.9(7)

N2(C2(C1	102.6(7)

N2(C2(C14	114.9(6)

C1(C2(C14	111.0(6)

N2(C2(H2	109.3

C1(C2(H2	109.3

C14(C2(H2	109.3

C30(C29(C6	112.8(7)

C30(C29(H29A	109.0

C6(C29(H29A	109.0

C30(C29(H29B	109.0

C6(C29(H29B	109.0

H29A(C29(H29B	107.8

C12(C13(C8	120.7(9)

C12(C13(H13	119.7

C8(C13(H13	119.7

C20(C4(C5	113.2(7)

C20(C4(C3	114.0(7)

C5(C4(C3	104.2(6)

C20(C4(H4	108.4

C5(C4(H4	108.4

C3(C4(H4	108.4

N1(C1(C2	102.9(6)

N1(C1(H1A	111.2

C2(C1(H1A	111.2

N1(C1(H1B	111.2

C2(C1(H1B	111.2

H1A(C1(H1B	109.1

O3(C23(O4	125.1(8)

O3(C23(C5	124.8(9)

O4(C23(C5	110.0(8)

C31(C32(H32A	109.5

C31(C32(H32B	109.5

H32A(C32(H32B	109.5

C31(C32(H32C	109.5

H32A(C32(H32C	109.5

H32B(C32(H32C	109.5

C18(C19(C14	120.4(9)

C18(C19(H19	119.8

C14(C19(H19	119.8

C12(C11(C10	117.1(8)

C12(C11(H11	121.4

C10(C11(H11	121.4

C9(C10(C11	117.3(9)

C9(C10(H10	121.4

C11(C10(H10	121.4

C23(C5(C4	112.6(7)

C23(C5(C6	116.4(6)

C4(C5(C6	101.6(6)

C23(C5(H5	108.7

C4(C5(H5	108.7

C6(C5(H5	108.7

C21(C22(H22A	109.5

C21(C22(H22B	109.5

H22A(C22(H22B	109.5

C21(C22(H22C	109.5

H22A(C22(H22C	109.5

H22B(C22(H22C	109.5

O8(C31(C32	107.8(7)

O8(C31(H31A	110.1

C32(C31(H31A	110.1

O8(C31(H31B	110.1

C32(C31(H31B	110.1

H31A(C31(H31B	108.5

C17(C16(C15	120.2(8)

C17(C16(H16	119.9

C15(C16(H16	119.9

O4(C24(C25	107.4(8)

O4(C24(H24A	110.2

C25(C24(H24A	110.2

O4(C24(H24B	110.2

C25(C24(H24B	110.2

H24A(C24(H24B	108.5

O2(C21(C22	107.1(7)

O2(C21(H21A	110.3

C22(C21(H21A	110.3

O2(C21(H21B	110.3

C22(C21(H21B	110.3

H21A(C21(H21B	108.5

C8(C9(C10	125.8(9)

C8(C9(H9	117.1

C10(C9(H9	117.1

C19(C18(C17	119.6(9)

C19(C18(H18	120.2

C17(C18(H18	120.2

O6(C27(C28	109.9(10)

O6(C27(H27A	109.7

C28(C27(H27A	109.7

O6(C27(H27B	109.7

C28(C27(H27B	109.7

H27A(C27(H27B	108.2

C13(C12(C11	123.5(10)

C13(C12(H12	118.3

C11(C12(H12	118.3

C27(C28(H28A	109.5

C27(C28(H28B	109.5

H28A(C28(H28B	109.5

C27(C28(H28C	109.5

H28A(C28(H28C	109.5

H28B(C28(H28C	109.5

C24(C25(H25A	109.5

C24(C25(H25B	109.5

H25A(C25(H25B	109.5

C24(C25(H25C	109.5

H25A(C25(H25C	109.5

H25B(C25(H25C	109.5

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

O8	18(3) 	39(3)	77(4) 	1(3)	6(2) 	3(3)

O6	45(4) 	78(5)	48(4) 	6(3)	6(3) 	(5(3)

O7	26(3) 	32(4)	95(4) 	5(3)	5(3) 	(2(3)

O1	30(3) 	41(4)	116(5) 	2(3)	13(3) 	4(3)

O5	23(3) 	46(4)	69(4) 	7(3)	1(3) 	(3(3)

N1	23(4) 	35(4)	60(4) 	4(3)	1(3) 	(7(3)

N2	22(4) 	42(4)	50(4) 	4(3)	2(3) 	(1(3)

O2	23(3) 	44(4)	101(4) 	5(3)	8(3) 	10(3)

C30	28(5) 	53(7)	51(5) 	0(4)	1(4) 	0(5)

O4	33(3) 	66(4)	68(4) 	(18(3)	12(3) 	(11(3)

C20	17(5) 	42(6)	82(6) 	(3(5)	14(4) 	(18(4)

O3	39(4) 	81(5)	81(4) 	(5(3)	20(3) 	(15(3)

C17	23(5) 	72(7)	64(5) 	(6(5)	9(4) 	(20(5)

C8	27(5) 	26(5)	60(5) 	5(4)	3(4) 	(17(4)

C15	26(5) 	63(6)	56(5) 	(6(4)	8(4) 	(9(5)

C3	13(4) 	52(5)	63(5) 	(4(4)	8(4) 	(12(4)

C14	24(5) 	51(6)	62(5) 	0(4)	(2(4) 	(5(5)

C7	25(5) 	38(6)	76(6) 	3(4)	3(4) 	(6(4)

C6	14(4) 	41(5)	62(5) 	6(4)	10(3) 	2(4)

C26	11(4) 	42(6)	66(6) 	(3(4)	9(4) 	(5(4)

C2	26(5) 	44(5)	46(4) 	6(4)	7(3) 	8(4)

C29	21(4) 	42(5)	66(5) 	(8(4)	6(4) 	(6(4)

C13	38(5) 	46(6)	59(5) 	5(4)	0(4) 	(10(5)

C4	22(4) 	38(5)	70(5) 	10(4)	4(4) 	1(4)

C1	22(4) 	42(5)	62(5) 	4(4)	11(4) 	(3(4)

C23	35(6) 	52(6)	75(6) 	(8(5)	11(5) 	8(5)

C32	21(5) 	64(7)	82(6) 	1(5)	3(4) 	(9(4)

C19	28(5) 	49(6)	67(5) 	4(5)	2(4) 	(4(4)

C11	37(5) 	39(5)	75(6) 	14(5)	(15(4) 	(20(5)

C10	59(7) 	76(8)	62(6) 	(11(5)	3(5) 	(53(6)

C5	25(5) 	56(6)	54(5) 	(2(4)	1(4) 	1(4)

C22	31(5) 	60(7)	91(7) 	8(5)	11(5) 	15(5)

C31	28(5) 	45(5)	78(6) 	(3(4)	5(4) 	(17(4)

C16	19(5) 	43(6)	86(6) 	(12(4)	4(4) 	(2(4)

C24	45(6) 	89(8)	67(6) 	(24(6)	13(5) 	(9(6)

C21	23(5) 	63(7)	89(6) 	(6(5)	9(4) 	12(5)

C9	33(5) 	21(4)	63(6) 	1(4)	3(4) 	(19(4)

C18	29(5) 	71(7)	70(6) 	12(5)	(1(4) 	(11(5)

C27	59(7) 	104(9)	47(6) 	18(6)	1(5) 	(12(6)

C12	52(6) 	37(6)	70(7) 	9(4)	(7(5) 	(28(4)

C28	112(11) 	80(9)	80(8) 	6(6)	1(7) 	(1(8)

C25	62(8) 	90(9)	86(8) 	(8(6)	(1(6) 	(32(7)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H17	3668	8605	4277	63	1

H15	5274	10968	3546	58	1

H3	7182	11429	3054	51	1

H7A	7472	11602	4366	56	1

H7B	8138	11092	3945	56	1

H2	6354	7829	3261	46	1

H29A	5620	8332	1396	52	1

H29B	5577	7879	2258	52	1

H13	8725	8641	4423	57	1

H4	7641	10456	2044	52	1

H1A	6481	10048	4409	50	1

H1B	6765	8363	4456	50	1

H32A	3202	7648	1703	83	1

H32B	2762	8792	2169	83	1

H32C	3331	7761	2595	83	1

H19	5464	6541	3890	57	1

H11	8876	8117	6646	61	1

H10	7964	9979	6758	79	1

H5	6904	7724	2180	54	1

H22A	9609	9383	1759	91	1

H22B	10268	9122	2325	91	1

H22C	9847	10651	2347	91	1

H31A	3623	10047	1578	60	1

H31B	3753	10160	2473	60	1

H16	4125	10845	3919	59	1

H24A	7114	6637	(75	80	1

H24B	6743	8205	(256	80	1

H21A	9314	7826	2760	70	1

H21B	9543	9116	3346	70	1

H9	7500	11053	5681	47	1

H18	4337	6431	4269	68	1

H27A	6568	12733	575	84	1

H27B	5746	12860	602	84	1

H12	9245	7643	5473	64	1

H28A	6408	11035	(416	136	1

H28B	6095	12639	(624	136	1

H28C	5594	11310	(410	136	1

H25A	6042	5531	6	119	1

H25B	6107	6271	(802	119	1

H25C	5677	7092	(185	119	1