|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	04src0076    (iBuMIMPF6)

Empirical formula 	C12H17F6N2P

Formula weight 	334.25

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/n

Unit cell dimensions	a = 10.8197(5) Å	( = 90°

b = 11.9252(7) Å	( = 92.577(4)°

c = 11.2662(6) Å	(  = 90°

Volume	1452.17(13) Å3

Z	4

Density (calculated)	1.529 Mg / m3

Absorption coefficient	0.250 mm(1

F(000)	688

Crystal	block; colourless

Crystal size	0.60 ( 0.60 ( 0.40 mm3

( range for data collection	2.49 ( 20.61°

Index ranges	(10 ( h ( 10, (11 ( k ( 11, (11 ( l ( 11

Reflections collected	15921

Independent reflections	1469 [Rint = 0.0692]

Completeness to ( = 20.61°	99.5 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9067 and 0.8646

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	1469 / 0 / 194

Goodness-of-fit on F2	1.273

Final R indices [F2 > 2((F2)]	R1 = 0.0385, wR2 = 0.1022

R indices (all data)	R1 = 0.0406, wR2 = 0.1042

Extinction coefficient	0.070(6)

Largest diff. peak and hole	0.292 and (0.328 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	5208(2)	(1154(2)	3808(2)	25(1)	1

C2	5769(2)	(1872(2)	4642(2)	32(1)	1

C3	5055(3)	(2188(2)	5564(2)	37(1)	1

C4	3841(3)	(1829(2)	5654(2)	37(1)	1

C5	3280(2)	(1129(2)	4829(2)	32(1)	1

C6	3995(2)	(793(2)	3902(2)	25(1)	1

C7	4751(2)	2(2)	2343(2)	30(1)	1

C8	6892(3)	(745(3)	2376(2)	43(1)	1

C9	2578(2)	548(2)	2737(2)	32(1)	1

C10	1651(2)	(116(2)	1970(2)	30(1)	1

C11	1982(3)	(79(2)	670(2)	36(1)	1

C12	356(2)	327(3)	2134(3)	41(1)	1

N1	5649(2)	(637(2)	2812(2)	28(1)	1

N2	3749(2)	(56(2)	2963(2)	25(1)	1

F1	1381(1)	2943(1)	6054(1)	41(1)	1

F2	859(2)	1223(1)	5343(2)	48(1)	1

F3	1228(1)	2626(1)	4071(1)	40(1)	1

F4	(718(1)	1994(1)	4238(1)	45(1)	1

F5	(178(2)	3710(1)	4939(1)	42(1)	1

F6	(560(2)	2312(1)	6217(1)	46(1)	1

P1	332(1)	2455(1)	5140(1)	31(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(N1	1.385(3)

C1(C2	1.390(4)

C1(C6	1.390(4)

C2(C3	1.375(4)

C3(C4	1.389(4)

C4(C5	1.371(4)

C5(C6	1.386(4)

C6(N2	1.392(3)

C7(N2	1.318(3)

C7(N1	1.326(3)

C8(N1	1.457(3)

C9(N2	1.470(3)

C9(C10	1.517(4)

C10(C12	1.516(4)

C10(C11	1.524(4)

F1(P1	1.6069(16)

F2(P1	1.5892(17)

F3(P1	1.5923(16)

F4(P1	1.5882(17)

F5(P1	1.6069(16)

F6(P1	1.5938(16)

N1(C1(C2	131.8(2)

N1(C1(C6	106.6(2)

C2(C1(C6	121.6(2)

C3(C2(C1	115.8(3)

C2(C3(C4	122.4(3)

C5(C4(C3	122.0(3)

C4(C5(C6	116.2(3)

C5(C6(N2	131.4(2)

C5(C6(C1	121.9(2)

N2(C6(C1	106.6(2)

N2(C7(N1	111.3(2)

N2(C9(C10	112.7(2)

C12(C10(C9	109.9(2)

C12(C10(C11	111.4(2)

C9(C10(C11	110.8(2)

C7(N1(C1	107.8(2)

C7(N1(C8	126.0(2)

C1(N1(C8	126.2(2)

C7(N2(C6	107.6(2)

C7(N2(C9	127.3(2)

C6(N2(C9	125.1(2)

F2(P1(F4	90.78(9)

F2(P1(F3	89.99(9)

F4(P1(F3	90.14(8)

F2(P1(F6	90.97(9)

F4(P1(F6	90.54(9)

F3(P1(F6	178.81(9)

F2(P1(F5	179.04(9)

F4(P1(F5	90.03(9)

F3(P1(F5	89.50(8)

F6(P1(F5	89.52(9)

F2(P1(F1	90.23(9)

F4(P1(F1	178.96(9)

F3(P1(F1	90.14(9)

F6(P1(F1	89.16(9)

F5(P1(F1	88.96(9)

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	30(2) 	25(2)	20(2) 	(4(1)	(2(1) 	(2(1)

C2	34(2) 	29(2)	32(2) 	(5(1)	(6(1) 	1(1)

C3	45(2) 	29(2)	35(2) 	5(1)	(9(1) 	(5(1)

C4	44(2) 	39(2)	29(2) 	6(1)	2(1) 	(15(2)

C5	30(2) 	35(2)	32(2) 	(5(1)	0(1) 	(7(1)

C6	30(2) 	24(2)	21(2) 	(4(1)	(2(1) 	(5(1)

C7	36(2) 	33(2)	20(2) 	(1(1)	(2(1) 	1(1)

C8	32(2) 	62(2)	35(2) 	(4(1)	8(1) 	4(1)

C9	33(2) 	31(2)	32(2) 	(2(1)	(2(1) 	8(1)

C10	35(2) 	28(2)	28(2) 	2(1)	(4(1) 	2(1)

C11	40(2) 	39(2)	29(2) 	(1(1)	(5(1) 	3(1)

C12	33(2) 	55(2)	35(2) 	(2(2)	(4(1) 	5(2)

N1	27(1) 	35(1)	23(1) 	(3(1)	1(1) 	2(1)

N2	27(1) 	26(1)	21(1) 	(2(1)	(2(1) 	0(1)

F1	37(1) 	48(1)	39(1) 	(7(1)	(5(1) 	0(1)

F2	61(1) 	33(1)	50(1) 	3(1)	1(1) 	6(1)

F3	41(1) 	42(1)	39(1) 	(6(1)	14(1) 	(4(1)

F4	35(1) 	59(1)	42(1) 	(12(1)	(1(1) 	(6(1)

F5	56(1) 	38(1)	31(1) 	(2(1)	3(1) 	15(1)

F6	46(1) 	58(1)	35(1) 	1(1)	15(1) 	(6(1)

P1	30(1) 	33(1)	30(1) 	(2(1)	4(1) 	1(1)