|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	03src0062

Empirical formula 	C36H35CrN15O5.50

Formula weight 	817.79

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 10.138(5) Å	( = 105.284(5)°

b = 11.861(5) Å	( = 93.568(5)°

c = 17.072(5) Å	(  = 110.991(5)°

Volume	1820.6(13) Å3

Z	2

Density (calculated)	1.492 Mg / m3

Absorption coefficient	0.383 mm(1

F(000)	848

Crystal	Rod; Yellow

Crystal size	0.28 ( 0.08 ( 0.04 mm3

( range for data collection	3.03 ( 27.48°

Index ranges	(13 ( h ( 13, (15 ( k ( 15, (22 ( l ( 20

Reflections collected	38174

Independent reflections	8330 [Rint = 0.0850]

Completeness to ( = 27.48°	99.6 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9848 and 0.9003

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	8330 / 18 / 559

Goodness-of-fit on F2	1.078

Final R indices [F2 > 2((F2)]	R1 = 0.0595, wR2 = 0.1322

R indices (all data)	R1 = 0.0902, wR2 = 0.1443

Largest diff. peak and hole	0.467 and (0.525 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

All hydrogen atoms were fixed.

There are 5½ molecules of water in the asymmetric unit.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Cr1	7755(1)	3765(1)	2484(1)	23(1)	1

C1	6861(3)	5549(2)	2015(2)	24(1)	1

C2	6986(3)	5468(3)	782(2)	26(1)	1

C3	6667(3)	5780(3)	2875(2)	28(1)	1

C4	6134(3)	6642(3)	3289(2)	33(1)	1

C5	5960(3)	6717(3)	4098(2)	38(1)	1

C6	6307(3)	5937(3)	4465(2)	38(1)	1

C7	6853(3)	5094(3)	4015(2)	32(1)	1

C8	6881(3)	5736(3)	(4(2)	27(1)	1

C9	6444(3)	6691(3)	(75(2)	30(1)	1

C10	6316(3)	6899(3)	(829(2)	32(1)	1

C11	6630(3)	6151(3)	(1499(2)	33(1)	1

C12	7060(3)	5221(3)	(1378(2)	35(1)	1

N1	7289(2)	4605(2)	1688(1)	25(1)	1

N2	7379(2)	4539(2)	887(1)	27(1)	1

N3	6653(2)	6126(2)	1472(1)	26(1)	1

N4	7037(2)	5013(2)	3238(1)	25(1)	1

N5	7200(3)	5001(2)	(651(2)	33(1)	1

C21	9834(3)	3940(3)	3777(2)	26(1)	1

C22	8999(3)	2512(3)	4319(2)	28(1)	1

C23	10635(3)	5025(3)	3503(2)	26(1)	1

C24	11993(3)	5903(3)	3870(2)	32(1)	1

C25	12610(3)	6920(3)	3570(2)	34(1)	1

C26	11849(3)	7003(3)	2900(2)	32(1)	1

C27	10496(3)	6083(3)	2554(2)	28(1)	1

C28	8846(3)	1711(3)	4867(2)	32(1)	1

C29	10004(4)	1847(3)	5406(2)	40(1)	1

C30	9792(4)	1083(3)	5914(2)	49(1)	1

C31	8439(4)	225(3)	5869(2)	49(1)	1

C32	7322(4)	140(3)	5316(2)	48(1)	1

N21	8473(2)	3245(2)	3389(1)	25(1)	1

N22	7920(2)	2306(2)	3743(1)	27(1)	1

N23	10231(3)	3522(2)	4366(1)	31(1)	1

N24	9874(2)	5110(2)	2850(1)	24(1)	1

N25	7503(3)	859(2)	4810(2)	42(1)	1

C41	5698(3)	1287(3)	1613(2)	25(1)	1

C42	3702(3)	990(3)	1969(2)	26(1)	1

C43	6972(3)	1297(2)	1245(2)	24(1)	1

C44	7047(3)	307(3)	629(2)	29(1)	1

C45	8319(3)	501(3)	313(2)	33(1)	1

C46	9452(3)	1658(3)	621(2)	35(1)	1

C47	9319(3)	2595(3)	1249(2)	31(1)	1

C48	2156(3)	431(3)	2007(2)	30(1)	1

C49	1549(3)	1203(3)	2417(2)	29(1)	1

C50	124(3)	700(4)	2440(2)	45(1)	1

C51	(709(3)	(560(4)	2045(2)	45(1)	1

C52	(51(3)	(1323(3)	1635(2)	44(1)	1

N41	5841(2)	2339(2)	2204(1)	25(1)	1

N42	4544(2)	2157(2)	2445(1)	27(1)	1

N43	4366(2)	397(2)	1431(1)	27(1)	1

N44	8116(2)	2430(2)	1565(1)	24(1)	1

N45	1393(3)	(839(3)	1609(2)	47(1)	1

O1W	4047(2)	(2057(2)	343(2)	44(1)	1

O2W	5184(3)	2348(3)	4290(1)	49(1)	1

O3W	5514(3)	(1923(3)	1836(2)	57(1)	1

O4W	5143(3)	(735(3)	3421(2)	68(1)	1

O5W	9199(4)	3741(4)	(691(2)	90(1)	1

O6W	6965(9)	6513(8)	6349(5)	99(2)	0.50

Table 3. Bond lengths [Å] and angles [°].

Cr1(N41	1.990(2)

Cr1(N21	1.996(2)

Cr1(N1	2.008(2)

Cr1(N4	2.065(2)

Cr1(N44	2.068(2)

Cr1(N24	2.098(2)

C1(N3	1.335(3)

C1(N1	1.343(3)

C1(C3	1.460(4)

C2(N2	1.346(3)

C2(N3	1.366(3)

C2(C8	1.465(4)

C3(N4	1.365(3)

C3(C4	1.378(4)

C4(C5	1.388(4)

C4(H4	0.9500

C5(C6	1.373(4)

C5(H5	0.9500

C6(C7	1.393(4)

C6(H6	0.9500

C7(N4	1.334(4)

C7(H7	0.9500

C8(N5	1.350(4)

C8(C9	1.386(4)

C9(C10	1.381(4)

C9(H9	0.9500

C10(C11	1.382(4)

C10(H10	0.9500

C11(C12	1.379(4)

C11(H11	0.9500

C12(N5	1.344(4)

C12(H12	0.9500

N1(N2	1.361(3)

C21(N23	1.332(3)

C21(N21	1.344(3)

C21(C23	1.465(4)

C22(N22	1.331(4)

C22(N23	1.367(4)

C22(C28	1.477(4)

C23(N24	1.364(3)

C23(C24	1.377(4)

C24(C25	1.390(4)

C24(H24	0.9500

C25(C26	1.385(4)

C25(H25	0.9500

C26(C27	1.381(4)

C26(H26	0.9500

C27(N24	1.345(3)

C27(H27	0.9500

C28(N25	1.352(4)

C28(C29	1.380(4)

C29(C30	1.385(4)

C29(H29	0.9500

C30(C31	1.366(5)

C30(H30	0.9500

C31(C32	1.384(5)

C31(H31	0.9500

C32(N25	1.344(4)

C32(H32	0.9500

N21(N22	1.367(3)

C41(N43	1.337(3)

C41(N41	1.336(4)

C41(C43	1.469(4)

C42(N42	1.334(4)

C42(N43	1.366(4)

C42(C48	1.480(4)

C43(N44	1.366(3)

C43(C44	1.384(4)

C44(C45	1.395(4)

C44(H44	0.9500

C45(C46	1.377(4)

C45(H45	0.9500

C46(C47	1.378(4)

C46(H46	0.9500

C47(N44	1.336(3)

C47(H47	0.9500

C48(C49	1.351(4)

C48(N45	1.375(4)

C49(C50	1.359(4)

C49(H49	0.9500

C50(C51	1.376(5)

C50(H50	0.9500

C51(C52	1.383(5)

C51(H51	0.9500

C52(N45	1.376(4)

C52(H52	0.9500

N41(N42	1.362(3)

O1W(H1WA	0.842(5)

O1W(H1WB	0.843(5)

O2W(H2WA	0.840(5)

O2W(H2WB	0.841(5)

O3W(H3WA	0.844(5)

O3W(H3WB	0.845(5)

O4W(H4WA	0.846(5)

O4W(H4WB	0.843(5)

O5W(H5WA	0.844(5)

O5W(H5WB	0.844(5)

O6W(H6WA	0.841(5)

O6W(H6WB	0.841(5)

N41(Cr1(N21	94.01(9)

N41(Cr1(N1	95.31(9)

N21(Cr1(N1	169.60(9)

N41(Cr1(N4	93.12(9)

N21(Cr1(N4	95.31(9)

N1(Cr1(N4	79.58(9)

N41(Cr1(N44	79.35(9)

N21(Cr1(N44	93.66(9)

N1(Cr1(N44	92.60(9)

N4(Cr1(N44	168.68(9)

N41(Cr1(N24	172.08(9)

N21(Cr1(N24	78.70(9)

N1(Cr1(N24	92.22(9)

N4(Cr1(N24	90.65(9)

N44(Cr1(N24	97.87(9)

N3(C1(N1	112.5(2)

N3(C1(C3	130.0(2)

N1(C1(C3	117.4(2)

N2(C2(N3	114.0(2)

N2(C2(C8	123.6(2)

N3(C2(C8	122.4(2)

N4(C3(C4	122.1(3)

N4(C3(C1	112.7(2)

C4(C3(C1	125.1(3)

C3(C4(C5	118.4(3)

C3(C4(H4	120.8

C5(C4(H4	120.8

C6(C5(C4	119.9(3)

C6(C5(H5	120.0

C4(C5(H5	120.0

C5(C6(C7	118.8(3)

C5(C6(H6	120.6

C7(C6(H6	120.6

N4(C7(C6	122.2(3)

N4(C7(H7	118.9

C6(C7(H7	118.9

N5(C8(C9	122.1(3)

N5(C8(C2	117.2(2)

C9(C8(C2	120.7(3)

C10(C9(C8	119.5(3)

C10(C9(H9	120.3

C8(C9(H9	120.3

C9(C10(C11	119.2(3)

C9(C10(H10	120.4

C11(C10(H10	120.4

C12(C11(C10	117.8(3)

C12(C11(H11	121.1

C10(C11(H11	121.1

N5(C12(C11	124.2(3)

N5(C12(H12	117.9

C11(C12(H12	117.9

C1(N1(N2	108.0(2)

C1(N1(Cr1	115.08(17)

N2(N1(Cr1	136.78(18)

C2(N2(N1	103.8(2)

C1(N3(C2	101.7(2)

C7(N4(C3	118.6(2)

C7(N4(Cr1	126.34(19)

C3(N4(Cr1	115.02(18)

C12(N5(C8	117.1(3)

N23(C21(N21	113.1(2)

N23(C21(C23	130.3(2)

N21(C21(C23	116.5(2)

N22(C22(N23	114.7(2)

N22(C22(C28	121.8(3)

N23(C22(C28	123.5(3)

N24(C23(C24	122.2(2)

N24(C23(C21	112.9(2)

C24(C23(C21	124.9(2)

C23(C24(C25	119.1(3)

C23(C24(H24	120.5

C25(C24(H24	120.5

C26(C25(C24	118.9(3)

C26(C25(H25	120.5

C24(C25(H25	120.5

C27(C26(C25	119.2(3)

C27(C26(H26	120.4

C25(C26(H26	120.4

N24(C27(C26	122.5(3)

N24(C27(H27	118.7

C26(C27(H27	118.7

N25(C28(C29	122.9(3)

N25(C28(C22	115.6(3)

C29(C28(C22	121.5(3)

C28(C29(C30	119.0(3)

C28(C29(H29	120.5

C30(C29(H29	120.5

C31(C30(C29	118.8(3)

C31(C30(H30	120.6

C29(C30(H30	120.6

C30(C31(C32	119.4(3)

C30(C31(H31	120.3

C32(C31(H31	120.3

N25(C32(C31	123.0(3)

N25(C32(H32	118.5

C31(C32(H32	118.5

C21(N21(N22	107.2(2)

C21(N21(Cr1	117.01(17)

N22(N21(Cr1	135.83(18)

C22(N22(N21	103.9(2)

C21(N23(C22	101.1(2)

C27(N24(C23	118.0(2)

C27(N24(Cr1	126.98(18)

C23(N24(Cr1	114.74(17)

C32(N25(C28	117.0(3)

N43(C41(N41	113.0(2)

N43(C41(C43	130.3(3)

N41(C41(C43	116.7(2)

N42(C42(N43	114.8(2)

N42(C42(C48	121.4(3)

N43(C42(C48	123.7(3)

N44(C43(C44	121.9(2)

N44(C43(C41	112.5(2)

C44(C43(C41	125.6(2)

C43(C44(C45	118.3(3)

C43(C44(H44	120.8

C45(C44(H44	120.8

C46(C45(C44	119.4(3)

C46(C45(H45	120.3

C44(C45(H45	120.3

C45(C46(C47	119.3(3)

C45(C46(H46	120.3

C47(C46(H46	120.3

N44(C47(C46	122.4(3)

N44(C47(H47	118.8

C46(C47(H47	118.8

C49(C48(N45	122.8(3)

C49(C48(C42	118.3(3)

N45(C48(C42	118.9(3)

C48(C49(C50	118.5(3)

C48(C49(H49	120.7

C50(C49(H49	120.7

C49(C50(C51	121.7(3)

C49(C50(H50	119.1

C51(C50(H50	119.1

C50(C51(C52	118.2(3)

C50(C51(H51	120.9

C52(C51(H51	120.9

N45(C52(C51	121.2(3)

N45(C52(H52	119.4

C51(C52(H52	119.4

C41(N41(N42	107.7(2)

C41(N41(Cr1	116.49(17)

N42(N41(Cr1	135.70(18)

C42(N42(N41	103.6(2)

C41(N43(C42	100.9(2)

C47(N44(C43	118.6(2)

C47(N44(Cr1	126.35(19)

C43(N44(Cr1	114.99(17)

C48(N45(C52	117.5(3)

H1WA(O1W(H1WB	106.5(9)

H2WA(O2W(H2WB	106.8(9)

H3WA(O3W(H3WB	106.2(9)

H4WA(O4W(H4WB	105.8(9)

H5WA(O5W(H5WB	106.0(9)

H6WA(O6W(H6WB	106.8(9)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Cr1	19(1) 	24(1)	27(1) 	11(1)	5(1) 	7(1)

C1	17(1) 	24(1)	32(1) 	12(1)	5(1) 	6(1)

C2	19(1) 	28(2)	30(1) 	12(1)	7(1) 	7(1)

C3	20(1) 	28(2)	33(2) 	11(1)	5(1) 	7(1)

C4	29(2) 	35(2)	39(2) 	13(1)	9(1) 	15(1)

C5	35(2) 	40(2)	40(2) 	7(1)	13(1) 	17(1)

C6	38(2) 	48(2)	33(2) 	16(1)	18(1) 	17(2)

C7	31(2) 	33(2)	36(2) 	16(1)	10(1) 	11(1)

C8	18(1) 	29(2)	33(2) 	12(1)	5(1) 	7(1)

C9	28(2) 	30(2)	33(2) 	11(1)	9(1) 	13(1)

C10	28(2) 	32(2)	40(2) 	18(1)	7(1) 	12(1)

C11	24(1) 	42(2)	33(2) 	19(1)	7(1) 	9(1)

C12	33(2) 	41(2)	32(2) 	11(1)	12(1) 	16(1)

N1	21(1) 	27(1)	28(1) 	12(1)	5(1) 	8(1)

N2	22(1) 	31(1)	30(1) 	13(1)	6(1) 	9(1)

N3	22(1) 	29(1)	30(1) 	12(1)	7(1) 	9(1)

N4	21(1) 	26(1)	28(1) 	11(1)	6(1) 	6(1)

N5	33(1) 	36(1)	34(1) 	14(1)	10(1) 	16(1)

C21	23(1) 	28(2)	29(1) 	10(1)	6(1) 	9(1)

C22	31(2) 	26(2)	29(1) 	10(1)	8(1) 	11(1)

C23	24(1) 	26(1)	30(1) 	10(1)	10(1) 	12(1)

C24	25(1) 	34(2)	34(2) 	12(1)	4(1) 	9(1)

C25	23(1) 	33(2)	41(2) 	10(1)	6(1) 	6(1)

C26	29(2) 	28(2)	40(2) 	14(1)	14(1) 	9(1)

C27	25(1) 	29(2)	34(2) 	15(1)	11(1) 	11(1)

C28	40(2) 	27(2)	29(2) 	11(1)	9(1) 	13(1)

C29	41(2) 	43(2)	40(2) 	19(2)	6(1) 	17(2)

C30	66(2) 	54(2)	41(2) 	24(2)	11(2) 	33(2)

C31	76(3) 	41(2)	40(2) 	24(2)	19(2) 	25(2)

C32	63(2) 	32(2)	41(2) 	15(2)	17(2) 	6(2)

N21	22(1) 	25(1)	28(1) 	11(1)	7(1) 	7(1)

N22	27(1) 	27(1)	31(1) 	16(1)	10(1) 	10(1)

N23	30(1) 	31(1)	31(1) 	14(1)	3(1) 	9(1)

N24	22(1) 	25(1)	27(1) 	10(1)	8(1) 	10(1)

N25	46(2) 	35(2)	40(2) 	19(1)	11(1) 	5(1)

C41	22(1) 	26(1)	28(1) 	13(1)	4(1) 	8(1)

C42	21(1) 	31(2)	30(1) 	17(1)	6(1) 	9(1)

C43	23(1) 	25(1)	28(1) 	12(1)	4(1) 	9(1)

C44	25(1) 	29(2)	32(2) 	9(1)	2(1) 	9(1)

C45	38(2) 	34(2)	33(2) 	10(1)	9(1) 	19(1)

C46	30(2) 	44(2)	38(2) 	15(1)	15(1) 	20(1)

C47	22(1) 	34(2)	38(2) 	15(1)	8(1) 	9(1)

C48	22(1) 	37(2)	33(2) 	21(1)	5(1) 	7(1)

C49	18(1) 	35(2)	37(2) 	19(1)	8(1) 	9(1)

C50	34(2) 	65(2)	50(2) 	31(2)	15(2) 	26(2)

C51	22(2) 	66(2)	51(2) 	37(2)	9(1) 	8(2)

C52	28(2) 	50(2)	48(2) 	23(2)	6(1) 	4(2)

N41	20(1) 	29(1)	30(1) 	13(1)	9(1) 	11(1)

N42	20(1) 	34(1)	32(1) 	17(1)	10(1) 	11(1)

N43	21(1) 	28(1)	34(1) 	13(1)	6(1) 	7(1)

N44	20(1) 	26(1)	30(1) 	12(1)	6(1) 	8(1)

N45	32(1) 	57(2)	49(2) 	26(2)	9(1) 	9(1)

O1W	41(1) 	35(1)	53(2) 	8(1)	1(1) 	14(1)

O2W	49(2) 	59(2)	48(1) 	23(1)	24(1) 	24(1)

O3W	65(2) 	67(2)	46(1) 	13(1)	6(1) 	37(2)

O4W	56(2) 	58(2)	61(2) 	7(2)	16(1) 	(3(1)

O5W	105(3) 	129(3)	98(3) 	69(3)	58(2) 	85(3)

O6W	85(5) 	103(6)	80(5) 	(11(4)	20(4) 	33(5)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H4	5891	7172	3026	39	1

H5	5602	7309	4399	45	1

H6	6177	5970	5016	46	1

H7	7103	4559	4269	39	1

H9	6233	7199	392	36	1

H10	6015	7550	(887	38	1

H11	6553	6273	(2025	39	1

H12	7270	4702	(1839	42	1

H24	12502	5816	4322	38	1

H25	13539	7547	3820	41	1

H26	12253	7685	2680	38	1

H27	9985	6140	2090	33	1

H29	10932	2455	5429	48	1

H30	10573	1154	6288	58	1

H31	8267	(307	6212	58	1

H32	6385	(455	5294	57	1

H44	6253	(486	427	35	1

H45	8402	(160	(112	40	1

H46	10318	1809	403	42	1

H47	10112	3386	1465	37	1

H49	2107	2078	2683	35	1

H50	(308	1231	2736	54	1

H51	(1709	(895	2054	54	1

H52	(605	(2198	1367	53	1

H1WA	3750(30)	(1500(20)	580(20)	67	1

H1WB	3310(20)	(2724(18)	120(20)	67	1

H2WA	5820(30)	2080(40)	4140(20)	74	1

H2WB	4710(40)	2330(40)	3860(12)	74	1

H3WA	5240(40)	(1640(40)	2275(12)	86	1

H3WB	4870(30)	(2050(40)	1445(14)	86	1

H4WA	5370(50)	(730(40)	2953(11)	102	1

H4WB	5820(30)	(130(30)	3768(18)	102	1

H5WA	9000(60)	4380(30)	(510(40)	135	1

H5WB	8470(40)	3110(30)	(690(40)	135	1

H6WA	6620(150)	6160(90)	6700(50)	148	0.50

H6WB	7050(150)	7270(40)	6530(70)	148	0.50