|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	03src0134

Empirical formula 	C60H66F18N30O34Pb4S6

Formula weight 	3114.55

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 12.78640(10) Å	( = 99.36°

b = 17.18250(10) Å	( = 99.42°

c = 22.74430(10) Å	(  = 99.68°

Volume	4765.68(5) Å3

Z	2

Density (calculated)	2.170 Mg / m3

Absorption coefficient	7.308 mm(1

F(000)	2988

Crystal	Slab; Orange

Crystal size	0.24 ( 0.16 ( 0.04 mm3

( range for data collection	2.94 ( 27.48°

Index ranges	(15 ( h ( 16, (22 ( k ( 22, (29 ( l ( 29

Reflections collected	96608

Independent reflections	21745 [Rint = 0.0650]

Completeness to ( = 27.48°	99.5 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.7587 and 0.2729

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	21745 / 429 / 1454

Goodness-of-fit on F2	1.080

Final R indices [F2 > 2((F2)]	R1 = 0.0321, wR2 = 0.0783

R indices (all data)	R1 = 0.0358, wR2 = 0.0802

Largest diff. peak and hole	2.154 and (1.796 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

All hydrogen atoms are fixed.

One of the triflate anions is disordered over two sites.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Pb1	1670(1)	2721(1)	(866(1)	28(1)	1

Pb2	3274(1)	2963(1)	894(1)	23(1)	1

Pb3	4648(1)	3213(1)	4020(1)	24(1)	1

Pb4	5193(1)	2962(1)	5748(1)	26(1)	1

C1	2188(4)	4502(3)	(1509(2)	32(1)	1

C2	2692(4)	5256(3)	(1576(2)	29(1)	1

C3	3379(4)	5760(3)	(1070(2)	28(1)	1

C4	3570(4)	5484(3)	(527(2)	26(1)	1

C5	3041(3)	4717(2)	(506(2)	24(1)	1

C6	3217(4)	4367(3)	56(2)	25(1)	1

C7	4572(3)	4918(2)	1521(2)	23(1)	1

C8	4733(3)	4551(3)	2072(2)	24(1)	1

C9	4364(4)	3448(3)	2500(2)	29(1)	1

C10	5334(4)	4982(3)	2632(2)	25(1)	1

C11	5375(4)	4592(3)	3123(2)	26(1)	1

C12	5906(4)	5006(3)	3756(2)	25(1)	1

C13	6147(3)	4534(3)	5161(2)	24(1)	1

C14	6689(4)	4881(3)	5808(2)	25(1)	1

C15	7324(4)	5647(3)	5985(2)	31(1)	1

C16	7781(4)	5922(3)	6599(2)	38(1)	1

C17	7587(5)	5415(3)	7005(2)	42(1)	1

C18	6959(5)	4662(3)	6788(2)	38(1)	1

N1	2348(3)	4233(2)	(986(2)	28(1)	1

N2	3853(3)	4833(2)	535(2)	24(1)	1

N3	3987(3)	4443(2)	1030(2)	24(1)	1

N4	5037(3)	5685(2)	1556(2)	27(1)	1

N5	4245(3)	3776(2)	2006(2)	26(1)	1

N6	4871(3)	3816(2)	3052(2)	27(1)	1

N7	6427(3)	5775(2)	3866(2)	28(1)	1

N8	5774(3)	4586(2)	4177(2)	25(1)	1

N9	6290(3)	4988(2)	4762(2)	27(1)	1

N10	6511(3)	4386(2)	6196(2)	32(1)	1

O1	2719(3)	3633(2)	25(1)	28(1)	1

O2	5609(3)	3799(2)	5045(1)	28(1)	1

C21	(565(5)	3519(3)	(485(3)	40(1)	1

C22	(1463(5)	3584(3)	(240(3)	43(1)	1

C23	(1744(4)	3085(3)	154(3)	40(1)	1

C24	(1103(4)	2537(3)	289(2)	33(1)	1

C25	(194(4)	2510(3)	27(2)	28(1)	1

C26	558(4)	1953(3)	165(2)	26(1)	1

C27	618(4)	304(3)	836(2)	24(1)	1

C28	1425(4)	(141(3)	1096(2)	25(1)	1

C29	1808(4)	(1322(3)	1286(2)	36(1)	1

C30	2426(3)	268(3)	1435(2)	24(1)	1

C31	3083(4)	(197(3)	1705(2)	25(1)	1

C32	4144(4)	167(3)	2128(2)	25(1)	1

C33	5386(4)	1787(3)	3130(2)	26(1)	1

C34	6450(4)	2170(3)	3538(2)	25(1)	1

C35	7373(4)	1853(3)	3545(2)	32(1)	1

C36	8311(4)	2251(3)	3947(2)	35(1)	1

C37	8304(4)	2973(3)	4326(2)	34(1)	1

C38	7347(4)	3248(3)	4297(2)	30(1)	1

N21	76(3)	2992(2)	(353(2)	31(1)	1

N22	196(3)	1403(2)	455(2)	26(1)	1

N23	947(3)	931(2)	607(2)	25(1)	1

N24	(409(3)	74(2)	866(2)	30(1)	1

N25	1097(3)	(941(2)	1022(2)	29(1)	1

N26	2787(3)	(997(2)	1625(2)	30(1)	1

N27	4637(3)	(332(2)	2408(2)	31(1)	1

N28	4438(3)	943(2)	2207(2)	29(1)	1

N29	5410(3)	1252(2)	2642(2)	30(1)	1

N30	6427(3)	2855(2)	3924(2)	25(1)	1

O21	1478(2)	2066(2)	5(1)	28(1)	1

O22	4522(3)	1961(2)	3247(1)	31(1)	1

C41	1390(4)	4174(3)	1112(2)	33(1)	1

C42	517(4)	4467(3)	1293(3)	39(1)	1

C43	(73(4)	4061(3)	1645(2)	37(1)	1

C44	217(4)	3371(3)	1803(2)	33(1)	1

C45	1109(3)	3123(2)	1617(2)	24(1)	1

C46	1547(3)	2410(2)	1799(2)	24(1)	1

C47	795(4)	848(3)	2496(2)	26(1)	1

C48	1296(4)	226(3)	2764(2)	26(1)	1

C49	1196(4)	(1077(3)	2863(2)	37(1)	1

C50	2316(4)	437(3)	3139(2)	28(1)	1

C51	2710(4)	(188(3)	3358(2)	26(1)	1

C52	3787(4)	(58(3)	3767(2)	26(1)	1

C53	5540(3)	1543(3)	4754(2)	24(1)	1

C54	6629(4)	1741(3)	5150(2)	27(1)	1

C55	7404(4)	1269(3)	5089(2)	34(1)	1

C56	8409(4)	1516(4)	5463(2)	39(1)	1

C57	8630(4)	2223(3)	5888(2)	40(1)	1

C58	7810(4)	2655(3)	5934(2)	36(1)	1

N41	1689(3)	3515(2)	1270(2)	27(1)	1

N42	1029(3)	2021(2)	2159(2)	29(1)	1

N43	1495(3)	1423(2)	2387(2)	29(1)	1

N44	(282(3)	738(2)	2385(2)	34(1)	1

N45	723(3)	(526(2)	2626(2)	32(1)	1

N46	2167(3)	(948(2)	3221(2)	32(1)	1

N47	4274(3)	(668(2)	3793(2)	31(1)	1

N48	4222(3)	671(2)	4080(2)	27(1)	1

N49	5261(3)	811(2)	4432(2)	27(1)	1

N50	6836(3)	2425(2)	5573(2)	28(1)	1

O41	2347(2)	2225(2)	1615(2)	28(1)	1

O42	4952(2)	2087(2)	4758(1)	25(1)	1

C61	5234(4)	1692(3)	(701(2)	43(1)	1

O61	3392(3)	2000(2)	(555(2)	33(1)	1

O62	4625(3)	3026(2)	(857(2)	45(1)	1

O63	4985(3)	2764(2)	167(2)	41(1)	1

F61	4832(3)	1327(2)	(1271(2)	60(1)	1

F62	6275(3)	2019(3)	(651(2)	72(1)	1

F63	5174(3)	1140(2)	(353(2)	63(1)	1

S61	4491(1)	2461(1)	(461(1)	29(1)	1

C64	8849(4)	7861(3)	4997(3)	47(1)	1

O64	6934(3)	7129(2)	5023(2)	37(1)	1

O65	7463(3)	8574(2)	5431(2)	45(1)	1

O66	8217(5)	7643(3)	5987(2)	68(1)	1

F64	8504(3)	7935(3)	4432(2)	74(1)	1

F65	9263(3)	7208(3)	4976(3)	90(2)	1

F66	9637(3)	8484(3)	5269(2)	70(1)	1

S64	7742(1)	7798(1)	5407(1)	33(1)	1

C67	8721(4)	9732(3)	3738(2)	42(1)	1

O67	7889(4)	9143(4)	2614(2)	68(1)	1

O68	7148(3)	8531(2)	3373(2)	48(1)	1

O69	6813(3)	9844(2)	3238(2)	41(1)	1

F67	9173(3)	10434(2)	3621(2)	67(1)	1

F68	8503(3)	9871(2)	4298(2)	54(1)	1

F69	9457(3)	9267(3)	3750(2)	60(1)	1

S67	7502(1)	9270(1)	3175(1)	37(1)	1

C70	3177(4)	9353(3)	9076(3)	45(1)	1

O70	3088(3)	7889(2)	8577(2)	48(1)	1

O71	2812(3)	8863(3)	7923(2)	51(1)	1

O72	1431(3)	8408(2)	8467(2)	41(1)	1

F70	4246(3)	9514(2)	9144(2)	76(1)	1

F71	2817(3)	10027(2)	8994(2)	56(1)	1

F72	2902(4)	9173(3)	9590(2)	73(1)	1

S70	2563(1)	8533(1)	8439(1)	34(1)	1

C73	3043(5)	6952(3)	2065(3)	52(2)	1

O73	4801(3)	6700(2)	2680(2)	41(1)	1

O74	4756(3)	8028(2)	2457(2)	56(1)	1

O75	3811(3)	7559(3)	3205(2)	50(1)	1

F73	3314(5)	6884(3)	1527(2)	99(2)	1

F74	2529(5)	6257(3)	2124(3)	141(3)	1

F75	2337(3)	7444(2)	2072(2)	63(1)	1

S73	4228(1)	7355(1)	2670(1)	32(1)	1

C76A	9586(11)	5128(8)	4058(7)	56(3)	0.513(6)

O76A	9946(19)	5228(18)	3006(13)	86(5)	0.513(6)

O77A	8132(11)	5107(8)	3158(6)	82(4)	0.513(6)

O78A	8969(13)	3947(8)	3135(8)	96(4)	0.513(6)

F76A	10052(13)	5888(7)	4245(6)	108(4)	0.513(6)

F77A	10322(9)	4711(7)	4226(5)	106(3)	0.513(6)

F78A	8809(17)	4990(17)	4377(12)	91(4)	0.513(6)

S76A	9092(11)	4811(8)	3253(7)	57(1)	0.513(6)

C76B	9563(12)	5317(9)	4036(8)	56(3)	0.487(6)

O76B	9630(20)	5270(19)	2922(14)	86(5)	0.487(6)

O77B	7969(11)	4636(8)	3156(6)	82(4)	0.487(6)

O78B	9595(13)	4042(9)	3316(9)	96(4)	0.487(6)

F76B	9268(12)	6012(7)	4099(6)	108(4)	0.487(6)

F77B	10632(9)	5479(9)	4197(6)	106(3)	0.487(6)

F78B	9110(20)	4943(18)	4429(13)	91(4)	0.487(6)

S76B	9114(12)	4743(9)	3272(7)	57(1)	0.487(6)

O1W	5984(3)	8636(2)	4306(2)	42(1)	1

O2W	102(4)	2920(4)	8199(2)	66(1)	1

O3W	1127(3)	1095(2)	(1568(2)	33(1)	1

O4W	3005(3)	969(2)	332(2)	33(1)	1

O5W	4585(3)	1916(2)	1313(2)	38(1)	1

O6W	7040(4)	7380(3)	1938(2)	56(1)	1

O7W	7372(4)	6854(3)	3048(2)	58(1)	1

O8W	9518(4)	6798(4)	2869(3)	71(1)	1

O9W	9971(4)	2564(3)	3064(2)	67(1)	1

O10W	3402(5)	6753(4)	7553(3)	74(1)	1

Table 3. Bond lengths [Å] and angles [°].

Pb1(O1	2.394(3)

Pb1(O21	2.459(3)

Pb1(N21	2.579(4)

Pb1(N1	2.669(4)

Pb1(O61	2.752(3)

Pb2(N3	2.503(3)

Pb2(O1	2.510(3)

Pb2(O41	2.550(3)

Pb2(N41	2.587(4)

Pb2(N5	2.669(4)

Pb3(O2	2.418(3)

Pb3(N8	2.487(4)

Pb3(N30	2.487(4)

Pb3(O22	2.511(3)

Pb3(N6	2.617(4)

Pb4(O2	2.382(3)

Pb4(O42	2.437(3)

Pb4(N50	2.496(4)

Pb4(N10	2.665(4)

C1(N1	1.342(6)

C1(C2	1.390(6)

C1(H1	0.9500

C2(C3	1.391(6)

C2(H2	0.9500

C3(C4	1.394(6)

C3(H3	0.9500

C4(C5	1.388(6)

C4(H4	0.9500

C5(N1	1.344(6)

C5(C6	1.499(6)

C6(O1	1.299(5)

C6(N2	1.302(6)

C7(N3	1.303(5)

C7(N4	1.334(5)

C7(C8	1.493(6)

C8(N5	1.346(6)

C8(C10	1.395(6)

C9(N6	1.317(6)

C9(N5	1.333(6)

C9(H9	0.9500

C10(C11	1.391(6)

C10(H10	0.9500

C11(N6	1.352(6)

C11(C12	1.491(6)

C12(N8	1.304(6)

C12(N7	1.339(6)

C13(O2	1.294(5)

C13(N9	1.305(6)

C13(C14	1.498(6)

C14(N10	1.341(6)

C14(C15	1.383(7)

C15(C16	1.391(7)

C15(H15	0.9500

C16(C17	1.392(8)

C16(H16	0.9500

C17(C18	1.370(8)

C17(H17	0.9500

C18(N10	1.348(6)

C18(H18	0.9500

N2(N3	1.402(5)

N4(H4A	0.8800

N4(H4B	0.8800

N7(H7A	0.8800

N7(H7B	0.8800

N8(N9	1.394(5)

C21(N21	1.356(6)

C21(C22	1.369(8)

C21(H21	0.9500

C22(C23	1.385(8)

C22(H22	0.9500

C23(C24	1.388(7)

C23(H23	0.9500

C24(C25	1.395(7)

C24(H24	0.9500

C25(N21	1.337(6)

C25(C26	1.498(6)

C26(O21	1.281(5)

C26(N22	1.304(6)

C27(N23	1.307(5)

C27(N24	1.322(6)

C27(C28	1.489(6)

C28(N25	1.341(6)

C28(C30	1.387(6)

C29(N25	1.329(6)

C29(N26	1.335(6)

C29(H29	0.9500

C30(C31	1.391(6)

C30(H30	0.9500

C31(N26	1.337(6)

C31(C32	1.499(6)

C32(N28	1.297(6)

C32(N27	1.329(6)

C33(O22	1.250(5)

C33(N29	1.329(6)

C33(C34	1.495(6)

C34(N30	1.358(6)

C34(C35	1.378(6)

C35(C36	1.381(7)

C35(H35	0.9500

C36(C37	1.392(7)

C36(H36	0.9500

C37(C38	1.380(7)

C37(H37	0.9500

C38(N30	1.335(6)

C38(H38	0.9500

N22(N23	1.394(5)

N23(H23A	0.8800

N24(H24A	0.8800

N24(H24B	0.8800

N27(H27A	0.8800

N27(H27B	0.8800

N28(N29	1.417(5)

N29(H29A	0.8800

C41(N41	1.336(6)

C41(C42	1.393(7)

C41(H41	0.9500

C42(C43	1.378(7)

C42(H42	0.9500

C43(C44	1.384(7)

C43(H43	0.9500

C44(C45	1.389(6)

C44(H44	0.9500

C45(N41	1.350(6)

C45(C46	1.519(6)

C46(O41	1.236(5)

C46(N42	1.328(6)

C47(N43	1.302(6)

C47(N44	1.333(6)

C47(C48	1.497(6)

C48(N45	1.333(6)

C48(C50	1.392(7)

C49(N46	1.331(7)

C49(N45	1.344(6)

C49(H49	0.9500

C50(C51	1.389(6)

C50(H50	0.9500

C51(N46	1.333(6)

C51(C52	1.489(6)

C52(N47	1.310(6)

C52(N48	1.316(6)

C53(O42	1.295(5)

C53(N49	1.309(6)

C53(C54	1.482(6)

C54(N50	1.349(6)

C54(C55	1.393(6)

C55(C56	1.377(7)

C55(H55	0.9500

C56(C57	1.379(8)

C56(H56	0.9500

C57(C58	1.391(7)

C57(H57	0.9500

C58(N50	1.333(6)

C58(H58	0.9500

N42(N43	1.399(5)

N42(H42A	0.8800

N44(H44A	0.8800

N44(H44B	0.8800

N47(H47A	0.8800

N47(H47B	0.8800

N48(N49	1.395(5)

N48(H48	0.8800

C61(F61	1.321(6)

C61(F63	1.332(6)

C61(F62	1.333(6)

C61(S61	1.818(5)

O61(S61	1.457(3)

O62(S61	1.435(4)

O63(S61	1.436(4)

C64(F65	1.316(6)

C64(F64	1.324(7)

C64(F66	1.328(6)

C64(S64	1.816(5)

O64(S64	1.459(3)

O65(S64	1.432(4)

O66(S64	1.444(4)

C67(F69	1.333(6)

C67(F67	1.335(6)

C67(F68	1.339(6)

C67(S67	1.815(5)

O67(S67	1.441(4)

O68(S67	1.440(4)

O69(S67	1.435(4)

C70(F70	1.326(6)

C70(F72	1.342(7)

C70(F71	1.344(6)

C70(S70	1.815(5)

O70(S70	1.438(4)

O71(S70	1.440(4)

O72(S70	1.441(3)

C73(F74	1.302(6)

C73(F73	1.319(7)

C73(F75	1.336(7)

C73(S73	1.822(5)

O73(S73	1.443(3)

O74(S73	1.432(4)

O75(S73	1.423(4)

C76A(F76A	1.310(12)

C76A(F77A	1.320(12)

C76A(F78A	1.335(12)

C76A(S76A	1.797(11)

O76A(S76A	1.445(11)

O77A(S76A	1.404(11)

O78A(S76A	1.441(11)

C76B(F76B	1.304(13)

C76B(F77B	1.325(12)

C76B(F78B	1.337(13)

C76B(S76B	1.802(11)

O76B(S76B	1.446(12)

O77B(S76B	1.418(11)

O78B(S76B	1.453(11)

O1W(H1WA	0.840(5)

O1W(H1WB	0.839(5)

O2W(H2WA	0.840(5)

O2W(H2WB	0.842(5)

O3W(H3WA	0.840(5)

O3W(H3WB	0.841(5)

O4W(H4WA	0.840(5)

O4W(H4WB	0.840(5)

O5W(H5WA	0.842(5)

O5W(H5WB	0.841(5)

O6W(H6WA	0.841(5)

O6W(H6WB	0.842(5)

O7W(H7WA	0.841(5)

O7W(H7WB	0.842(5)

O8W(H8WA	0.843(5)

O8W(H8WB	0.844(5)

O9W(H9WA	0.841(5)

O9W(H9WB	0.842(5)

O10W(H10W	0.843(5)

O10W(H11W	0.843(5)

O1(Pb1(O21	72.67(10)

O1(Pb1(N21	82.91(12)

O21(Pb1(N21	64.85(11)

O1(Pb1(N1	63.46(11)

O21(Pb1(N1	134.29(11)

N21(Pb1(N1	96.52(12)

O1(Pb1(O61	76.95(11)

O21(Pb1(O61	68.62(10)

N21(Pb1(O61	132.93(11)

N1(Pb1(O61	111.07(10)

N3(Pb2(O1	62.61(11)

N3(Pb2(O41	127.64(11)

O1(Pb2(O41	137.12(10)

N3(Pb2(N41	80.00(12)

O1(Pb2(N41	81.70(11)

O41(Pb2(N41	63.07(11)

N3(Pb2(N5	61.76(11)

O1(Pb2(N5	123.29(10)

O41(Pb2(N5	75.11(11)

N41(Pb2(N5	78.93(12)

O2(Pb3(N8	63.60(11)

O2(Pb3(N30	81.87(11)

N8(Pb3(N30	80.42(12)

O2(Pb3(O22	137.52(11)

N8(Pb3(O22	131.40(11)

N30(Pb3(O22	66.00(11)

O2(Pb3(N6	125.79(11)

N8(Pb3(N6	62.63(11)

N30(Pb3(N6	83.21(12)

O22(Pb3(N6	78.81(11)

O2(Pb4(O42	72.64(10)

O2(Pb4(N50	85.81(12)

O42(Pb4(N50	66.39(11)

O2(Pb4(N10	62.70(11)

O42(Pb4(N10	129.35(11)

N50(Pb4(N10	87.03(13)

N1(C1(C2	123.3(4)

N1(C1(H1	118.4

C2(C1(H1	118.4

C1(C2(C3	118.0(4)

C1(C2(H2	121.0

C3(C2(H2	121.0

C2(C3(C4	119.3(4)

C2(C3(H3	120.3

C4(C3(H3	120.3

C5(C4(C3	118.5(4)

C5(C4(H4	120.8

C3(C4(H4	120.8

N1(C5(C4	122.8(4)

N1(C5(C6	115.3(4)

C4(C5(C6	121.9(4)

O1(C6(N2	125.8(4)

O1(C6(C5	117.5(4)

N2(C6(C5	116.7(4)

N3(C7(N4	124.9(4)

N3(C7(C8	115.7(4)

N4(C7(C8	119.3(4)

N5(C8(C10	120.9(4)

N5(C8(C7	116.5(4)

C10(C8(C7	122.6(4)

N6(C9(N5	126.6(4)

N6(C9(H9	116.7

N5(C9(H9	116.7

C11(C10(C8	117.7(4)

C11(C10(H10	121.2

C8(C10(H10	121.2

N6(C11(C10	120.7(4)

N6(C11(C12	116.2(4)

C10(C11(C12	123.0(4)

N8(C12(N7	124.2(4)

N8(C12(C11	115.7(4)

N7(C12(C11	119.9(4)

O2(C13(N9	125.9(4)

O2(C13(C14	116.9(4)

N9(C13(C14	117.1(4)

N10(C14(C15	123.2(4)

N10(C14(C13	114.3(4)

C15(C14(C13	122.5(4)

C14(C15(C16	118.3(5)

C14(C15(H15	120.8

C16(C15(H15	120.8

C15(C16(C17	118.8(5)

C15(C16(H16	120.6

C17(C16(H16	120.6

C18(C17(C16	118.9(5)

C18(C17(H17	120.5

C16(C17(H17	120.5

N10(C18(C17	123.1(5)

N10(C18(H18	118.5

C17(C18(H18	118.5

C1(N1(C5	118.1(4)

C1(N1(Pb1	124.9(3)

C5(N1(Pb1	116.2(3)

C6(N2(N3	112.2(3)

C7(N3(N2	112.6(3)

C7(N3(Pb2	126.8(3)

N2(N3(Pb2	120.4(2)

C7(N4(H4A	120.0

C7(N4(H4B	120.0

H4A(N4(H4B	120.0

C9(N5(C8	116.8(4)

C9(N5(Pb2	124.4(3)

C8(N5(Pb2	118.6(3)

C9(N6(C11	117.1(4)

C9(N6(Pb3	123.0(3)

C11(N6(Pb3	118.9(3)

C12(N7(H7A	120.0

C12(N7(H7B	120.0

H7A(N7(H7B	120.0

C12(N8(N9	114.2(4)

C12(N8(Pb3	125.9(3)

N9(N8(Pb3	119.8(3)

C13(N9(N8	111.4(4)

C14(N10(C18	117.7(4)

C14(N10(Pb4	117.5(3)

C18(N10(Pb4	124.8(3)

C6(O1(Pb1	126.8(3)

C6(O1(Pb2	117.3(3)

Pb1(O1(Pb2	113.89(12)

C13(O2(Pb4	128.2(3)

C13(O2(Pb3	119.0(3)

Pb4(O2(Pb3	112.21(12)

N21(C21(C22	122.9(5)

N21(C21(H21	118.5

C22(C21(H21	118.5

C21(C22(C23	119.0(5)

C21(C22(H22	120.5

C23(C22(H22	120.5

C22(C23(C24	118.9(5)

C22(C23(H23	120.5

C24(C23(H23	120.5

C23(C24(C25	118.9(5)

C23(C24(H24	120.5

C25(C24(H24	120.5

N21(C25(C24	122.1(4)

N21(C25(C26	115.7(4)

C24(C25(C26	122.2(4)

O21(C26(N22	126.7(4)

O21(C26(C25	118.6(4)

N22(C26(C25	114.7(4)

N23(C27(N24	121.8(4)

N23(C27(C28	119.3(4)

N24(C27(C28	118.9(4)

N25(C28(C30	122.8(4)

N25(C28(C27	116.2(4)

C30(C28(C27	120.8(4)

N25(C29(N26	127.4(4)

N25(C29(H29	116.3

N26(C29(H29	116.3

C28(C30(C31	116.3(4)

C28(C30(H30	121.8

C31(C30(H30	121.8

N26(C31(C30	122.1(4)

N26(C31(C32	115.4(4)

C30(C31(C32	122.4(4)

N28(C32(N27	127.5(4)

N28(C32(C31	115.9(4)

N27(C32(C31	116.5(4)

O22(C33(N29	122.2(4)

O22(C33(C34	121.3(4)

N29(C33(C34	116.5(4)

N30(C34(C35	122.0(4)

N30(C34(C33	113.8(4)

C35(C34(C33	124.1(4)

C34(C35(C36	119.3(4)

C34(C35(H35	120.4

C36(C35(H35	120.4

C35(C36(C37	118.9(5)

C35(C36(H36	120.5

C37(C36(H36	120.5

C38(C37(C36	118.5(4)

C38(C37(H37	120.8

C36(C37(H37	120.8

N30(C38(C37	123.1(4)

N30(C38(H38	118.4

C37(C38(H38	118.4

C25(N21(C21	118.2(4)

C25(N21(Pb1	116.1(3)

C21(N21(Pb1	125.4(3)

C26(N22(N23	112.7(4)

C27(N23(N22	117.3(4)

C27(N23(H23A	121.3

N22(N23(H23A	121.3

C27(N24(H24A	120.0

C27(N24(H24B	120.0

H24A(N24(H24B	120.0

C29(N25(C28	115.4(4)

C29(N26(C31	116.0(4)

C32(N27(H27A	120.0

C32(N27(H27B	120.0

H27A(N27(H27B	120.0

C32(N28(N29	112.9(4)

C33(N29(N28	118.3(4)

C33(N29(H29A	120.8

N28(N29(H29A	120.8

C38(N30(C34	118.1(4)

C38(N30(Pb3	122.3(3)

C34(N30(Pb3	119.0(3)

C26(O21(Pb1	118.9(3)

C33(O22(Pb3	117.6(3)

N41(C41(C42	122.8(4)

N41(C41(H41	118.6

C42(C41(H41	118.6

C43(C42(C41	119.0(5)

C43(C42(H42	120.5

C41(C42(H42	120.5

C42(C43(C44	118.9(5)

C42(C43(H43	120.6

C44(C43(H43	120.6

C43(C44(C45	119.0(4)

C43(C44(H44	120.5

C45(C44(H44	120.5

N41(C45(C44	122.5(4)

N41(C45(C46	113.9(4)

C44(C45(C46	123.6(4)

O41(C46(N42	123.9(4)

O41(C46(C45	119.9(4)

N42(C46(C45	116.2(4)

N43(C47(N44	128.7(4)

N43(C47(C48	113.7(4)

N44(C47(C48	117.5(4)

N45(C48(C50	122.6(4)

N45(C48(C47	117.0(4)

C50(C48(C47	120.4(4)

N46(C49(N45	126.8(4)

N46(C49(H49	116.6

N45(C49(H49	116.6

C51(C50(C48	115.8(4)

C51(C50(H50	122.1

C48(C50(H50	122.1

N46(C51(C50	123.2(4)

N46(C51(C52	114.5(4)

C50(C51(C52	122.2(4)

N47(C52(N48	122.5(4)

N47(C52(C51	119.0(4)

N48(C52(C51	118.5(4)

O42(C53(N49	126.0(4)

O42(C53(C54	118.8(4)

N49(C53(C54	115.2(4)

N50(C54(C55	121.5(4)

N50(C54(C53	115.6(4)

C55(C54(C53	123.0(4)

C56(C55(C54	119.0(5)

C56(C55(H55	120.5

C54(C55(H55	120.5

C55(C56(C57	119.7(5)

C55(C56(H56	120.2

C57(C56(H56	120.2

C56(C57(C58	118.3(5)

C56(C57(H57	120.8

C58(C57(H57	120.8

N50(C58(C57	122.6(5)

N50(C58(H58	118.7

C57(C58(H58	118.7

C41(N41(C45	117.9(4)

C41(N41(Pb2	121.8(3)

C45(N41(Pb2	120.3(3)

C46(N42(N43	116.8(4)

C46(N42(H42A	121.6

N43(N42(H42A	121.6

C47(N43(N42	113.6(4)

C47(N44(H44A	120.0

C47(N44(H44B	120.0

H44A(N44(H44B	120.0

C48(N45(C49	116.0(4)

C49(N46(C51	115.7(4)

C52(N47(H47A	120.0

C52(N47(H47B	120.0

H47A(N47(H47B	120.0

C52(N48(N49	119.0(4)

C52(N48(H48	120.5

N49(N48(H48	120.5

C53(N49(N48	111.5(4)

C58(N50(C54	119.0(4)

C58(N50(Pb4	125.4(3)

C54(N50(Pb4	114.1(3)

C46(O41(Pb2	122.6(3)

C53(O42(Pb4	113.7(3)

F61(C61(F63	108.3(4)

F61(C61(F62	109.0(4)

F63(C61(F62	108.1(5)

F61(C61(S61	110.8(4)

F63(C61(S61	110.2(4)

F62(C61(S61	110.3(4)

S61(O61(Pb1	119.54(18)

O62(S61(O63	115.5(2)

O62(S61(O61	113.9(2)

O63(S61(O61	113.8(2)

O62(S61(C61	105.6(3)

O63(S61(C61	103.8(2)

O61(S61(C61	102.4(2)

F65(C64(F64	107.9(5)

F65(C64(F66	107.6(5)

F64(C64(F66	109.2(5)

F65(C64(S64	110.9(4)

F64(C64(S64	110.4(4)

F66(C64(S64	110.7(4)

O65(S64(O66	114.8(3)

O65(S64(O64	115.2(2)

O66(S64(O64	114.8(2)

O65(S64(C64	103.1(2)

O66(S64(C64	103.7(3)

O64(S64(C64	102.9(2)

F69(C67(F67	107.7(4)

F69(C67(F68	107.1(4)

F67(C67(F68	107.9(5)

F69(C67(S67	112.1(4)

F67(C67(S67	110.6(4)

F68(C67(S67	111.2(4)

O69(S67(O68	114.9(2)

O69(S67(O67	116.8(3)

O68(S67(O67	113.0(3)

O69(S67(C67	103.9(2)

O68(S67(C67	102.4(2)

O67(S67(C67	103.6(3)

F70(C70(F72	109.6(5)

F70(C70(F71	108.0(4)

F72(C70(F71	106.9(5)

F70(C70(S70	111.4(4)

F72(C70(S70	110.2(4)

F71(C70(S70	110.6(4)

O70(S70(O71	116.2(3)

O70(S70(O72	114.8(2)

O71(S70(O72	113.8(2)

O70(S70(C70	103.3(2)

O71(S70(C70	103.1(3)

O72(S70(C70	103.3(2)

F74(C73(F73	109.4(6)

F74(C73(F75	106.6(6)

F73(C73(F75	106.8(5)

F74(C73(S73	112.1(4)

F73(C73(S73	111.0(5)

F75(C73(S73	110.8(4)

O75(S73(O74	114.9(3)

O75(S73(O73	113.6(2)

O74(S73(O73	114.8(3)

O75(S73(C73	105.3(3)

O74(S73(C73	102.2(3)

O73(S73(C73	104.1(2)

F76A(C76A(F77A	106.1(12)

F76A(C76A(F78A	106.2(14)

F77A(C76A(F78A	107.2(14)

F76A(C76A(S76A	115.8(11)

F77A(C76A(S76A	108.5(10)

F78A(C76A(S76A	112.5(13)

O77A(S76A(O78A	115.9(11)

O77A(S76A(O76A	113.3(13)

O78A(S76A(O76A	114.6(14)

O77A(S76A(C76A	103.2(9)

O78A(S76A(C76A	105.3(10)

O76A(S76A(C76A	102.4(11)

F76B(C76B(F77B	105.9(12)

F76B(C76B(F78B	104.4(15)

F77B(C76B(F78B	111.2(15)

F76B(C76B(S76B	112.3(11)

F77B(C76B(S76B	111.7(11)

F78B(C76B(S76B	111.0(14)

O77B(S76B(O76B	113.8(13)

O77B(S76B(O78B	118.4(12)

O76B(S76B(O78B	113.1(14)

O77B(S76B(C76B	105.5(10)

O76B(S76B(C76B	102.1(13)

O78B(S76B(C76B	101.2(10)

H1WA(O1W(H1WB	107.1(9)

H2WA(O2W(H2WB	106.7(9)

H3WA(O3W(H3WB	106.7(9)

H4WA(O4W(H4WB	106.8(9)

H5WA(O5W(H5WB	106.7(9)

H6WA(O6W(H6WB	106.6(9)

H7WA(O7W(H7WB	106.7(9)

H8WA(O8W(H8WB	106.3(9)

H9WA(O9W(H9WB	106.8(9)

H10W(O10W(H11W	106.3(9)

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Pb1	32(1) 	24(1)	24(1) 	5(1)	0(1) 	2(1)

Pb2	25(1) 	21(1)	23(1) 	5(1)	4(1) 	4(1)

Pb3	23(1) 	25(1)	22(1) 	4(1)	2(1) 	5(1)

Pb4	31(1) 	26(1)	23(1) 	5(1)	6(1) 	9(1)

C1	31(2) 	34(2)	25(2) 	6(2)	(3(2) 	2(2)

C2	29(2) 	32(2)	29(2) 	14(2)	5(2) 	10(2)

C3	26(2) 	28(2)	30(2) 	8(2)	7(2) 	4(2)

C4	26(2) 	28(2)	24(2) 	6(2)	4(2) 	6(2)

C5	26(2) 	22(2)	25(2) 	3(2)	3(2) 	7(2)

C6	27(2) 	26(2)	23(2) 	7(2)	5(2) 	7(2)

C7	27(2) 	23(2)	21(2) 	5(2)	5(2) 	7(2)

C8	26(2) 	23(2)	22(2) 	3(2)	4(2) 	6(2)

C9	35(2) 	24(2)	27(2) 	6(2)	2(2) 	2(2)

C10	29(2) 	22(2)	24(2) 	3(2)	4(2) 	4(2)

C11	26(2) 	26(2)	24(2) 	3(2)	3(2) 	7(2)

C12	26(2) 	26(2)	23(2) 	4(2)	4(2) 	7(2)

C13	25(2) 	25(2)	22(2) 	1(2)	3(2) 	8(2)

C14	26(2) 	29(2)	22(2) 	2(2)	3(2) 	11(2)

C15	33(2) 	32(2)	26(2) 	2(2)	1(2) 	10(2)

C16	36(3) 	39(3)	32(3) 	(3(2)	(2(2) 	5(2)

C17	52(3) 	48(3)	20(2) 	2(2)	(3(2) 	12(3)

C18	50(3) 	42(3)	20(2) 	5(2)	1(2) 	10(2)

N1	29(2) 	27(2)	25(2) 	7(2)	1(2) 	3(2)

N2	28(2) 	23(2)	21(2) 	4(1)	2(1) 	2(1)

N3	28(2) 	23(2)	21(2) 	5(1)	4(1) 	2(1)

N4	38(2) 	21(2)	18(2) 	3(1)	0(2) 	0(2)

N5	28(2) 	26(2)	24(2) 	6(2)	4(2) 	5(2)

N6	30(2) 	26(2)	24(2) 	5(2)	3(2) 	4(2)

N7	37(2) 	23(2)	21(2) 	2(1)	(1(2) 	3(2)

N8	28(2) 	25(2)	19(2) 	0(1)	(1(1) 	6(2)

N9	27(2) 	28(2)	22(2) 	1(1)	0(1) 	5(2)

N10	38(2) 	33(2)	24(2) 	4(2)	3(2) 	11(2)

O1	35(2) 	24(2)	22(2) 	5(1)	1(1) 	0(1)

O2	35(2) 	24(2)	22(2) 	4(1)	2(1) 	5(1)

C21	48(3) 	28(2)	42(3) 	12(2)	(3(2) 	8(2)

C22	45(3) 	34(3)	49(3) 	6(2)	(1(2) 	18(2)

C23	35(3) 	37(3)	49(3) 	6(2)	3(2) 	17(2)

C24	33(2) 	29(2)	34(2) 	4(2)	2(2) 	9(2)

C25	27(2) 	25(2)	28(2) 	2(2)	(4(2) 	4(2)

C26	25(2) 	24(2)	23(2) 	0(2)	(1(2) 	3(2)

C27	27(2) 	22(2)	22(2) 	2(2)	3(2) 	5(2)

C28	29(2) 	25(2)	22(2) 	4(2)	5(2) 	9(2)

C29	40(3) 	22(2)	40(3) 	3(2)	(3(2) 	5(2)

C30	29(2) 	22(2)	19(2) 	2(2)	5(2) 	4(2)

C31	30(2) 	25(2)	21(2) 	2(2)	7(2) 	9(2)

C32	27(2) 	31(2)	18(2) 	4(2)	5(2) 	10(2)

C33	28(2) 	24(2)	26(2) 	7(2)	2(2) 	6(2)

C34	29(2) 	24(2)	23(2) 	5(2)	5(2) 	5(2)

C35	35(2) 	31(2)	29(2) 	2(2)	4(2) 	10(2)

C36	29(2) 	38(3)	37(3) 	3(2)	4(2) 	9(2)

C37	25(2) 	39(3)	34(2) 	0(2)	1(2) 	3(2)

C38	28(2) 	28(2)	28(2) 	0(2)	2(2) 	1(2)

N21	34(2) 	22(2)	34(2) 	6(2)	(2(2) 	6(2)

N22	28(2) 	26(2)	26(2) 	8(2)	4(2) 	8(2)

N23	23(2) 	24(2)	27(2) 	5(1)	5(1) 	6(1)

N24	23(2) 	30(2)	38(2) 	12(2)	6(2) 	6(2)

N25	31(2) 	23(2)	32(2) 	4(2)	1(2) 	7(2)

N26	33(2) 	23(2)	30(2) 	2(2)	(2(2) 	6(2)

N27	29(2) 	28(2)	33(2) 	7(2)	0(2) 	5(2)

N28	28(2) 	27(2)	28(2) 	(1(2)	(3(2) 	8(2)

N29	28(2) 	26(2)	31(2) 	(1(2)	(3(2) 	8(2)

N30	24(2) 	26(2)	23(2) 	2(1)	4(1) 	2(1)

O21	26(2) 	27(2)	30(2) 	9(1)	3(1) 	4(1)

O22	28(2) 	33(2)	28(2) 	(1(1)	4(1) 	5(1)

C41	38(3) 	28(2)	36(3) 	11(2)	9(2) 	9(2)

C42	45(3) 	32(3)	45(3) 	11(2)	10(2) 	19(2)

C43	35(3) 	37(3)	43(3) 	6(2)	11(2) 	17(2)

C44	29(2) 	34(2)	37(3) 	7(2)	10(2) 	8(2)

C45	25(2) 	21(2)	23(2) 	0(2)	2(2) 	6(2)

C46	25(2) 	21(2)	24(2) 	1(2)	2(2) 	3(2)

C47	31(2) 	25(2)	24(2) 	2(2)	6(2) 	8(2)

C48	30(2) 	25(2)	26(2) 	5(2)	10(2) 	6(2)

C49	42(3) 	21(2)	43(3) 	4(2)	0(2) 	3(2)

C50	31(2) 	23(2)	31(2) 	5(2)	9(2) 	4(2)

C51	29(2) 	24(2)	24(2) 	2(2)	8(2) 	6(2)

C52	31(2) 	26(2)	24(2) 	7(2)	8(2) 	8(2)

C53	26(2) 	26(2)	25(2) 	7(2)	9(2) 	7(2)

C54	28(2) 	31(2)	25(2) 	7(2)	6(2) 	9(2)

C55	34(2) 	38(3)	34(2) 	7(2)	11(2) 	14(2)

C56	30(2) 	56(3)	39(3) 	18(2)	7(2) 	17(2)

C57	27(2) 	55(3)	37(3) 	13(2)	3(2) 	6(2)

C58	33(2) 	44(3)	29(2) 	7(2)	2(2) 	6(2)

N41	31(2) 	22(2)	29(2) 	5(2)	7(2) 	7(2)

N42	25(2) 	30(2)	34(2) 	11(2)	8(2) 	9(2)

N43	31(2) 	30(2)	29(2) 	10(2)	10(2) 	9(2)

N44	28(2) 	32(2)	43(2) 	11(2)	5(2) 	6(2)

N45	35(2) 	26(2)	32(2) 	7(2)	2(2) 	4(2)

N46	36(2) 	23(2)	35(2) 	4(2)	4(2) 	4(2)

N47	37(2) 	25(2)	32(2) 	4(2)	4(2) 	11(2)

N48	28(2) 	23(2)	30(2) 	4(2)	6(2) 	9(2)

N49	26(2) 	26(2)	30(2) 	4(2)	6(2) 	9(2)

N50	28(2) 	33(2)	23(2) 	6(2)	4(2) 	6(2)

O41	27(2) 	28(2)	33(2) 	9(1)	9(1) 	8(1)

O42	26(2) 	27(2)	25(2) 	6(1)	6(1) 	9(1)

C61	30(2) 	43(3)	49(3) 	(5(2)	9(2) 	1(2)

O61	30(2) 	30(2)	41(2) 	9(1)	10(2) 	4(1)

O62	56(2) 	35(2)	44(2) 	16(2)	9(2) 	(3(2)

O63	48(2) 	39(2)	30(2) 	1(2)	6(2) 	(2(2)

F61	61(2) 	62(2)	48(2) 	(16(2)	17(2) 	8(2)

F62	33(2) 	76(3)	95(3) 	(18(2)	23(2) 	3(2)

F63	66(2) 	44(2)	80(3) 	13(2)	1(2) 	24(2)

S61	33(1) 	24(1)	29(1) 	5(1)	9(1) 	2(1)

C64	33(3) 	53(3)	56(4) 	2(3)	10(3) 	13(2)

O64	33(2) 	32(2)	42(2) 	(3(2)	8(2) 	3(1)

O65	29(2) 	33(2)	69(3) 	(3(2)	12(2) 	5(2)

O66	107(4) 	51(3)	34(2) 	11(2)	(1(2) 	(9(3)

F64	73(3) 	102(3)	43(2) 	7(2)	28(2) 	(2(2)

F65	56(2) 	84(3)	132(4) 	(3(3)	17(3) 	45(2)

F66	28(2) 	80(3)	91(3) 	(2(2)	14(2) 	(3(2)

S64	35(1) 	31(1)	31(1) 	2(1)	11(1) 	3(1)

C67	40(3) 	50(3)	38(3) 	9(2)	8(2) 	12(2)

O67	65(3) 	118(4)	36(2) 	18(2)	23(2) 	46(3)

O68	50(2) 	36(2)	56(2) 	4(2)	5(2) 	16(2)

O69	37(2) 	41(2)	46(2) 	8(2)	5(2) 	17(2)

F67	53(2) 	66(2)	75(3) 	22(2)	4(2) 	(6(2)

F68	49(2) 	71(2)	37(2) 	(1(2)	4(2) 	15(2)

F69	40(2) 	93(3)	55(2) 	20(2)	9(2) 	31(2)

S67	36(1) 	47(1)	29(1) 	5(1)	6(1) 	17(1)

C70	40(3) 	38(3)	55(3) 	4(2)	0(3) 	12(2)

O70	35(2) 	38(2)	66(3) 	3(2)	4(2) 	10(2)

O71	43(2) 	70(3)	46(2) 	12(2)	14(2) 	21(2)

O72	25(2) 	49(2)	50(2) 	13(2)	5(2) 	9(2)

F70	40(2) 	47(2)	118(4) 	(8(2)	(18(2) 	5(2)

F71	56(2) 	39(2)	69(2) 	0(2)	5(2) 	16(2)

F72	105(3) 	69(3)	38(2) 	2(2)	(2(2) 	21(2)

S70	27(1) 	38(1)	37(1) 	2(1)	4(1) 	9(1)

C73	59(4) 	39(3)	51(4) 	15(3)	(12(3) 	6(3)

O73	54(2) 	36(2)	32(2) 	4(2)	1(2) 	23(2)

O74	51(2) 	44(2)	74(3) 	29(2)	0(2) 	7(2)

O75	58(2) 	63(3)	35(2) 	8(2)	10(2) 	30(2)

F73	129(4) 	128(4)	33(2) 	(11(2)	(17(2) 	62(4)

F74	116(4) 	64(3)	188(6) 	73(4)	(109(4) 	(46(3)

F75	37(2) 	74(3)	81(3) 	37(2)	(1(2) 	14(2)

S73	42(1) 	28(1)	25(1) 	3(1)	2(1) 	13(1)

C76A	56(4) 	53(7)	48(4) 	12(5)	(8(3) 	(10(4)

O76A	122(14) 	88(5)	57(7) 	28(4)	26(9) 	24(8)

O77A	90(6) 	90(8)	59(4) 	(26(7)	(11(4) 	65(8)

O78A	113(12) 	56(5)	114(10) 	(4(5)	7(9) 	40(8)

F76A	149(11) 	74(5)	68(6) 	(28(4)	27(8) 	(30(8)

F77A	106(6) 	113(6)	90(5) 	2(6)	(8(5) 	41(6)

F78A	90(11) 	127(5)	51(5) 	13(3)	18(7) 	8(7)

S76A	72(1) 	55(2)	44(1) 	2(1)	12(1) 	24(1)

C76B	56(4) 	53(7)	48(4) 	12(5)	(8(3) 	(10(4)

O76B	122(14) 	88(5)	57(7) 	28(4)	26(9) 	24(8)

O77B	90(6) 	90(8)	59(4) 	(26(7)	(11(4) 	65(8)

O78B	113(12) 	56(5)	114(10) 	(4(5)	7(9) 	40(8)

F76B	149(11) 	74(5)	68(6) 	(28(4)	27(8) 	(30(8)

F77B	106(6) 	113(6)	90(5) 	2(6)	(8(5) 	41(6)

F78B	90(11) 	127(5)	51(5) 	13(3)	18(7) 	8(7)

S76B	72(1) 	55(2)	44(1) 	2(1)	12(1) 	24(1)

O1W	41(2) 	45(2)	48(2) 	21(2)	11(2) 	13(2)

O2W	44(2) 	84(4)	61(3) 	26(3)	(6(2) 	(10(2)

O3W	34(2) 	31(2)	32(2) 	4(1)	7(1) 	2(1)

O4W	32(2) 	37(2)	34(2) 	13(2)	9(1) 	9(2)

O5W	29(2) 	42(2)	48(2) 	20(2)	7(2) 	11(2)

O6W	65(3) 	47(2)	54(3) 	7(2)	9(2) 	5(2)

O7W	60(3) 	64(3)	55(3) 	18(2)	12(2) 	17(2)

O8W	61(3) 	84(4)	62(3) 	9(3)	8(2) 	5(3)

O9W	71(3) 	72(3)	64(3) 	8(3)	32(3) 	17(3)

O10W	74(3) 	75(4)	72(4) 	0(3)	21(3) 	22(3)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1	1707	4159	(1851	38	1

H2	2570	5422	(1955	35	1

H3	3715	6288	(1094	33	1

H4	4051	5813	(179	31	1

H9	4051	2894	2448	35	1

H10	5703	5523	2677	30	1

H15	7445	5976	5696	37	1

H16	8217	6446	6737	46	1

H17	7886	5589	7427	50	1

H18	6833	4319	7068	46	1

H4A	4959	5904	1232	32	1

H4B	5422	5971	1904	32	1

H7A	6705	6028	4242	34	1

H7B	6490	6027	3562	34	1

H21	(382	3858	(759	48	1

H22	(1887	3966	(339	51	1

H23	(2365	3118	328	48	1

H24	(1281	2185	556	39	1

H29	1596	(1891	1226	43	1

H30	2650	834	1480	28	1

H35	7363	1366	3276	38	1

H36	8951	2036	3966	42	1

H37	8944	3269	4598	41	1

H38	7344	3741	4555	36	1

H23A	1616	1050	552	30	1

H24A	(891	345	730	36	1

H24B	(609	(351	1022	36	1

H27A	5235	(142	2682	37	1

H27B	4365	(852	2319	37	1

H29A	6014	1094	2590	36	1

H41	1789	4453	866	40	1

H42	331	4940	1175	46	1

H43	(668	4252	1776	45	1

H44	(189	3072	2036	39	1

H49	797	(1615	2764	44	1

H50	2718	975	3238	34	1

H55	7242	784	4794	41	1

H56	8947	1201	5428	47	1

H57	9324	2409	6142	48	1

H58	7951	3134	6234	43	1

H42A	421	2134	2250	34	1

H44A	(605	1082	2215	41	1

H44B	(670	321	2481	41	1

H47A	4916	(598	4027	38	1

H47B	3958	(1148	3577	38	1

H48	3863	1064	4068	32	1

H1WA	6430(30)	8680(40)	4628(12)	51	1

H1WB	6330(30)	8620(40)	4021(15)	51	1

H2WA	(557(13)	2850(50)	8040(30)	79	1

H2WB	430(40)	2830(50)	7912(19)	79	1

H3WA	730(30)	1060(30)	(1907(10)	40	1

H3WB	1720(20)	980(30)	(1637(19)	40	1

H4WA	3030(40)	1110(30)	(4(11)	40	1

H4WB	3616(19)	1160(30)	557(17)	40	1

H5WA	5252(10)	2050(40)	1320(20)	46	1

H5WB	4530(40)	1700(30)	1616(17)	46	1

H6WA	6410(20)	7150(30)	1950(30)	68	1

H6WB	7140(50)	7849(16)	2140(30)	68	1

H7WA	7020(50)	6930(30)	2724(17)	70	1

H7WB	7340(60)	6355(8)	3010(30)	70	1

H8WA	9050(50)	7040(40)	2990(40)	85	1

H8WB	9460(60)	6370(30)	3010(40)	85	1

H9WA	9860(50)	2560(50)	3417(13)	80	1

H9WB	9440(40)	2710(50)	2870(30)	80	1

H10W	2840(40)	6590(50)	7280(30)	88	1

H11W	3270(60)	7130(40)	7800(30)	88	1