|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	00sot039

Empirical formula 	C14H14BrF3O2

Formula weight 	351.16

Temperature 	298(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P-1

Unit cell dimensions	a = 7.9539(16) Å	( = 97.61(3)°

b = 9.5523(19) Å	( = 110.44(3)°

c = 10.695(2) Å	(  = 104.17(3)°

Volume	716.7(2) Å3

Z	2

Density (calculated)	1.627 Mg / m3

Absorption coefficient	2.899 mm(1

F(000)	352

Crystal	block; colourless

Crystal size	0.35 ( 0.35 ( 0.35 mm3

( range for data collection	2.69 ( 27.47°

Index ranges	(10 ( h ( 10, (12 ( k ( 12, (13 ( l ( 13

Reflections collected	5354

Independent reflections	2944 [Rint = 0.0494]

Completeness to ( = 27.47°	89.6 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.4302 and 0.4302

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2944 / 0 / 182

Goodness-of-fit on F2	1.002

Final R indices [F2 > 2((F2)]	R1 = 0.0576, wR2 = 0.1393

R indices (all data)	R1 = 0.1379, wR2 = 0.1797

Extinction coefficient	0.015(4)

Largest diff. peak and hole	0.438 and (0.548 e Å(3

Diffractometer: Enraf Nonius KappaCCD area detector (( scans and ( scans to fill Ewald sphere). Data collection and cell

refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography,

part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing,

Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Program used to solve structure:

SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Program used to refine structure: SHELXL97 (G. M. Sheldrick

(1997), University of Göttingen, Germany).

Further information:  http://www.soton.ac.uk/~xservice/strat.htm

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Br1	781(1)	9044(1)	8605(1)	130(1)	1

F1	7830(4)	14658(4)	5278(3)	91(1)	1

F2	9383(5)	13107(4)	5512(3)	100(1)	1

F3	10410(4)	15164(4)	7034(3)	86(1)	1

O1	9008(4)	12645(4)	7862(3)	63(1)	1

O2	7349(4)	15466(4)	10032(3)	63(1)	1

C1	2376(8)	9932(6)	7779(6)	77(1)	1

C2	1812(7)	10789(6)	6893(6)	82(2)	1

C3	3005(6)	11464(6)	6320(5)	71(1)	1

C4	4785(6)	11304(5)	6621(5)	62(1)	1

C5	5295(7)	10409(6)	7520(5)	73(1)	1

C6	4128(8)	9750(6)	8084(6)	81(2)	1

C7	6056(6)	12037(6)	5992(4)	65(1)	1

C8	7787(6)	13309(5)	7008(4)	54(1)	1

C9	8855(7)	14075(7)	6214(5)	70(1)	1

C10	7274(5)	14448(5)	7832(4)	49(1)	1

C11	7696(5)	14510(5)	9150(4)	54(1)	1

C12	6541(7)	16537(6)	9450(5)	72(1)	1

C13	5151(7)	15888(6)	7994(5)	74(1)	1

C14	6129(6)	15358(6)	7124(4)	63(1)	1

Table 3. Bond lengths [Å] and angles [°].

Br1(C1	1.887(6)

F1(C9	1.333(5)

F2(C9	1.349(6)

F3(C9	1.324(6)

O1(C8	1.420(5)

O2(C11	1.370(5)

O2(C12	1.435(6)

C1(C2	1.363(8)

C1(C6	1.376(8)

C2(C3	1.379(7)

C3(C4	1.390(6)

C4(C5	1.391(7)

C4(C7	1.489(7)

C5(C6	1.352(7)

C7(C8	1.530(6)

C8(C10	1.530(6)

C8(C9	1.530(6)

C10(C11	1.319(6)

C10(C14	1.497(6)

C12(C13	1.496(7)

C13(C14	1.517(6)

C11(O2(C12	115.2(3)

C2(C1(C6	119.4(5)

C2(C1(Br1	120.0(4)

C6(C1(Br1	120.6(5)

C1(C2(C3	119.6(5)

C2(C3(C4	122.0(5)

C3(C4(C5	116.5(5)

C3(C4(C7	121.4(5)

C5(C4(C7	122.1(4)

C6(C5(C4	121.6(5)

C5(C6(C1	121.0(5)

C4(C7(C8	113.9(4)

O1(C8(C7	106.6(4)

O1(C8(C10	112.5(3)

C7(C8(C10	112.8(3)

O1(C8(C9	106.0(3)

C7(C8(C9	108.8(4)

C10(C8(C9	109.9(4)

F3(C9(F1	106.8(5)

F3(C9(F2	106.9(4)

F1(C9(F2	105.5(4)

F3(C9(C8	112.3(4)

F1(C9(C8	113.4(4)

F2(C9(C8	111.4(5)

C11(C10(C14	120.4(4)

C11(C10(C8	118.8(4)

C14(C10(C8	120.4(3)

C10(C11(O2	126.2(4)

O2(C12(C13	111.7(4)

C12(C13(C14	109.8(4)

C10(C14(C13	109.4(4)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Br1	124(1) 	106(1)	176(1) 	34(1)	96(1) 	11(1)

F1	77(2) 	154(3)	67(2) 	57(2)	37(2) 	49(2)

F2	101(2) 	143(3)	93(2) 	32(2)	68(2) 	58(2)

F3	56(2) 	115(3)	87(2) 	35(2)	32(2) 	14(2)

O1	54(2) 	78(2)	57(2) 	13(2)	18(2) 	31(2)

O2	59(2) 	89(2)	45(2) 	10(2)	21(1) 	32(2)

C1	76(3) 	55(3)	92(4) 	0(3)	39(3) 	9(3)

C2	53(3) 	74(4)	105(4) 	0(3)	30(3) 	8(3)

C3	53(3) 	72(3)	75(3) 	4(3)	17(2) 	17(3)

C4	54(2) 	61(3)	57(3) 	(8(3)	20(2) 	11(2)

C5	67(3) 	72(3)	76(3) 	7(3)	25(3) 	26(3)

C6	94(4) 	64(3)	91(4) 	15(3)	43(3) 	27(3)

C7	56(3) 	76(3)	52(2) 	(1(2)	17(2) 	21(3)

C8	50(2) 	70(3)	45(2) 	15(2)	18(2) 	24(2)

C9	55(3) 	104(4)	59(3) 	20(3)	26(2) 	31(3)

C10	40(2) 	64(3)	41(2) 	12(2)	15(2) 	14(2)

C11	40(2) 	71(3)	48(2) 	11(2)	14(2) 	19(2)

C12	66(3) 	76(4)	72(3) 	6(3)	25(3) 	27(3)

C13	69(3) 	86(4)	70(3) 	13(3)	21(3) 	42(3)

C14	61(3) 	73(3)	54(2) 	16(2)	18(2) 	25(3)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1	9994	13290	8383	94	1

H2	629	10918	6675	98	1

H3	2606	12045	5715	85	1

H5	6467	10260	7738	87	1

H6	4515	9165	8688	97	1

H7A	5340	12421	5258	78	1

H7B	6479	11296	5585	78	1

H11	8286	13842	9515	65	1

H12A	7541	17379	9483	87	1

H12B	5913	16895	9995	87	1

H13A	4615	16633	7637	89	1

H13B	4131	15059	7957	89	1

H14A	5194	14764	6231	76	1

H14B	6945	16207	6986	76	1