|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	04src0091

Empirical formula 	C11H11FeN4O10

Formula weight 	415.09

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2/c

Unit cell dimensions	a = 12.463(5) Å	( = 90.000(5)°

b = 10.797(5) Å	( = 91.765(5)°

c = 22.201(5) Å	(  = 90.000(5)°

Volume	2986.0(19) Å3

Z	8

Density (calculated)	1.847 Mg / m3

Absorption coefficient	1.079 mm(1

F(000)	1688

Crystal	Shard; Orange

Crystal size	0.10 ( 0.05 ( 0.05 mm3

( range for data collection	3.07 ( 27.44°

Index ranges	(16 ( h ( 16, (13 ( k ( 13, (28 ( l ( 28

Reflections collected	18064

Independent reflections	3398 [Rint = 0.1110]

Completeness to ( = 27.44°	99.5 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9480 and 0.8998

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3398 / 6 / 251

Goodness-of-fit on F2	1.032

Final R indices [F2 > 2((F2)]	R1 = 0.0516, wR2 = 0.1240

R indices (all data)	R1 = 0.0815, wR2 = 0.1389

Largest diff. peak and hole	0.538 and (0.706 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

All hydrogen atoms were fixed.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	1225(3)	2145(3)	259(2)	25(1)	1

C2	1245(3)	2032(3)	(358(2)	27(1)	1

C3	1348(3)	869(3)	(606(2)	30(1)	1

C4	1409(3)	(142(3)	(230(2)	26(1)	1

C5	1382(3)	30(3)	387(2)	23(1)	1

C6	1417(3)	(992(3)	824(2)	24(1)	1

C7	1426(3)	(2251(3)	683(2)	28(1)	1

C8	1418(3)	(3100(3)	1145(2)	32(1)	1

C9	1398(3)	(2709(3)	1737(2)	30(1)	1

C10	1378(3)	(1446(3)	1847(2)	24(1)	1

C11	1282(3)	(866(3)	2456(2)	24(1)	1

N1	1294(2)	1174(2)	637(1)	22(1)	1

N2	1395(2)	(621(2)	1399(1)	22(1)	1

O1	1225(2)	326(2)	2440(1)	24(1)	1

O2	1240(2)	(1493(2)	2916(1)	27(1)	1

O11	(279(2)	1326(2)	1584(1)	24(1)	1

O12	2932(2)	1371(2)	1668(1)	25(1)	1

Fe1	1328(1)	1280(1)	1636(1)	22(1)	1

N21	1332(3)	3552(2)	1973(1)	27(1)	1

O21	1341(2)	2640(2)	2339(1)	28(1)	1

O22	1337(2)	3230(2)	1420(1)	28(1)	1

O23	1315(2)	4614(2)	2137(1)	36(1)	1

N31	3974(3)	(927(3)	910(1)	30(1)	1

O31	3843(3)	(152(2)	505(1)	45(1)	1

O32	4037(2)	(626(2)	1457(1)	39(1)	1

O33	4035(2)	(2065(2)	776(1)	35(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(N1	1.345(4)

C1(C2	1.376(5)

C1(H1	0.9500

C2(C3	1.379(5)

C2(H2	0.9500

C3(C4	1.375(5)

C3(H3	0.9500

C4(C5	1.383(5)

C4(H4	0.9500

C5(N1	1.360(4)

C5(C6	1.470(5)

C6(N2	1.337(4)

C6(C7	1.395(4)

C7(C8	1.376(5)

C7(H7	0.9500

C8(C9	1.383(5)

C8(H8	0.9500

C9(C10	1.385(4)

C9(H9	0.9500

C10(N2	1.337(4)

C10(C11	1.499(5)

C11(O2	1.228(4)

C11(O1	1.289(4)

N1(Fe1	2.221(3)

N2(Fe1	2.121(3)

O1(Fe1	2.067(2)

O11(Fe1	2.003(3)

O11(H11A	0.834(10)

O11(H11B	0.836(10)

O12(Fe1	2.001(3)

O12(H12A	0.835(10)

O12(H12B	0.834(10)

Fe1(O21	2.142(2)

Fe1(O22	2.160(2)

N21(O23	1.204(3)

N21(O21	1.275(3)

N21(O22	1.277(4)

N31(O31	1.235(4)

N31(O32	1.256(4)

N31(O33	1.268(4)

N1(C1(C2	123.3(3)

N1(C1(H1	118.3

C2(C1(H1	118.3

C1(C2(C3	118.9(3)

C1(C2(H2	120.6

C3(C2(H2	120.6

C4(C3(C2	119.0(3)

C4(C3(H3	120.5

C2(C3(H3	120.5

C3(C4(C5	119.5(3)

C3(C4(H4	120.3

C5(C4(H4	120.3

N1(C5(C4	122.1(3)

N1(C5(C6	114.4(3)

C4(C5(C6	123.6(3)

N2(C6(C7	120.5(3)

N2(C6(C5	113.8(3)

C7(C6(C5	125.6(3)

C8(C7(C6	118.7(3)

C8(C7(H7	120.6

C6(C7(H7	120.6

C7(C8(C9	120.4(3)

C7(C8(H8	119.8

C9(C8(H8	119.8

C8(C9(C10	118.0(3)

C8(C9(H9	121.0

C10(C9(H9	121.0

N2(C10(C9	121.6(3)

N2(C10(C11	113.4(3)

C9(C10(C11	124.9(3)

O2(C11(O1	124.8(3)

O2(C11(C10	121.8(3)

O1(C11(C10	113.4(3)

C1(N1(C5	117.3(3)

C1(N1(Fe1	125.6(2)

C5(N1(Fe1	117.1(2)

C10(N2(C6	120.8(3)

C10(N2(Fe1	117.3(2)

C6(N2(Fe1	121.9(2)

C11(O1(Fe1	121.1(2)

Fe1(O11(H11A	124(3)

Fe1(O11(H11B	117(2)

H11A(O11(H11B	108.1(17)

Fe1(O12(H12A	133(3)

Fe1(O12(H12B	114(3)

H12A(O12(H12B	108.1(17)

O12(Fe1(O11	175.54(9)

O12(Fe1(O1	94.70(10)

O11(Fe1(O1	88.52(10)

O12(Fe1(N2	90.55(10)

O11(Fe1(N2	93.27(10)

O1(Fe1(N2	74.73(10)

O12(Fe1(O21	87.39(10)

O11(Fe1(O21	90.59(10)

O1(Fe1(O21	73.29(9)

N2(Fe1(O21	147.66(10)

O12(Fe1(O22	86.98(10)

O11(Fe1(O22	88.57(9)

O1(Fe1(O22	132.69(9)

N2(Fe1(O22	152.57(10)

O21(Fe1(O22	59.54(9)

O12(Fe1(N1	91.49(10)

O11(Fe1(N1	87.47(11)

O1(Fe1(N1	146.82(9)

N2(Fe1(N1	72.64(10)

O21(Fe1(N1	139.65(9)

O22(Fe1(N1	80.12(9)

O23(N21(O21	122.9(3)

O23(N21(O22	123.4(3)

O21(N21(O22	113.7(2)

N21(O21(Fe1	93.84(18)

N21(O22(Fe1	92.93(17)

O31(N31(O32	122.1(3)

O31(N31(O33	119.6(3)

O32(N31(O33	118.4(3)

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	28(2) 	18(2)	29(2) 	3(1)	2(2) 	0(1)

C2	31(2) 	23(2)	28(2) 	5(1)	1(2) 	(4(2)

C3	36(2) 	32(2)	23(2) 	2(2)	1(2) 	(2(2)

C4	32(2) 	22(2)	25(2) 	(6(1)	1(2) 	(2(2)

C5	27(2) 	18(2)	24(2) 	0(1)	2(2) 	(1(1)

C6	31(2) 	16(2)	26(2) 	(2(1)	3(2) 	0(1)

C7	36(2) 	19(2)	28(2) 	(3(1)	0(2) 	0(2)

C8	46(2) 	14(2)	35(2) 	(2(1)	(2(2) 	2(2)

C9	44(2) 	16(2)	29(2) 	5(1)	2(2) 	2(2)

C10	30(2) 	18(2)	26(2) 	4(1)	2(2) 	(1(1)

C11	28(2) 	17(2)	26(2) 	0(1)	1(2) 	(1(1)

N1	28(2) 	17(1)	23(2) 	(1(1)	2(1) 	1(1)

N2	28(2) 	13(1)	25(1) 	(1(1)	(1(1) 	1(1)

O1	35(2) 	13(1)	25(1) 	2(1)	0(1) 	2(1)

O2	39(2) 	18(1)	24(1) 	4(1)	3(1) 	3(1)

O11	31(1) 	18(1)	25(1) 	3(1)	3(1) 	0(1)

O12	27(1) 	16(1)	31(1) 	(6(1)	1(1) 	0(1)

Fe1	30(1) 	12(1)	23(1) 	0(1)	1(1) 	1(1)

N21	33(2) 	20(1)	29(2) 	(1(1)	(1(1) 	(2(1)

O21	40(2) 	15(1)	27(1) 	2(1)	4(1) 	2(1)

O22	39(2) 	16(1)	28(1) 	0(1)	1(1) 	0(1)

O23	60(2) 	12(1)	37(2) 	(4(1)	1(1) 	1(1)

N31	31(2) 	23(2)	36(2) 	(2(1)	0(1) 	3(1)

O31	66(2) 	27(1)	43(2) 	13(1)	6(2) 	11(1)

O32	50(2) 	34(2)	34(2) 	(8(1)	(1(1) 	14(1)

O33	45(2) 	21(1)	37(2) 	(3(1)	(2(1) 	4(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1	1158	2951	426	30	1

H2	1190	2744	(609	33	1

H3	1376	767	(1031	37	1

H4	1469	(952	(393	32	1

H7	1436	(2517	275	33	1

H8	1427	(3961	1056	38	1

H9	1398	(3288	2059	36	1

H11A	(670(30)	1170(30)	1874(13)	53(15)	1

H11B	(570(30)	1900(20)	1382(13)	31(11)	1

H12A	3410(20)	830(30)	1654(19)	57(15)	1

H12B	3180(30)	1970(20)	1867(17)	54(14)	1

Table 6. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

O11(H11A...O1i	0.834(10)	1.925(14)	2.723(3)	160(3)

O11(H11B...O33ii	0.836(10)	1.808(13)	2.621(4)	164(3)

O12(H12A...O32	0.835(10)	1.816(15)	2.609(4)	158(4)

O12(H12B...O2iii	0.834(10)	1.870(16)	2.679(3)	163(4)

Symmetry transformations used to generate equivalent atoms:

(i) (x,y,(z+1/2    (ii) x(1/2,y+1/2,z    (iii) (x+1/2,y+1/2,(z+1/2