|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	04src0196

Empirical formula 	C44H36Cl4Mn2N16O16

Formula weight 	1296.57

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	Pbcn

Unit cell dimensions	a = 17.335(3) Å	( = 90°

b = 12.828(2) Å	( = 90°

c = 23.107(4) Å	(  = 90°

Volume	5138.4(15) Å3

Z	4

Density (calculated)	1.676 Mg / m3

Absorption coefficient	0.787 mm(1

F(000)	2632

Crystal	Slab; Orange

Crystal size	0.20 ( 0.16 ( 0.06 mm3

( range for data collection	2.94 ( 27.33°

Index ranges	(19 ( h ( 22, (16 ( k ( 12, (27 ( l ( 29

Reflections collected	37974

Independent reflections	5772 [Rint = 0.1823]

Completeness to ( = 27.33°	99.6 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9543 and 0.8584

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	5772 / 0 / 370

Goodness-of-fit on F2	1.066

Final R indices [F2 > 2((F2)]	R1 = 0.0548, wR2 = 0.1298

R indices (all data)	R1 = 0.0745, wR2 = 0.1422

Largest diff. peak and hole	0.675 and (0.555 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

All hydrogen atoms were fixed.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	1069(2)	7000(2)	4554(1)	27(1)	1

C2	1441(2)	6505(2)	5006(1)	28(1)	1

C3	1359(2)	5429(2)	5061(1)	28(1)	1

C4	890(2)	4901(2)	4676(1)	25(1)	1

C5	517(1)	5453(2)	4236(1)	19(1)	1

C6	(19(2)	4951(2)	3815(1)	20(1)	1

C7	(189(2)	3885(2)	3803(1)	23(1)	1

C8	(701(2)	3509(2)	3393(1)	25(1)	1

C9	(1039(2)	4193(2)	3002(1)	24(1)	1

C10	(839(1)	5244(2)	3031(1)	20(1)	1

C11	(1098(1)	6059(2)	2612(1)	19(1)	1

C12	1046(2)	8637(2)	2646(1)	19(1)	1

C13	795(1)	9418(2)	3092(1)	19(1)	1

C14	1009(2)	10460(2)	3096(1)	25(1)	1

C15	666(2)	11109(2)	3503(1)	29(1)	1

C16	128(2)	10717(2)	3886(1)	25(1)	1

C17	(45(1)	9654(2)	3870(1)	20(1)	1

C18	(603(1)	9129(2)	4266(1)	20(1)	1

C19	(981(2)	9633(2)	4716(1)	27(1)	1

C20	(1493(2)	9076(3)	5064(1)	31(1)	1

C21	(1606(2)	8026(3)	4954(2)	32(1)	1

C22	(1218(2)	7572(2)	4497(2)	27(1)	1

N1	615(1)	6494(2)	4171(1)	22(1)	1

N2	(337(1)	5604(2)	3432(1)	19(1)	1

N3	(1507(1)	5793(2)	2145(1)	23(1)	1

N4	(849(1)	7000(2)	2722(1)	19(1)	1

N5	852(1)	7670(2)	2765(1)	19(1)	1

N6	1387(1)	8949(2)	2158(1)	21(1)	1

N7	288(1)	9024(2)	3479(1)	19(1)	1

N8	(723(1)	8097(2)	4154(1)	22(1)	1

Mn1	(25(1)	7318(1)	3446(1)	19(1)	1

O1	(2482(1)	7462(2)	3495(1)	49(1)	1

O2	(3246(2)	6575(2)	4148(1)	58(1)	1

O3	(3333(2)	6155(2)	3182(1)	68(1)	1

O4	(2229(1)	5690(2)	3707(1)	54(1)	1

Cl1	(2811(1)	6466(1)	3630(1)	26(1)	1

O11	(2413(1)	3841(2)	1906(1)	39(1)	1

O12	(2734(1)	3849(2)	917(1)	48(1)	1

O13	(2537(1)	2249(2)	1395(1)	36(1)	1

O14	(1489(1)	3368(2)	1217(1)	39(1)	1

Cl11	(2296(1)	3329(1)	1357(1)	23(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(N1	1.351(4)

C1(C2	1.382(4)

C1(H1	0.9500

C2(C3	1.393(5)

C2(H2	0.9500

C3(C4	1.382(4)

C3(H3	0.9500

C4(C5	1.395(4)

C4(H4	0.9500

C5(N1	1.355(4)

C5(C6	1.493(4)

C6(N2	1.338(4)

C6(C7	1.398(4)

C7(C8	1.386(4)

C7(H7	0.9500

C8(C9	1.389(4)

C8(H8	0.9500

C9(C10	1.393(4)

C9(H9	0.9500

C10(N2	1.352(4)

C10(C11	1.494(4)

C11(N4	1.306(3)

C11(N3	1.337(4)

C12(N5	1.314(3)

C12(N6	1.334(4)

C12(C13	1.501(4)

C13(N7	1.352(3)

C13(C14	1.388(4)

C14(C15	1.390(4)

C14(H14	0.9500

C15(C16	1.381(4)

C15(H15	0.9500

C16(C17	1.396(4)

C16(H16	0.9500

C17(N7	1.343(4)

C17(C18	1.491(4)

C18(N8	1.365(4)

C18(C19	1.388(4)

C19(C20	1.395(4)

C19(H19	0.9500

C20(C21	1.385(5)

C20(H20	0.9500

C21(C22	1.380(5)

C21(H21	0.9500

C22(N8	1.348(4)

C22(H22	0.9500

N1(Mn1	2.269(2)

N2(Mn1	2.264(2)

N3(H3A	0.8800

N3(H3B	0.8800

N4(N5i	1.415(3)

N4(Mn1	2.238(2)

N5(N4i	1.415(3)

N5(Mn1	2.236(2)

N6(H6A	0.8800

N6(H6B	0.8800

N7(Mn1	2.256(2)

N8(Mn1	2.266(2)

O1(Cl1	1.434(3)

O2(Cl1	1.421(3)

O3(Cl1	1.433(3)

O4(Cl1	1.428(2)

O11(Cl11	1.441(2)

O12(Cl11	1.434(2)

O13(Cl11	1.449(2)

O14(Cl11	1.438(2)

N1(C1(C2	123.1(3)

N1(C1(H1	118.4

C2(C1(H1	118.4

C1(C2(C3	118.4(3)

C1(C2(H2	120.8

C3(C2(H2	120.8

C4(C3(C2	119.1(3)

C4(C3(H3	120.5

C2(C3(H3	120.5

C3(C4(C5	119.5(3)

C3(C4(H4	120.3

C5(C4(H4	120.3

N1(C5(C4	121.6(3)

N1(C5(C6	115.4(2)

C4(C5(C6	123.0(3)

N2(C6(C7	120.9(3)

N2(C6(C5	114.7(2)

C7(C6(C5	124.4(3)

C8(C7(C6	119.3(3)

C8(C7(H7	120.4

C6(C7(H7	120.4

C7(C8(C9	119.6(3)

C7(C8(H8	120.2

C9(C8(H8	120.2

C8(C9(C10	118.4(3)

C8(C9(H9	120.8

C10(C9(H9	120.8

N2(C10(C9	121.6(3)

N2(C10(C11	113.4(2)

C9(C10(C11	124.9(3)

N4(C11(N3	124.6(3)

N4(C11(C10	115.0(2)

N3(C11(C10	120.2(2)

N5(C12(N6	124.9(3)

N5(C12(C13	114.4(2)

N6(C12(C13	120.6(2)

N7(C13(C14	122.0(3)

N7(C13(C12	113.2(2)

C14(C13(C12	124.7(3)

C13(C14(C15	117.9(3)

C13(C14(H14	121.1

C15(C14(H14	121.1

C16(C15(C14	120.3(3)

C16(C15(H15	119.9

C14(C15(H15	119.9

C15(C16(C17	119.0(3)

C15(C16(H16	120.5

C17(C16(H16	120.5

N7(C17(C16	120.8(3)

N7(C17(C18	114.7(2)

C16(C17(C18	124.4(3)

N8(C18(C19	121.4(3)

N8(C18(C17	114.9(2)

C19(C18(C17	123.6(3)

C18(C19(C20	119.6(3)

C18(C19(H19	120.2

C20(C19(H19	120.2

C21(C20(C19	118.7(3)

C21(C20(H20	120.6

C19(C20(H20	120.6

C22(C21(C20	118.9(3)

C22(C21(H21	120.6

C20(C21(H21	120.6

N8(C22(C21	123.2(3)

N8(C22(H22	118.4

C21(C22(H22	118.4

C1(N1(C5	118.2(3)

C1(N1(Mn1	123.02(19)

C5(N1(Mn1	118.74(19)

C6(N2(C10	120.3(2)

C6(N2(Mn1	119.99(19)

C10(N2(Mn1	119.75(18)

C11(N3(H3A	120.0

C11(N3(H3B	120.0

H3A(N3(H3B	120.0

C11(N4(N5i	114.0(2)

C11(N4(Mn1	121.55(18)

N5i(N4(Mn1	119.11(15)

C12(N5(N4i	114.1(2)

C12(N5(Mn1	120.77(18)

N4i(N5(Mn1	115.73(15)

C12(N6(H6A	120.0

C12(N6(H6B	120.0

H6A(N6(H6B	120.0

C17(N7(C13	120.0(2)

C17(N7(Mn1	120.24(18)

C13(N7(Mn1	119.75(18)

C22(N8(C18	118.1(3)

C22(N8(Mn1	122.9(2)

C18(N8(Mn1	118.88(18)

N5(Mn1(N4	86.78(9)

N5(Mn1(N7	70.36(8)

N4(Mn1(N7	110.81(8)

N5(Mn1(N2	110.37(8)

N4(Mn1(N2	70.11(8)

N7(Mn1(N2	178.92(9)

N5(Mn1(N8	141.46(8)

N4(Mn1(N8	106.23(8)

N7(Mn1(N8	71.11(8)

N2(Mn1(N8	108.16(8)

N5(Mn1(N1	106.31(8)

N4(Mn1(N1	141.19(8)

N7(Mn1(N1	108.00(8)

N2(Mn1(N1	71.09(8)

N8(Mn1(N1	86.24(9)

O2(Cl1(O4	109.78(18)

O2(Cl1(O3	107.5(2)

O4(Cl1(O3	109.99(17)

O2(Cl1(O1	107.89(17)

O4(Cl1(O1	111.57(17)

O3(Cl1(O1	109.97(18)

O12(Cl11(O14	109.81(16)

O12(Cl11(O11	109.68(16)

O14(Cl11(O11	108.61(14)

O12(Cl11(O13	109.59(15)

O14(Cl11(O13	109.09(14)

O11(Cl11(O13	110.04(15)

Symmetry transformations used to generate equivalent atoms:

(i) (x,y,(z+1/2

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	24(1) 	28(2)	28(2) 	(1(1)	1(1) 	(3(1)

C2	22(1) 	39(2)	24(2) 	(3(1)	1(1) 	(1(1)

C3	23(1) 	37(2)	25(2) 	2(1)	(2(1) 	7(1)

C4	25(1) 	26(2)	25(2) 	1(1)	0(1) 	3(1)

C5	17(1) 	23(1)	16(1) 	1(1)	5(1) 	2(1)

C6	17(1) 	20(1)	22(2) 	1(1)	3(1) 	2(1)

C7	23(1) 	21(1)	26(2) 	5(1)	3(1) 	0(1)

C8	24(1) 	16(1)	34(2) 	4(1)	1(1) 	(3(1)

C9	21(1) 	22(1)	28(2) 	(3(1)	(1(1) 	(3(1)

C10	18(1) 	18(1)	23(2) 	1(1)	3(1) 	0(1)

C11	15(1) 	19(1)	23(2) 	(1(1)	2(1) 	2(1)

C12	16(1) 	20(1)	21(2) 	0(1)	(3(1) 	(1(1)

C13	17(1) 	20(1)	20(2) 	1(1)	(2(1) 	1(1)

C14	24(1) 	24(1)	26(2) 	(1(1)	1(1) 	(3(1)

C15	33(2) 	19(1)	34(2) 	(5(1)	0(1) 	(3(1)

C16	24(1) 	22(1)	29(2) 	(5(1)	0(1) 	0(1)

C17	19(1) 	20(1)	21(2) 	(2(1)	(3(1) 	2(1)

C18	17(1) 	22(1)	20(2) 	(1(1)	(3(1) 	2(1)

C19	24(1) 	31(2)	25(2) 	(4(1)	(1(1) 	3(1)

C20	24(1) 	44(2)	25(2) 	(1(1)	5(1) 	6(1)

C21	23(1) 	41(2)	31(2) 	9(1)	4(1) 	(1(1)

C22	26(1) 	28(2)	27(2) 	7(1)	0(1) 	0(1)

N1	18(1) 	24(1)	23(1) 	0(1)	2(1) 	(1(1)

N2	19(1) 	19(1)	20(1) 	1(1)	2(1) 	(1(1)

N3	27(1) 	19(1)	24(1) 	1(1)	(7(1) 	(2(1)

N4	20(1) 	18(1)	18(1) 	1(1)	0(1) 	1(1)

N5	20(1) 	20(1)	17(1) 	(1(1)	(1(1) 	(1(1)

N6	24(1) 	20(1)	20(1) 	1(1)	2(1) 	(1(1)

N7	17(1) 	18(1)	22(1) 	0(1)	(1(1) 	(2(1)

N8	19(1) 	22(1)	24(1) 	1(1)	0(1) 	0(1)

Mn1	22(1) 	16(1)	19(1) 	0(1)	0(1) 	(2(1)

O1	36(1) 	46(2)	65(2) 	20(1)	3(1) 	(12(1)

O2	75(2) 	39(2)	61(2) 	(1(1)	40(2) 	3(1)

O3	94(2) 	39(2)	73(2) 	(19(2)	(52(2) 	14(2)

O4	40(1) 	55(2)	68(2) 	15(2)	2(1) 	23(1)

Cl1	23(1) 	27(1)	28(1) 	(3(1)	0(1) 	2(1)

O11	33(1) 	48(1)	37(2) 	(18(1)	9(1) 	(14(1)

O12	50(1) 	40(1)	53(2) 	7(1)	(23(1) 	0(1)

O13	39(1) 	28(1)	42(2) 	0(1)	9(1) 	(11(1)

O14	27(1) 	34(1)	54(2) 	6(1)	17(1) 	1(1)

Cl11	20(1) 	23(1)	26(1) 	(2(1)	3(1) 	(1(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1	1135	7731	4511	32	1

H2	1745	6889	5273	34	1

H3	1622	5063	5359	34	1

H4	821	4169	4710	30	1

H7	45	3425	4073	28	1

H8	(821	2787	3380	30	1

H9	(1397	3950	2722	29	1

H14	1379	10721	2829	29	1

H15	802	11826	3517	34	1

H16	(120	11163	4156	30	1

H19	(891	10352	4785	32	1

H20	(1759	9412	5372	37	1

H21	(1944	7625	5189	38	1

H22	(1305	6854	4420	32	1

H3A	(1625	6267	1884	28	1

H3B	(1657	5143	2097	28	1

H6A	1499	8492	1887	25	1

H6B	1500	9611	2108	25	1

Table 6. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

N3(H3A...O13ii	0.88	2.23	3.039(3)	152.8

N3(H3B...O11	0.88	2.17	3.007(3)	159.0

N6(H6A...O1i	0.88	2.33	3.084(3)	144.0

N6(H6B...O3iii	0.88	2.11	2.977(4)	168.2

Symmetry transformations used to generate equivalent atoms:

(i) (x,y,(z+1/2    (ii) (x(1/2,y+1/2,z    (iii) x+1/2,y+1/2,(z+1/2