|  | University of Southampton · School of Chemistry # EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	04src0333

Empirical formula 	C48H59Cl6Fe4N24O35.50

Formula weight 	1976.29

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 14.668(5) Å	a = 90.000(5)°

b = 19.628(5) Å	b = 93.882(5)°

c = 25.461(5) Å	g  = 90.000(5)°

Volume	7313(3) Å3

Z	4

Density (calculated)	1.795 Mg / m3

Absorption coefficient	1.107 mm-1

F(000)	4020

Crystal	Block; Dark Brown

Crystal size	0.28 ´ 0.12 ´ 0.08 mm3

q range for data collection	2.92 - 27.48°

Index ranges	-18 £ h £ 19, -25 £ k £ 24, -29 £ l £ 33

Reflections collected	100334

Independent reflections	16735 [Rint = 0.0626]

Completeness to q = 27.48°	99.9 %

Absorption correction	Semi-empirical from equivalents

Max. and min. transmission	0.9167 and 0.7469

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	16735 / 550 / 1109

Goodness-of-fit on F2	1.072

Final R indices [F2 > 2s(F2)]	R1 = 0.0724, wR2 = 0.1642

R indices (all data)	R1 = 0.1105, wR2 = 0.1817

Largest diff. peak and hole	1.452 and -0.954 e Å-3

Diffractometer: Nonius KappaCCD area detector (f scans and w scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307-326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33-37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421-426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467-473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

All hydrogen atoms were fixed.

It was not possible to locate the hydrogen atoms of the water molecules, thus they have only been included for completeness.

Table 2. Atomic coordinates [´ 104], equivalent isotropic displacement parameters [Å2 ´ 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Fe1	10067(1)	2513(1)	9009(1)	24(1)	1

Fe2	8389(1)	1259(1)	8424(1)	20(1)	1

Fe3	8188(1)	3689(1)	9213(1)	24(1)	1

Fe4	6583(1)	2246(1)	8929(1)	20(1)	1

O1	10537(3)	3434(2)	9198(2)	34(1)	1

O2	9398(2)	682(2)	8056(1)	27(1)	1

O3	9288(3)	4092(2)	9516(2)	47(1)	1

O4	5390(2)	2722(2)	9195(1)	29(1)	1

O11	8843(2)	2863(2)	9040(1)	25(1)	1

O12	7633(2)	1860(2)	8728(1)	22(1)	1

C1	12204(4)	2520(3)	9080(2)	35(1)	1

C2	13039(4)	2655(4)	8871(3)	43(2)	1

C3	13083(4)	2681(3)	8338(3)	37(1)	1

C4	12316(4)	2538(3)	8009(2)	31(1)	1

C5	11509(3)	2393(3)	8243(2)	26(1)	1

C6	10637(3)	2224(3)	7947(2)	24(1)	1

C7	8637(3)	2380(3)	7612(2)	24(1)	1

C8	7823(3)	2001(3)	7391(2)	25(1)	1

C9	7289(4)	2197(3)	6947(2)	30(1)	1

C10	6581(4)	1771(3)	6766(2)	33(1)	1

C11	6430(4)	1169(3)	7028(2)	32(1)	1

C12	6988(3)	1019(3)	7477(2)	26(1)	1

C13	6897(3)	400(3)	7802(2)	23(1)	1

C14	6335(4)	-148(3)	7669(2)	34(1)	1

C15	6367(4)	-703(3)	7997(2)	37(1)	1

C16	6914(4)	-698(3)	8459(2)	31(1)	1

C17	7435(3)	-128(3)	8574(2)	25(1)	1

C18	8045(3)	-28(3)	9055(2)	24(1)	1

C19	9480(3)	1242(3)	9456(2)	25(1)	1

C20	9965(3)	1571(3)	9910(2)	27(1)	1

C21	10003(4)	1307(3)	10416(2)	34(1)	1

C22	10403(4)	1683(4)	10823(2)	39(2)	1

C23	10745(4)	2323(4)	10717(2)	43(2)	1

C24	10701(4)	2552(3)	10204(2)	36(1)	1

N1	11444(3)	2402(2)	8770(2)	28(1)	1

N2	10647(3)	1964(2)	7473(2)	29(1)	1

N3	9913(3)	2340(2)	8212(2)	24(1)	1

N4	9077(3)	2066(2)	8006(2)	23(1)	1

N5	8876(3)	2961(2)	7406(2)	30(1)	1

N6	7667(3)	1428(2)	7653(2)	22(1)	1

N7	7434(3)	410(2)	8248(2)	23(1)	1

N8	8084(3)	-482(2)	9443(2)	28(1)	1

N9	8493(3)	541(2)	9060(2)	23(1)	1

N10	9010(3)	695(2)	9526(2)	24(1)	1

N11	9515(2)	1561(2)	8999(1)	9(1)	1

N12	10312(3)	2184(2)	9804(2)	28(1)	1

C31	7621(5)	5187(3)	9509(2)	39(1)	1

C32	7346(5)	5680(3)	9856(3)	43(2)	1

C33	6978(5)	5482(3)	10312(3)	46(2)	1

C34	6849(5)	4793(3)	10407(2)	39(1)	1

C35	7118(4)	4337(3)	10035(2)	30(1)	1

C36	6975(4)	3596(3)	10077(2)	28(1)	1

C37	7460(3)	2086(3)	10046(2)	22(1)	1

C38	7027(3)	1404(2)	9934(2)	20(1)	1

C39	7151(3)	833(3)	10241(2)	23(1)	1

C40	6634(4)	261(3)	10109(2)	26(1)	1

C41	6032(3)	267(3)	9670(2)	25(1)	1

C42	5978(3)	851(3)	9362(2)	22(1)	1

C43	5413(3)	924(3)	8860(2)	24(1)	1

C44	4758(4)	464(3)	8673(2)	30(1)	1

C45	4284(4)	601(3)	8201(2)	36(1)	1

C46	4462(4)	1187(3)	7921(2)	31(1)	1

C47	5126(3)	1626(3)	8137(2)	24(1)	1

C48	5420(3)	2265(3)	7894(2)	24(1)	1

C49	6964(3)	3458(3)	8279(2)	23(1)	1

C50	7525(4)	4038(3)	8122(2)	25(1)	1

C51	7407(4)	4358(3)	7637(2)	32(1)	1

C52	8003(4)	4873(3)	7527(2)	36(1)	1

C53	8703(4)	5048(3)	7890(3)	40(2)	1

C54	8769(4)	4711(3)	8369(2)	35(1)	1

N31	7504(3)	4520(2)	9592(2)	29(1)	1

N32	6337(3)	3363(3)	10369(2)	35(1)	1

N33	7499(3)	3222(2)	9794(2)	24(1)	1

N34	7202(3)	2549(2)	9703(2)	22(1)	1

N35	8021(3)	2177(2)	10470(2)	25(1)	1

N36	6456(3)	1411(2)	9497(2)	22(1)	1

N37	5593(3)	1489(2)	8600(2)	22(1)	1

N38	5026(3)	2491(2)	7442(2)	32(1)	1

N39	6076(3)	2578(2)	8169(2)	24(1)	1

N40	6432(3)	3152(2)	7936(2)	26(1)	1

N41	7087(2)	3272(2)	8778(1)	10(1)	1

N42	8186(3)	4215(2)	8489(2)	26(1)	1

O111	1587(3)	857(2)	9364(2)	44(1)	1

O112	2454(3)	228(2)	8790(2)	40(1)	1

O113	968(3)	-98(2)	8924(2)	51(1)	1

O114	1225(3)	892(2)	8452(2)	37(1)	1

Cl11	1570(1)	477(1)	8887(1)	26(1)	1

O121	4938(3)	8842(2)	9285(2)	36(1)	1

O122	5058(3)	8143(3)	8560(2)	55(1)	1

O123	3848(3)	7985(2)	9099(2)	34(1)	1

O124	3871(3)	8942(2)	8568(2)	53(1)	1

Cl12	4435(1)	8470(1)	8876(1)	30(1)	1

O131	752(5)	6856(3)	8430(3)	68(2)	0.806(8)

O132	1191(5)	6450(3)	9256(3)	72(2)	0.806(8)

O133	1454(8)	5789(5)	8537(4)	125(3)	0.806(8)

O134	-51(6)	5971(6)	8788(5)	115(4)	0.806(8)

Cl13	831(4)	6245(3)	8752(2)	60(1)	0.806(8)

O331	20(20)	6089(18)	9063(13)	92(8)	0.194(8)

O332	989(18)	6957(10)	8831(11)	65(6)	0.194(8)

O333	620(20)	6106(14)	8227(8)	79(7)	0.194(8)

O334	1566(19)	5863(15)	8945(13)	89(7)	0.194(8)

Cl33	785(16)	6257(10)	8777(9)	66(5)	0.194(8)

O141	8539(4)	9535(3)	7521(2)	68(2)	1

O142	9842(4)	9210(2)	8038(2)	57(1)	1

O143	9468(3)	8679(2)	7232(2)	39(1)	1

O144	8594(3)	8466(3)	7953(2)	53(1)	1

Cl14	9098(1)	8968(1)	7690(1)	37(1)	1

O151	6169(3)	6580(3)	8327(2)	52(1)	1

O152	7722(4)	6578(3)	8160(3)	88(2)	1

O153	6968(4)	7590(3)	8246(3)	75(2)	1

O154	7249(4)	6922(4)	8978(2)	101(2)	1

Cl15	7043(1)	6899(1)	8428(1)	41(1)	1

O161	4882(4)	3782(2)	8570(2)	64(1)	1

O162	5679(5)	4768(3)	8400(3)	110(3)	1

O163	5305(4)	4539(4)	9247(2)	84(2)	1

O164	4171(4)	4820(3)	8612(2)	68(2)	1

Cl16	5016(1)	4482(1)	8707(1)	52(1)	1

O201	8149(3)	1314(2)	11445(1)	34(1)	1

O202	5306(3)	6088(3)	9253(2)	61(1)	1

O203	5683(4)	7181(3)	9984(2)	67(2)	1

O204	6816(4)	8228(3)	9509(2)	62(1)	1

O205	8418(4)	9301(3)	6315(2)	57(1)	1

O206	9634(19)	4822(11)	10296(9)	187(10)	0.50

Table 3. Bond lengths [Å] and angles [°].

Fe1-O11	1.929(4)

Fe1-O1	1.983(4)

Fe1-N11	2.035(4)

Fe1-N3	2.055(4)

Fe1-N12	2.132(4)

Fe1-N1	2.160(4)

Fe2-O12	1.826(3)

Fe2-O2	2.130(4)

Fe2-N9	2.142(4)

Fe2-N6	2.193(4)

Fe2-N4	2.194(4)

Fe2-N7	2.203(4)

Fe2-N11	2.213(3)

Fe3-O3	1.911(4)

Fe3-O11	1.950(4)

Fe3-N33	2.064(4)

Fe3-N41	2.064(3)

Fe3-N42	2.111(5)

Fe3-N31	2.175(5)

Fe4-O12	1.821(3)

Fe4-N39	2.129(4)

Fe4-O4	2.134(4)

Fe4-N41	2.189(4)

Fe4-N34	2.194(4)

Fe4-N36	2.200(4)

Fe4-N37	2.204(4)

C1-N1	1.342(7)

C1-C2	1.394(8)

C1-H1	0.9500

C2-C3	1.363(9)

C2-H2	0.9500

C3-C4	1.385(8)

C3-H3	0.9500

C4-C5	1.390(8)

C4-H4	0.9500

C5-N1	1.352(7)

C5-C6	1.478(7)

C6-N2	1.312(7)

C6-N3	1.315(7)

C7-N4	1.309(6)

C7-N5	1.313(7)

C7-C8	1.484(7)

C8-N6	1.336(7)

C8-C9	1.386(7)

C9-C10	1.389(8)

C9-H9	0.9500

C10-C11	1.382(8)

C10-H10	0.9500

C11-C12	1.391(7)

C11-H11	0.9500

C12-N6	1.333(6)

C12-C13	1.481(7)

C13-N7	1.338(6)

C13-C14	1.383(7)

C14-C15	1.372(8)

C14-H14	0.9500

C15-C16	1.380(8)

C15-H15	0.9500

C16-C17	1.376(8)

C16-H16	0.9500

C17-N7	1.342(7)

C17-C18	1.480(7)

C18-N9	1.296(7)

C18-N8	1.329(7)

C19-N10	1.294(7)

C19-N11	1.324(6)

C19-C20	1.466(7)

C20-N12	1.341(7)

C20-C21	1.387(8)

C21-C22	1.370(8)

C21-H21	0.9500

C22-C23	1.385(10)

C22-H22	0.9500

C23-C24	1.379(9)

C23-H23	0.9500

C24-N12	1.343(7)

C24-H24	0.9500

N2-H2A	0.8800

N2-H2B	0.8800

N3-N4	1.407(6)

N5-H5A	0.8800

N5-H5B	0.8800

N8-H8A	0.8800

N8-H8B	0.8800

N9-N10	1.397(6)

C31-N31	1.339(7)

C31-C32	1.388(9)

C31-H31	0.9500

C32-C33	1.368(9)

C32-H32	0.9500

C33-C34	1.390(9)

C33-H33	0.9500

C34-C35	1.380(8)

C34-H34	0.9500

C35-N31	1.345(7)

C35-C36	1.474(8)

C36-N33	1.313(7)

C36-N32	1.316(7)

C37-N34	1.297(6)

C37-N35	1.325(6)

C37-C38	1.501(7)

C38-N36	1.348(6)

C38-C39	1.373(7)

C39-C40	1.384(7)

C39-H39	0.9500

C40-C41	1.376(7)

C40-H40	0.9500

C41-C42	1.388(7)

C41-H41	0.9500

C42-N36	1.336(6)

C42-C43	1.483(7)

C43-N37	1.328(7)

C43-C44	1.379(7)

C44-C45	1.373(8)

C44-H44	0.9500

C45-C46	1.386(8)

C45-H45	0.9500

C46-C47	1.387(7)

C46-H46	0.9500

C47-N37	1.349(6)

C47-C48	1.476(7)

C48-N39	1.305(6)

C48-N38	1.328(7)

C49-N40	1.280(7)

C49-N41	1.323(6)

C49-C50	1.475(7)

C50-N42	1.346(7)

C50-C51	1.387(8)

C51-C52	1.379(8)

C51-H51	0.9500

C52-C53	1.376(9)

C52-H52	0.9500

C53-C54	1.384(9)

C53-H53	0.9500

C54-N42	1.346(7)

C54-H54	0.9500

N32-H32A	0.8800

N32-H32B	0.8800

N33-N34	1.406(6)

N35-H35A	0.8800

N35-H35B	0.8800

N38-H38A	0.8800

N38-H38B	0.8800

N39-N40	1.392(6)

O111-Cl11	1.424(4)

O112-Cl11	1.423(4)

O113-Cl11	1.440(4)

O114-Cl11	1.439(4)

O121-Cl12	1.435(4)

O122-Cl12	1.412(4)

O123-Cl12	1.427(4)

O124-Cl12	1.439(4)

O131-Cl13	1.453(7)

O132-Cl13	1.412(7)

O133-Cl13	1.415(9)

O134-Cl13	1.409(8)

O331-Cl33	1.420(14)

O332-Cl33	1.412(14)

O333-Cl33	1.435(14)

O334-Cl33	1.422(14)

O141-Cl14	1.432(5)

O142-Cl14	1.438(4)

O143-Cl14	1.435(4)

O144-Cl14	1.426(5)

O151-Cl15	1.434(4)

O152-Cl15	1.396(5)

O153-Cl15	1.435(5)

O154-Cl15	1.414(5)

O161-Cl16	1.429(5)

O162-Cl16	1.405(6)

O163-Cl16	1.416(6)

O164-Cl16	1.412(5)

O11-Fe1-O1	88.49(16)

O11-Fe1-N11	87.54(15)

O1-Fe1-N11	166.22(16)

O11-Fe1-N3	93.43(16)

O1-Fe1-N3	113.80(17)

N11-Fe1-N3	79.62(15)

O11-Fe1-N12	99.55(16)

O1-Fe1-N12	90.67(17)

N11-Fe1-N12	77.00(16)

N3-Fe1-N12	152.63(18)

O11-Fe1-N1	159.81(17)

O1-Fe1-N1	81.04(17)

N11-Fe1-N1	106.44(16)

N3-Fe1-N1	75.39(17)

N12-Fe1-N1	97.80(17)

O12-Fe2-O2	171.61(15)

O12-Fe2-N9	96.90(16)

O2-Fe2-N9	88.09(15)

O12-Fe2-N6	90.58(15)

O2-Fe2-N6	89.68(15)

N9-Fe2-N6	141.43(16)

O12-Fe2-N4	92.94(16)

O2-Fe2-N4	79.25(15)

N9-Fe2-N4	146.09(15)

N6-Fe2-N4	70.44(15)

O12-Fe2-N7	100.36(16)

O2-Fe2-N7	87.65(15)

N9-Fe2-N7	70.67(16)

N6-Fe2-N7	70.76(15)

N4-Fe2-N7	138.95(15)

O12-Fe2-N11	89.66(14)

O2-Fe2-N11	85.65(13)

N9-Fe2-N11	70.43(14)

N6-Fe2-N11	147.70(15)

N4-Fe2-N11	77.29(14)

N7-Fe2-N11	140.69(14)

O3-Fe3-O11	91.15(17)

O3-Fe3-N33	109.6(2)

O11-Fe3-N33	93.69(16)

O3-Fe3-N41	171.37(19)

O11-Fe3-N41	85.91(14)

N33-Fe3-N41	78.73(15)

O3-Fe3-N42	95.8(2)

O11-Fe3-N42	100.48(16)

N33-Fe3-N42	150.60(17)

N41-Fe3-N42	76.76(15)

O3-Fe3-N31	85.02(18)

O11-Fe3-N31	166.58(16)

N33-Fe3-N31	75.61(17)

N41-Fe3-N31	99.62(15)

N42-Fe3-N31	92.71(17)

O12-Fe4-N39	96.95(16)

O12-Fe4-O4	177.31(15)

N39-Fe4-O4	84.84(15)

O12-Fe4-N41	91.77(14)

N39-Fe4-N41	70.10(15)

O4-Fe4-N41	86.94(14)

O12-Fe4-N34	93.41(15)

N39-Fe4-N34	146.23(17)

O4-Fe4-N34	84.01(15)

N41-Fe4-N34	77.56(14)

O12-Fe4-N36	89.23(15)

N39-Fe4-N36	141.72(16)

O4-Fe4-N36	90.61(15)

N41-Fe4-N36	147.71(14)

N34-Fe4-N36	70.17(15)

O12-Fe4-N37	99.23(16)

N39-Fe4-N37	71.28(16)

O4-Fe4-N37	83.24(15)

N41-Fe4-N37	140.80(14)

N34-Fe4-N37	138.30(16)

N36-Fe4-N37	70.45(15)

Fe1-O11-Fe3	141.2(2)

Fe4-O12-Fe2	159.6(2)

N1-C1-C2	121.6(6)

N1-C1-H1	119.2

C2-C1-H1	119.2

C3-C2-C1	119.3(5)

C3-C2-H2	120.3

C1-C2-H2	120.3

C2-C3-C4	120.2(6)

C2-C3-H3	119.9

C4-C3-H3	119.9

C3-C4-C5	117.5(5)

C3-C4-H4	121.2

C5-C4-H4	121.2

N1-C5-C4	122.8(5)

N1-C5-C6	113.1(5)

C4-C5-C6	124.0(5)

N2-C6-N3	126.7(5)

N2-C6-C5	119.6(5)

N3-C6-C5	113.6(5)

N4-C7-N5	125.7(5)

N4-C7-C8	113.4(4)

N5-C7-C8	120.9(4)

N6-C8-C9	122.3(5)

N6-C8-C7	113.2(4)

C9-C8-C7	124.5(5)

C8-C9-C10	118.2(5)

C8-C9-H9	120.9

C10-C9-H9	120.9

C11-C10-C9	119.7(5)

C11-C10-H10	120.1

C9-C10-H10	120.1

C10-C11-C12	118.3(5)

C10-C11-H11	120.9

C12-C11-H11	120.9

N6-C12-C11	122.2(5)

N6-C12-C13	113.6(4)

C11-C12-C13	124.2(5)

N7-C13-C14	121.6(5)

N7-C13-C12	113.2(4)

C14-C13-C12	125.2(5)

C15-C14-C13	118.4(5)

C15-C14-H14	120.8

C13-C14-H14	120.8

C14-C15-C16	120.5(5)

C14-C15-H15	119.8

C16-C15-H15	119.8

C17-C16-C15	118.0(5)

C17-C16-H16	121.0

C15-C16-H16	121.0

N7-C17-C16	122.1(5)

N7-C17-C18	112.5(4)

C16-C17-C18	125.4(5)

N9-C18-N8	125.1(5)

N9-C18-C17	113.6(5)

N8-C18-C17	121.3(5)

N10-C19-N11	124.5(5)

N10-C19-C20	119.4(5)

N11-C19-C20	116.0(5)

N12-C20-C21	122.0(5)

N12-C20-C19	114.1(5)

C21-C20-C19	123.8(5)

C22-C21-C20	119.3(6)

C22-C21-H21	120.4

C20-C21-H21	120.4

C21-C22-C23	119.0(6)

C21-C22-H22	120.5

C23-C22-H22	120.5

C24-C23-C22	119.0(6)

C24-C23-H23	120.5

C22-C23-H23	120.5

N12-C24-C23	122.3(6)

N12-C24-H24	118.9

C23-C24-H24	118.9

C1-N1-C5	118.4(5)

C1-N1-Fe1	124.9(4)

C5-N1-Fe1	114.2(3)

C6-N2-H2A	120.0

C6-N2-H2B	120.0

H2A-N2-H2B	120.0

C6-N3-N4	117.2(4)

C6-N3-Fe1	119.7(3)

N4-N3-Fe1	117.8(3)

C7-N4-N3	118.5(4)

C7-N4-Fe2	119.5(3)

N3-N4-Fe2	120.9(3)

C7-N5-H5A	120.0

C7-N5-H5B	120.0

H5A-N5-H5B	120.0

C12-N6-C8	119.3(4)

C12-N6-Fe2	121.0(3)

C8-N6-Fe2	119.1(3)

C13-N7-C17	119.4(4)

C13-N7-Fe2	120.9(3)

C17-N7-Fe2	119.6(3)

C18-N8-H8A	120.0

C18-N8-H8B	120.0

H8A-N8-H8B	120.0

C18-N9-N10	116.1(4)

C18-N9-Fe2	123.3(3)

N10-N9-Fe2	120.4(3)

C19-N10-N9	109.0(4)

C19-N11-Fe1	117.6(3)

C19-N11-Fe2	112.4(3)

Fe1-N11-Fe2	122.20(16)

C20-N12-C24	118.5(5)

C20-N12-Fe1	114.8(3)

C24-N12-Fe1	126.4(4)

N31-C31-C32	122.3(6)

N31-C31-H31	118.8

C32-C31-H31	118.8

C33-C32-C31	119.4(6)

C33-C32-H32	120.3

C31-C32-H32	120.3

C32-C33-C34	119.3(6)

C32-C33-H33	120.3

C34-C33-H33	120.3

C35-C34-C33	117.6(6)

C35-C34-H34	121.2

C33-C34-H34	121.2

N31-C35-C34	123.9(5)

N31-C35-C36	113.3(5)

C34-C35-C36	122.7(5)

N33-C36-N32	125.4(5)

N33-C36-C35	114.9(5)

N32-C36-C35	119.7(5)

N34-C37-N35	126.3(5)

N34-C37-C38	113.3(4)

N35-C37-C38	120.4(4)

N36-C38-C39	122.0(5)

N36-C38-C37	112.2(4)

C39-C38-C37	125.7(4)

C38-C39-C40	118.4(5)

C38-C39-H39	120.8

C40-C39-H39	120.8

C41-C40-C39	120.1(5)

C41-C40-H40	120.0

C39-C40-H40	120.0

C40-C41-C42	118.4(5)

C40-C41-H41	120.8

C42-C41-H41	120.8

N36-C42-C41	121.7(4)

N36-C42-C43	113.2(4)

C41-C42-C43	125.0(5)

N37-C43-C44	122.1(5)

N37-C43-C42	113.1(4)

C44-C43-C42	124.8(5)

C45-C44-C43	118.3(5)

C45-C44-H44	120.8

C43-C44-H44	120.8

C44-C45-C46	120.7(5)

C44-C45-H45	119.7

C46-C45-H45	119.7

C45-C46-C47	117.7(5)

C45-C46-H46	121.2

C47-C46-H46	121.2

N37-C47-C46	121.5(5)

N37-C47-C48	113.0(4)

C46-C47-C48	125.5(5)

N39-C48-N38	124.7(5)

N39-C48-C47	113.6(4)

N38-C48-C47	121.7(5)

N40-C49-N41	124.3(5)

N40-C49-C50	120.2(5)

N41-C49-C50	115.4(4)

N42-C50-C51	122.8(5)

N42-C50-C49	113.6(4)

C51-C50-C49	123.5(5)

C52-C51-C50	118.0(5)

C52-C51-H51	121.0

C50-C51-H51	121.0

C53-C52-C51	120.1(6)

C53-C52-H52	119.9

C51-C52-H52	119.9

C52-C53-C54	118.5(6)

C52-C53-H53	120.8

C54-C53-H53	120.8

N42-C54-C53	122.5(6)

N42-C54-H54	118.7

C53-C54-H54	118.7

C31-N31-C35	117.4(5)

C31-N31-Fe3	126.5(4)

C35-N31-Fe3	113.9(4)

C36-N32-H32A	120.0

C36-N32-H32B	120.0

H32A-N32-H32B	120.0

C36-N33-N34	115.5(4)

C36-N33-Fe3	118.6(4)

N34-N33-Fe3	117.4(3)

C37-N34-N33	118.2(4)

C37-N34-Fe4	119.9(3)

N33-N34-Fe4	120.5(3)

C37-N35-H35A	120.0

C37-N35-H35B	120.0

H35A-N35-H35B	120.0

C42-N36-C38	119.3(4)

C42-N36-Fe4	120.7(3)

C38-N36-Fe4	118.3(3)

C43-N37-C47	119.8(4)

C43-N37-Fe4	121.4(3)

C47-N37-Fe4	118.7(3)

C48-N38-H38A	120.0

C48-N38-H38B	120.0

H38A-N38-H38B	120.0

C48-N39-N40	115.8(4)

C48-N39-Fe4	123.0(4)

N40-N39-Fe4	121.2(3)

C49-N40-N39	108.5(4)

C49-N41-Fe3	117.2(3)

C49-N41-Fe4	113.4(3)

Fe3-N41-Fe4	122.14(16)

C50-N42-C54	118.0(5)

C50-N42-Fe3	116.0(3)

C54-N42-Fe3	126.1(4)

O112-Cl11-O111	111.3(3)

O112-Cl11-O114	109.8(2)

O111-Cl11-O114	110.2(3)

O112-Cl11-O113	108.1(3)

O111-Cl11-O113	109.2(3)

O114-Cl11-O113	108.0(3)

O122-Cl12-O123	110.8(3)

O122-Cl12-O121	109.0(3)

O123-Cl12-O121	110.1(2)

O122-Cl12-O124	110.6(3)

O123-Cl12-O124	107.9(3)

O121-Cl12-O124	108.5(3)

O134-Cl13-O132	109.8(7)

O134-Cl13-O133	113.8(8)

O132-Cl13-O133	108.6(7)

O134-Cl13-O131	108.2(6)

O132-Cl13-O131	106.7(5)

O133-Cl13-O131	109.5(7)

O332-Cl33-O331	110.1(17)

O332-Cl33-O334	109.8(18)

O331-Cl33-O334	111.7(19)

O332-Cl33-O333	108.6(17)

O331-Cl33-O333	111.3(18)

O334-Cl33-O333	105.2(16)

O144-Cl14-O141	111.9(3)

O144-Cl14-O143	110.2(3)

O141-Cl14-O143	107.7(3)

O144-Cl14-O142	109.6(3)

O141-Cl14-O142	108.9(3)

O143-Cl14-O142	108.6(3)

O152-Cl15-O154	112.7(5)

O152-Cl15-O151	112.0(4)

O154-Cl15-O151	108.7(3)

O152-Cl15-O153	108.1(3)

O154-Cl15-O153	107.3(4)

O151-Cl15-O153	107.8(3)

O162-Cl16-O164	110.4(4)

O162-Cl16-O163	109.6(5)

O164-Cl16-O163	109.4(3)

O162-Cl16-O161	109.7(4)

O164-Cl16-O161	107.8(4)

O163-Cl16-O161	110.0(4)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2´ 103]. The anisotropic displacement

factor exponent takes the form: -2p 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Fe1	20(1) 	27(1)	24(1) 	-1(1)	-5(1) 	-2(1)

Fe2	20(1) 	22(1)	19(1) 	1(1)	-4(1) 	-1(1)

Fe3	21(1) 	26(1)	25(1) 	-1(1)	-4(1) 	-3(1)

Fe4	18(1) 	23(1)	19(1) 	1(1)	-4(1) 	-2(1)

O1	27(2) 	31(2)	42(2) 	-7(2)	-3(2) 	-6(2)

O2	28(2) 	27(2)	26(2) 	1(2)	0(2) 	1(2)

O3	28(2) 	35(2)	76(3) 	-21(2)	-12(2) 	-3(2)

O4	23(2) 	35(2)	29(2) 	1(2)	-1(2) 	3(2)

O11	22(2) 	25(2)	28(2) 	-2(2)	-2(1) 	1(2)

O12	18(2) 	22(2)	26(2) 	0(2)	-5(1) 	-1(1)

C1	25(3) 	44(4)	35(3) 	-3(3)	-11(2) 	-1(3)

C2	18(3) 	59(4)	52(4) 	-9(3)	-7(3) 	6(3)

C3	20(3) 	43(4)	47(4) 	-6(3)	-1(2) 	2(2)

C4	26(3) 	33(3)	36(3) 	2(3)	1(2) 	4(2)

C5	24(3) 	21(3)	29(3) 	6(2)	-6(2) 	2(2)

C6	21(2) 	21(3)	28(3) 	7(2)	0(2) 	-1(2)

C7	23(2) 	24(3)	23(3) 	-1(2)	-5(2) 	0(2)

C8	25(3) 	24(3)	25(3) 	3(2)	-5(2) 	0(2)

C9	33(3) 	27(3)	27(3) 	4(2)	-7(2) 	-4(2)

C10	34(3) 	34(3)	29(3) 	1(2)	-14(2) 	1(3)

C11	31(3) 	31(3)	31(3) 	-1(2)	-12(2) 	-5(2)

C12	24(3) 	27(3)	25(3) 	-3(2)	-2(2) 	0(2)

C13	23(2) 	23(3)	23(3) 	-3(2)	-2(2) 	-2(2)

C14	33(3) 	38(3)	30(3) 	-4(3)	-5(2) 	-12(3)

C15	39(3) 	33(3)	39(3) 	-2(3)	-2(3) 	-15(3)

C16	38(3) 	27(3)	28(3) 	1(2)	5(2) 	-4(2)

C17	23(2) 	29(3)	24(3) 	-1(2)	0(2) 	0(2)

C18	22(2) 	24(3)	26(3) 	1(2)	4(2) 	3(2)

C19	19(2) 	29(3)	26(3) 	0(2)	-2(2) 	8(2)

C20	20(2) 	37(3)	22(3) 	-3(2)	-2(2) 	1(2)

C21	29(3) 	47(4)	26(3) 	6(3)	-5(2) 	-1(3)

C22	37(3) 	58(4)	21(3) 	3(3)	-5(2) 	8(3)

C23	37(3) 	63(4)	27(3) 	-12(3)	-11(3) 	-6(3)

C24	31(3) 	45(4)	31(3) 	-7(3)	-8(2) 	-2(3)

N1	19(2) 	32(3)	31(2) 	0(2)	-6(2) 	-1(2)

N2	26(2) 	36(3)	25(2) 	0(2)	0(2) 	-3(2)

N3	21(2) 	25(2)	24(2) 	6(2)	-7(2) 	-3(2)

N4	19(2) 	26(2)	24(2) 	1(2)	-7(2) 	-3(2)

N5	30(2) 	27(2)	31(2) 	7(2)	-11(2) 	-8(2)

N6	22(2) 	23(2)	20(2) 	-2(2)	-4(2) 	-4(2)

N7	21(2) 	27(2)	22(2) 	-1(2)	-2(2) 	-2(2)

N8	30(2) 	27(2)	27(2) 	5(2)	2(2) 	-2(2)

N9	23(2) 	25(2)	21(2) 	2(2)	-5(2) 	0(2)

N10	26(2) 	24(2)	22(2) 	1(2)	-3(2) 	0(2)

N11	8(2) 	13(2)	5(2) 	1(1)	-6(1) 	0(1)

N12	22(2) 	38(3)	23(2) 	-4(2)	-6(2) 	1(2)

C31	53(4) 	32(3)	31(3) 	-2(3)	3(3) 	-3(3)

C32	53(4) 	24(3)	50(4) 	-2(3)	1(3) 	-3(3)

C33	63(4) 	38(4)	37(4) 	-11(3)	8(3) 	16(3)

C34	55(4) 	31(3)	29(3) 	-1(3)	3(3) 	9(3)

C35	31(3) 	28(3)	29(3) 	0(2)	-6(2) 	7(2)

C36	29(3) 	29(3)	24(3) 	2(2)	-4(2) 	4(2)

C37	17(2) 	26(3)	21(2) 	-1(2)	0(2) 	-1(2)

C38	18(2) 	23(3)	18(2) 	1(2)	-1(2) 	0(2)

C39	22(2) 	26(3)	20(2) 	-1(2)	0(2) 	2(2)

C40	31(3) 	27(3)	21(3) 	5(2)	0(2) 	0(2)

C41	25(3) 	26(3)	24(3) 	0(2)	3(2) 	-4(2)

C42	16(2) 	28(3)	22(3) 	-1(2)	-1(2) 	-1(2)

C43	20(2) 	29(3)	22(3) 	-1(2)	0(2) 	1(2)

C44	32(3) 	29(3)	27(3) 	3(2)	-5(2) 	-7(2)

C45	28(3) 	37(3)	41(3) 	-3(3)	-8(2) 	-10(3)

C46	24(3) 	39(3)	27(3) 	-2(2)	-10(2) 	-5(2)

C47	19(2) 	28(3)	26(3) 	0(2)	-6(2) 	0(2)

C48	18(2) 	31(3)	23(3) 	-1(2)	-6(2) 	0(2)

C49	23(2) 	23(3)	22(3) 	0(2)	0(2) 	5(2)

C50	28(3) 	22(3)	24(3) 	-3(2)	3(2) 	1(2)

C51	33(3) 	33(3)	30(3) 	3(2)	2(2) 	1(2)

C52	46(3) 	28(3)	34(3) 	4(2)	10(3) 	-2(3)

C53	43(4) 	31(3)	48(4) 	0(3)	16(3) 	-9(3)

C54	34(3) 	28(3)	41(3) 	-4(3)	3(3) 	-6(2)

N31	29(2) 	28(2)	29(2) 	-2(2)	-4(2) 	-5(2)

N32	43(3) 	29(3)	32(3) 	4(2)	9(2) 	7(2)

N33	25(2) 	24(2)	22(2) 	0(2)	-6(2) 	-1(2)

N34	22(2) 	23(2)	20(2) 	0(2)	-6(2) 	-3(2)

N35	25(2) 	26(2)	24(2) 	2(2)	-5(2) 	-2(2)

N36	19(2) 	26(2)	21(2) 	-2(2)	-1(2) 	0(2)

N37	20(2) 	25(2)	20(2) 	1(2)	-4(2) 	-3(2)

N38	31(2) 	34(3)	27(2) 	3(2)	-11(2) 	-3(2)

N39	20(2) 	27(2)	24(2) 	3(2)	-2(2) 	-3(2)

N40	22(2) 	27(2)	27(2) 	3(2)	-4(2) 	-1(2)

N41	11(2) 	9(2)	9(2) 	2(1)	-4(1) 	-2(1)

N42	26(2) 	24(2)	30(2) 	-4(2)	2(2) 	-7(2)

O111	54(3) 	52(3)	25(2) 	-9(2)	-4(2) 	5(2)

O112	28(2) 	64(3)	28(2) 	6(2)	-1(2) 	14(2)

O113	51(3) 	43(2)	59(3) 	0(2)	10(2) 	-15(2)

O114	45(2) 	36(2)	28(2) 	3(2)	-4(2) 	13(2)

Cl11	28(1) 	28(1)	23(1) 	0(1)	-3(1) 	4(1)

O121	36(2) 	36(2)	35(2) 	-9(2)	-8(2) 	-5(2)

O122	46(3) 	66(3)	54(3) 	-28(2)	21(2) 	-15(2)

O123	36(2) 	32(2)	33(2) 	-1(2)	5(2) 	-7(2)

O124	53(3) 	47(3)	55(3) 	18(2)	-22(2) 	-16(2)

Cl12	30(1) 	33(1)	26(1) 	-4(1)	1(1) 	-9(1)

O131	78(5) 	71(4)	51(4) 	8(3)	-27(3) 	5(3)

O132	90(5) 	49(4)	68(4) 	7(3)	-55(4) 	-19(3)

O133	168(7) 	78(6)	127(8) 	-15(5)	1(7) 	43(6)

O134	85(4) 	94(7)	157(9) 	28(6)	-65(5) 	-54(4)

Cl13	61(2) 	47(2)	65(2) 	-6(2)	-34(2) 	-10(2)

O331	90(12) 	67(15)	118(16) 	-32(16)	-10(13) 	-42(12)

O332	69(13) 	57(8)	68(14) 	-27(9)	-1(12) 	-15(9)

O333	86(14) 	66(13)	76(9) 	-29(10)	-56(9) 	2(12)

O334	89(11) 	79(12)	91(15) 	5(15)	-52(12) 	4(11)

Cl33	72(9) 	50(8)	73(8) 	-39(7)	-15(7) 	9(7)

O141	78(4) 	63(3)	63(3) 	0(3)	4(3) 	49(3)

O142	79(3) 	48(3)	42(3) 	-2(2)	-20(2) 	-20(2)

O143	40(2) 	38(2)	38(2) 	-6(2)	-2(2) 	13(2)

O144	54(3) 	59(3)	46(3) 	-7(2)	3(2) 	-9(2)

Cl14	44(1) 	29(1)	38(1) 	-6(1)	-5(1) 	8(1)

O151	43(2) 	69(3)	41(3) 	-8(2)	-13(2) 	-15(2)

O152	75(4) 	50(3)	145(5) 	18(4)	56(4) 	12(3)

O153	73(4) 	50(3)	106(4) 	14(3)	34(3) 	10(2)

O154	73(4) 	179(7)	46(3) 	26(3)	-33(3) 	-60(4)

Cl15	31(1) 	55(1)	36(1) 	6(1)	-6(1) 	-4(1)

O161	60(3) 	38(2)	92(4) 	9(2)	1(3) 	9(2)

O162	123(5) 	70(4)	149(6) 	-2(4)	87(5) 	-25(4)

O163	67(4) 	105(5)	75(3) 	-7(3)	-19(3) 	17(4)

O164	89(3) 	78(4)	38(3) 	1(3)	5(2) 	53(3)

Cl16	54(1) 	41(1)	62(1) 	13(1)	18(1) 	14(1)

O201	45(2) 	28(2)	26(2) 	-1(2)	-9(2) 	-4(2)

O202	43(3) 	73(4)	68(3) 	-10(3)	16(2) 	-1(3)

O203	59(3) 	103(5)	40(3) 	-14(3)	14(2) 	-21(3)

O204	82(4) 	52(3)	53(3) 	13(2)	8(3) 	-16(3)

O205	61(3) 	59(3)	50(3) 	-4(2)	-3(2) 	15(3)

O206	250(20) 	138(15)	171(17) 	3(13)	13(15) 	-112(15)

Table 5. Hydrogen coordinates [´ 104] and isotropic displacement parameters [Å2 ´ 103].

Atom 	x	y	z	Ueq	S.o.f.

H1	12173	2511	9452	43	1

H2	13572	2729	9097	52	1

H3	13641	2798	8192	45	1

H4	12340	2540	7637	38	1

H9	7405	2612	6770	35	1

H10	6201	1892	6464	39	1

H11	5958	866	6905	38	1

H14	5937	-139	7359	41	1

H15	6009	-1095	7904	44	1

H16	6930	-1078	8692	37	1

H21	9755	870	10481	41	1

H22	10445	1508	11171	47	1

H23	11007	2600	10994	51	1

H24	10953	2985	10131	43	1

H2A	10131	1848	7299	35	1

H2B	11170	1906	7328	35	1

H5A	9372	3173	7533	36	1

H5B	8540	3139	7141	36	1

H8A	8434	-406	9731	33	1

H8B	7758	-858	9411	33	1

H31	7901	5328	9201	46	1

H32	7413	6150	9778	51	1

H33	6813	5813	10560	55	1

H34	6584	4641	10716	46	1

H39	7580	830	10538	28	1

H40	6694	-137	10321	32	1

H41	5663	-119	9580	30	1

H44	4637	63	8865	35	1

H45	3830	291	8065	43	1

H46	4140	1283	7593	37	1

H51	6929	4226	7387	39	1

H52	7932	5108	7201	43	1

H53	9130	5392	7813	48	1

H54	9246	4835	8622	41	1

H32A	6234	2922	10385	41	1

H32B	6014	3647	10548	41	1

H35A	8257	2582	10540	30	1

H35B	8159	1832	10681	30	1

H38A	5206	2878	7308	38	1

H38B	4586	2254	7277	38	1